## Slide 1: Bar Measurement Results during Material Screening
PANDA week June 2023, Prague, Czech Republic Georg Schepers

## Slide 2
Georg Schepers– March 2023
Storage of the Bars in Horseshoes

## Slide 3
Georg Schepers– March 2023
QA @ GSI: Nikon Bar Surface Roughness
Determination of the surface roughness H
with help of the internal reflectivity R of
6 laser wave lengths
via Scalar Scattering Theory (dotted lines)
Laser setup

## Slide 4
Georg Schepers– March 2023
Material Screening Measurements
Distribution of Transmission after 48 internal Reflections

## Slide 5
Georg Schepers– March 2023
Material Screening Measurements
Laser Setup
Material Screening setup
Same bar holder is used in the Laser setup as in the Material screening setup
No manipulation of the bar surface needed
Only faces of the bars accessible

## Slide 6
Georg Schepers– March 2023
Bar holder and Support for Material Screening
Mark
3D printed support
Storage in sledge
under heap-filter

## Slide 7
Georg Schepers– March 2023
New Material
Prototype CFRP in the Tube #3
ca. 0.4 m2 Surface
(Bar box ca. 1 m2)

## Slide 8
Georg Schepers– March 2023
Reflectivity Measurements
Nikon Bar #21 stays in Nitrogen air flow only (Reference bar)
Nikon Bar #41 stays in Nitrogen air flow over large amount of “Common” CFRP
Nikon Bar #61 in Nitrogen air flow over “Prototype” CFRP
Longer periods (several months) in the material screening setup needed
P-CFRP in
P-CFRP in
Ref in

## Slide 9
Georg Schepers– March 2023
Reflectivity Measurements
Nikon Bar #21 stays in Nitrogen air flow only (Reference bar)
Nikon Bar #41 stays in Nitrogen air flow over large amount of “old” CFRP
Nikon Bar #61 about to go into Nitrogen air flow over “original” CFRP
Longer periods (several months) in the material screening setup needed
Nov. 22
Feb. 23
March 23
3 days
14 days
Dez. 22
Time in the
Material screening
setup

## Slide 11
Georg Schepers– March 2023
Nikon Bar #21 stays in Nitrogen air flow only (Reference bar)
Nikon Bar #41 stays in Nitrogen air flow over large amount of “old” CFRP
Nikon Bar #61 about to go into Nitrogen air flow over “original” CFRP
Longer periods (several months) in the material screening setup needed
PANDA Technical Notes in preparation
Summary and Outlook

## Slide 12
Backup slides

## Slide 13
Georg Schepers– March 2023

## Slide 14
or 120000
Stefan Koch
Carbon Fiber vs Aluminum