## Slide 1
Radiation Tolerance of CMOS Sensors
Dennis Doering*, Michael Deveaux,
Benjamin Linnik, Stefan Strohauer and Joachim Stroth
for the CBM-MVD Collaboration
Goethe University Frankfurt am Main, Germany
*supported by BMBF (06FY9099I, 06FY173I and 05P12RFFC7),
GSI (F&E) and HIC for FAIR
CMOS Monolithic Active Pixel Sensors (MAPS)
PHD physics day
August 2013
The (P++, P, P++) doping of the MAPS sensor generates a potential minimum in the region of the epitaxial layer. Impinging particles excite electrons which diffuse within this region until they are collected by the P-Epi/N-Well diode.
Contact: doering@physik.uni-frankfurt.de
The Compressed Baryonic Matter (CBM) experiment at FAIR will explore the nuclear phase diagram in the region of highest net-baryon densities at moderate temperatures. One of the promising probes is open charm which will be identified by reconstructing their secondary vertex with 50 µm precision.
Sensor requirements for CBM@SIS-100:
- 5 µm spatial resolution
- 0.05 % X0 material budget (sensor only)
- 30 µs time resolution
- Power dissipation: ~350 mW/cm²
- Ionizing radiation tolerance: 1-3 Mrad
- Non-ionizing radiation tolerance: 1013 neq/cm²
The CBM-experiment (at FAIR)
Primary Beam: 25 AGeV Au Ions (up to 109/s)
Primary
vertex
Secondary
vertex
Short lived particle
D0 (ct = ~ 120 µm)
Detector 1
Detector2
Target
(Gold)
Z=5cm
Reconstruction concept for open charm
Conclusion: MAPS based on a 0.18 µm-CMOS process with a (1 kΩcm) high-resistivity epi-layer provide the radiation hardness needed for the next generation Heavy Ion experiments.
The Heavy Ion Experiment CBM
The Task
MAPS are pixel sensors for charged particle tracking. Their small pitch of 10 – 40 µm and 50 µm thickness provides excellent spatial resolution of a few µm.
Performance in beam
CBM radiation requirements fulfilled
Excellent detection efficiency of >99.5% despite of irradiation
Track of a particle
SiO2
-
-
P-Well
Epitaxial
Layer
Substrate
Diode
N+
P+
P-
P+
Pixel pitch: 10-40 µm
50 µm
Radiation damage in MAPS
Track of a particle
-
-
Surface damage
(ionizing radiation)
Bulk damage
(non-ionizing radiation)
Leakage current
due to surface damage
Leakage current
due to bulk damage
Signal recombinations
due to bulk damage
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
+
-
-
-
-
-
-
-
-
IPHC Strasbourg
-70 % leakage current
No reverse annealing
D.Doering et al. Annealing studies on X-ray and neutron irradiated CMOS MAPS, NIM-A 2011
Cooling helps
D.Doering et al. Pixel pitch dependence of the tolerance of CMOS MAPS to non-ionizing radiation, NIM-A 2013
Improved non-ionizing rad. tol.: High-resistivity and/or smaller pitch
High initial noise is currently under further study, maybe due to not yet optimized transistor layout
Tolerance to ionizing radiation
Tolerance to non-ionizing radiation
Thermal annealing
Sufficient S/N even after 10 Mrad