## Slide 1: Update on PANDA solenoid design and analysis
Gabriella Rolando
Helder Pais Da Silva
Herman ten Kate
Alexey Dudarev
3 November 2014

## Slide 2: Outline
Part I
  Conductor procurement status
  New conductor layout
  New coil layout
  Field quality & pressure on the coils
  Eddy current loss in the coil windings
  Eddy current loss in the casing
  Temperature distribution in the cold mass
  Shear stress at the coil-casing interface
Part II
  Coil cross-section
  Coil winding
  Coil and support cylinder analytic stress assessment
  Support cylinder dimensions
Pro’s & con’s of the new coil design
Conclusion
2

## Slide 3
Part I
  Conductor procurement status
  New conductor layout
  New coil layout
  Field quality & pressure on the coils
  Eddy current loss in the coil windings
  Eddy current loss in the casing
  Temperature distribution in the cold mass
  Shear stress at the coil-casing interface
3

## Slide 4: Conductor procurement status
Furukawa’s price offer of August 29 of 191 $/m; still 36% higher than expected.
Furukawa reported the unit length (max 3200 m ) as main price driver.
New quotation requested for 4 x 1600 m and 1 x 1500 m unit lengths on September 17.
On October 1, Furukawa replied that price will decrease further towards the expected target (120-140 $/m), although it would probably not reach the cost of the DS1 conductor (Mu2e experiment) due to the larger cross-section area. However, a number was not given.
A budgetary offer has been requested on October 21; for the 6-around-1 conductor. According to Furukawa price will likely not vary due to R&D required for Al-stabilized 6-around-1 conductor.
On October 31 , Furukawa replied and stated no significant cost reduction expected on 6-a-1 cable (no experience, R&D required). We will now propose the new conductor size with an 8 strands Rutherford cable instead.
For starting of real tender, still waiting for confirmation of tendering partner and budget.

## Slide 5: New conductor layout
Driving factors in conductor design:
  Minimize the risk of quenches temperature margin ΔT ≈ 2.4 K.
  Ease the coil winding low height-to-width ratio conductor
Parameter | TDR | Modified TDR | 6-around-1 |  | New Rutherford
Layout | - |  |  |  | 
N. of strands | 20 | 26 | 6 + 1 core* | 8 | 
Strand diameter [mm] | 0.8 |  | 1.5 | 1.4 | 
Cu : nonCu ratio | 1.5 | 1.2 | 1.0 | 1.0 | 
Cable dimensions [mm] | 8 x 1.15 | 9.7 x 1.5 | Ø 4.5 | 2.6 x 5.3 | 
Conductor bare dimensions [mm] | 24.6 x 3.4 |  | 7.9 x 10.9 |  | 
ΔT [K] | 1.8 | 2.4 | 2.3 | 2.4 | 
* Core material options: Cu, Al, SS

## Slide 6: New coil layout
Parameter | TDR | Modified TDR | 6-around-1 | Rutherford
Iop [kA] | 5 |  | 4.98 | 
Inner radius [mm] | 1050.0 |  | 1050.1 | 
Outer radius [mm] | 1100.0 |  | 1099.9 | 
Layers / coil | 2 |  | 6 | 
Up-stream coil | -1025.0 < z < -143.4 [mm] |  | -1024.9 < z < -143.5 [mm] | 
 | Turns = 464 |  | Turns = 468 | 
Center coil | 157.4 < z < 552.6 [mm] |  | 162.9 < z < 547.1 [mm] | 
 | Turns = 208 |  | Turns = 204 | 
Down-stream coil | 853.4 < z < 1735.0 [mm] |  | 853.5 < z < 1734.9 [mm] | 
 | Turns = 464 |  | Turns = 468 | 

## Slide 7: Field quality & pressure in the coils
Comparison of field quality in tracker region for the different conductor designs.
6 layers layout result in better field quality and lower peak field.
Design |  | Bpeak [T] | ¦δ¦max [%] | Intmax [mm]
Criterion: |  | - | < 2.0 | < 2.00
Modified TDR |  | 2.9 | 1.69 | 2.05
New design | 6-around-1 | 2.71 | 1.67 | 1.75
 | Rutherford | 2.75 | 1.60 | 1.76
Design |  | Max Faxial [MN] | Max Paxial [MPa] | Max Fradial [MN] | Max Pradial [MPa]
Modified TDR |  | 4.0 | 11.8 | 17.2 | 2.9
New design | 6-around-1 | 3.9 | 11.6 | 17.2 | 2.9
 | Rutherford | 3.9 | 11.6 | 17.2 | 2.9
Maximum axial and radial pressure on a sub-coil.
  TDR values are confirmed.

## Slide 8: Eddy current loss in the coil windings
Eddy currents in a rectangular thin plate
Parameter | TDR design | New design
Bpeak [T] | 3 | 3
ρAl @ 4.5 K [Ω·m] RRR = 1000 | 2.480 e-11 | 2.480 e-11
tramp [s] | 1500 | 1500
Peddy [W] | 5.2 | 0.6
tramp [s] | 2000 | 2000
Peddy [W] | 2.9 | 0.3
Conservative estimate:
  B = Bpeak on all the turns
  No magneto-resistance
The low height-to-width ratio conductor features practically zero loss for every ramp time.
Eddy current loss with TDR design add an extra 30% on top of casing loss.
What is the required current ramp time?

## Slide 9: Eddy current loss in the casing
Parameter | TDR design | New design
I [kA] | 5 | 4.98
ρAl-5083 @ 4.5 K [Ω·m] | 3.03e-8 | 3.03e-8
tramp [s] | 1500 | 1500
Peddy [W] | 17.4 | 17.2
tramp [s] | 2000 | 2000
Peddy [W] | 9.78 | 9.7
Eddy currents in the casing produce the main loss contribution during ramp & slow dump.
Eddy current power loss is reduced of ~ 2 when ramp time increases from 1500 s -> 2000 s.

## Slide 10: Temperature distribution in the cold mass
Cooling channels
Pure Al strip
coil
coil
coil
casing
Insulation
Steady-state thermal model of the cold mass during ramp up & slow dump
Features
  6 cooling channels
  1.5 mm thick high purity Al strips in thermal contact with the cooling channels and surrounding the 3 sub-coil modules

## Slide 11: Temperature distribution in the cold mass
Design | Tramp [s] | Tpeak [K]
TDR | 1500 | 4.57
TDR | 2000 | 4.54
New | 1500 | 4.56
New | 2000 | 4.54
The thin high purity Al strip in thermal contact with the cooling ribs ensures minimal increase of the cold mass temperature during current ramp up and slow dump of the magnet.
Loads
  Eddy current loss in the conductor
  Eddy current loss in the casing
  Radiation heat flux 0.12 W/m2
  (based on ATLAS CS data)

## Slide 12: Shear stress at the coil-casing interface
Design | Peak shear stress at coil-casing interface [MPa]
With spacers | 3
Without spacers | ≈10
Maximum epoxy shear stress 30 MPa.
Maximum shear stress at coil-casing interface below epoxy limit even without spacers between the coils.
TDR values are confirmed.
Magneto-structural model of the cold mass at operating current
casing
coil
coil
coil
coil
coil
coil
casing
Shear stress distribution in the cold mass

## Slide 13
Part II
  Coil cross-section
  Coil winding
  Analytic stress assessment
  Support cylinder dimensions

## Slide 14: Coil cross-section 1/2
Update:
Two flanges and one support cylinder per sub coil
Layer of G10 to compensate for winding and cable tolerances
Sliding interface between coil and flanges

## Slide 15: Coil cross-section 2/2
Update:
Two flanges and one support cylinder per sub coil
Layer of G10 to compensate for winding and cable tolerances
Sliding interface between coil and flanges
High purity aluminum strips to improve cooling

## Slide 16: Coil winding
A vertical winding set-up is preferable.
A simple collapsible mandrel will be designed for our purpose.
One of the coil flanges will be connected initially to the winding mandrel.
The cable winding is “transposed”, using joggles in every turn.

## Slide 17: Analytic stress assessment 1/3
Without external support the coil windings will yield.
Bare coil under radial magnetic force
Parameter | Value
Hoop stress [MPa] | 62
Hoop stress [MPa] | 59
Radial stress [MPa] | -2.9
Radial stress [MPa] | 0
Max. von Mises stress [MPa] | 64
Safety factor | 0.63
Parameter | Value
 | 62
 | 59
 | -2.9
 | 0
Max. von Mises stress [MPa] | 64
Safety factor | 0.63

## Slide 18: Analytic stress assessment 2/3
40 mm support cylinder with no contact pressure at cold
Parameter | Coil | Casing
Contact pressure [MPa] | 1.240 | 
Hoop Stress [MPa] | 34 | 33
Hoop Stress [MPa] | 35 | 33
Radial Stress [MPa] | -2.9 | 1.2
Radial Stress [MPa] | -1.2 | 0
Max. von Mises stress [MPa] | 36 | 35
Safety factor | 1.1 | 4.1
[mm] | 0.47 | 0.48
[mm] | 0.48 | 0.47
Parameter | Coil | Casing
Contact pressure [MPa] | 1.240 | 
 | 34 | 33
 | 35 | 33
 | -2.9 | 1.2
 | -1.2 | 0
Max. von Mises stress [MPa] | 36 | 35
Safety factor | 1.1 | 4.1
 | 0.47 | 0.48
 | 0.48 | 0.47
Support Cylinder
Coil
A 40 mm thick support cylinder allows operating the coil close to yielding of the conductor.
Contact Pressure

## Slide 19: Analytic stress assessment 3/3
40 mm support cylinder with 0.7 mm overlap
Support Cylinder
Coil
Pre-stress required to increase the safety factor to 1.5 is small.
The thickness could be reduced, but 40 mm is ideal for assembly purposes.
Required T between bodies for assembly ≈90 K.
Contact Pressure
 | Warm Magnet |  | Cold Magnet |  | Energized Magnet | 
 | Coil | Support Cylinder | Coil | Support Cylinder | Coil | Support Cylinder
Overlap [mm] | 0.7 |  | 0.5 |  | 0.5 | 
Contact Pressure [MPa] | 0.90 |  | 0.73 |  | 1.97 | 
Max. von Mises stress [MPa] | 20 | 26 | 16 | 21 | 20 | 56
Safety factor | 1.5 | 5.6 | 2.4 | 7.0 | 2.0 | 2.6
 | Warm Magnet |  | Cold Magnet |  | Energized Magnet | 
 | Coil | Support Cylinder | Coil | Support Cylinder | Coil | Support Cylinder
Overlap [mm] | 0.7 |  | 0.5 |  |  | 
Contact Pressure [MPa] | 0.90 |  | 0.73 |  |  | 
Max. von Mises stress [MPa] | 20 | 26 | 16 | 21 |  | 
Safety factor | 1.5 | 5.6 | 2.4 | 7.0 |  | 
 | Warm Magnet |  | Cold Magnet |  | Energized Magnet | 
 | Coil | Support Cylinder | Coil | Support Cylinder | Coil | Support Cylinder
Overlap [mm] | 0.7 |  |  |  |  | 
Contact Pressure [MPa] | 0.90 |  |  |  |  | 
Max. von Mises stress [MPa] | 20 | 26 |  |  |  | 
Safety factor | 1.5 | 5.6 |  |  |  | 

## Slide 20: Support cylinder dimensions
 | Coil |  | Cylinder | 
 | [mm] | [mm] | [mm] | [mm]
Energized magnet | 1045.1 | 1094.9 | 1094.9 | 1134.7
Cold magnet | 1044.6 | 1094.4 | 1094.4 | 1134.2
Cold separated components | 1044.8 | 1094.7 | 1094.2 | 1134.0
Warm | 1049.3 | 1099.4 | 1098.7 | 1138.7
Winding radius (10 MPa tension) | 1049.8 | 1099.9 | - | -
 | Coil |  | Cylinder | 
Energized magnet | 1045.1 | 1094.9 | 1094.9 | 1134.7
Cold magnet | 1044.6 | 1094.4 | 1094.4 | 1134.2
Cold separated components | 1044.8 | 1094.7 | 1094.2 | 1134.0
Warm | 1049.3 | 1099.4 | 1098.7 | 1138.7
Winding radius (10 MPa tension) | 1049.8 | 1099.9 | - | -
Cold dimensions of the coil and cylinder depend on:
Material properties
Initial dimensions of the components
Interference length
Notes:
The warm dimensions and interference of the components will be adjusted to compensate for non-conformities.
A 3D FEM stress analysis is needed to assess behavior near the coil ends.
A dummy coil will be first produced to test the coil winding and assembly procedure.

## Slide 21: Pro’s & con’s of the new coil design
Pro’s
  Easier co-extrusion process.
  Easier winding and cheaper winding tooling.
  Lower loss in the conductor during ramp up and slow dump.
  Improved field quality on tracker region.
  Lower peak field on the conductor.
Con’s
  Potentially higher temperature gradient on the coil due to the higher number of layers
…but
  The issue is not relevant when the sub-coil modules are surrounded by thin high purity Al strips in thermal contact with the cooling ribs.

## Slide 22: Conclusion
  The 6 layers winding solution is recommended as it allows easier manufacturing and cost reduction.
  The presence of a high thermal gradient over the winding during current ramp up/down is effectively avoided by surrounding the sub-coil modules with a thin high purity Al strip in thermal contact with the cooling ribs.
  The TDR value for the maximum axial and radial pressure on a sub-coil are confirmed.
  The TDR value for the maximum shear stress at the coil-casing interface is confirmed.
  The eddy current loss during ramp up and slow dump are assessed and in agreement with the TDR value for tramp = 2000 s and a coil former thickness of 30 mm.
  A budgetary offer for the 6-around-1 conductor has been requested to Furukawa. Price is comparable to 26 strands Rutherford.