## Slide 1: Materials research applications with high intensity laser driven proton beams
M. Tomut
GSI Helmholtzzentrum für Schwerionenforschung

## Slide 2
Materials research with laser driven proton beams:
response of accelerator target materials to short, intense particle beams pulses
ground testing of space materials and electronics in complex radiation environments
defect dynamics studies in irradiated materials
proton beam radiography of transient phenomena

## Slide 3: Accelerator components exposed to high intensity ion beams
360 MJ proton beam
1.2 m
Collimators
slow beam loss at 7 TeV:
1% of beam over 10 s –
500 kW
Accidental beam impact:
2 MJ/mm2 in 200 ns (0.5 kg TNT)
LHC

## Slide 4: Novel composite materials solution with improved thermal conductivity and mechanical robustness
Courtesy of A. Bertarelli
Cu-CD composite
Mo-CD composite
Mo-Gr composite
Mo-Gr/Mo sandwich
Notes: Mo-Gr with c oating C (per ridurre impedenza)

## Slide 5: Designing and testing new materials for high power targetry applications
Materials ranking by Figure of Merit
calculated based on material properties at room temperature, low strain rates, non-irradiated
experimental validation required

## Slide 6: Existing facilities
HighRadMat - High Radiation to Materials
Maximum specific energy deposition
in tungsten:
~ 7 KJ/g
(FLUKA calculation- source N. Tahir)

## Slide 7: HiRadMat- CERN: High Intensity Tests
    Inermet 180, 72 bunches
  Molybdenum, 72 & 144 bunches
  Glidcop, 72 bunches (2 x)
  Copper-Diamond
  144 bunches
  Molybdenum-Copper-Diamond 144 bunches
  Molybdenum-Graphite (3 grades)
  144 bunches
Experiments:
Thermal management
Pressure waves
Radiation damage
Designed for single-pulse experiments
long irradiation –excluded due to beam sharing & activation
Application :
•machine components
protection devices
targets
material studies
detector testing
electronics

## Slide 8: UNILAC, GSI- short pulse 4.8 MeV/u U beams
Beam parameters
  4.8 MeV/u U28+;; 0.15 ms pulse length; 1 Hz
  Up to 1.5×1010 i/cm2 per pulse
  Up to fluences of 1×1014 i/cm2
IR camera
LDV
Material response to beam-induced stress waves with radiation damage accumulation
Polycrystalline isotropic graphite 140 μm
Temperature - beam spot
Existing facilities

## Slide 9: Experimental set-up for measuring proton beam induced stress waves

## Slide 10: Response of accelerator target materials to short, intense proton beam pulses
Chart: 
time (s)
velocity (m/s)

## Slide 11
Ground testing of space materials in conditions similar to natural environment probed by satellites
Cosmic radiation and solar particle events includes protons, helium and heavier ions, and also electrons, neutrons, and ultraviolet radiation
Complex radiation environment might have a synergistic effect on materials damage
The energy spectrum of laser accelerated particles is quite similar to the natural one - exponential energy distribution
This condition is difficult to achieve by traditional accelerator facilities
Vacuum and extreme temperatures as well as thermal cycling alter physical properties and lead to material fatigue.
Impacts of micro-meteoroids and orbiting man-made debris can damage spacecrafts and components.

## Slide 12: Ground testing of space components
cummulative effects of mixed proton and ion irradiation can be tested at Z6 at lower energies and in the future at the APPA-Helmholtz beamline at higher energies
Proton fluences on Mars for SPE‘s
(source NASA technical paper)

## Slide 13: Ground testing of space components
  optical crystals and solar cell materials
  composite and polymeric materials for space technologies
  electronic components for cummulative dose effects
  cell cultures

## Slide 14: Dynamics of radiation induced defects in materials
in situ study of :
-defect recovery and clustering, effect of dose rate
-phase transformation ,
-and ion track formation
Fast diagnostic:
time resolved laser transmission, reflection, absorption, X-ray spectroscopy, RBS, optical spectroscopy, resistometry
~10 nm
fs-ps
ps - µs - h

## Slide 15: Conclusions and outlook
possible experiments are limited at the moment by the repetition rate - at the moment focus on single shot experiments
for studies on materials response to pressure waves –one could trade the narrow energy spread for intensity
need for fast probing beams: laser, VISAR, (laser driven) X-ray .. positron sources
.. if possible also with high repetition rate
heavier ions- Au, Pd?
LIGHT facility at Z6 can be a test bench for future experiments combining high energy ion beams and laser driven proton beams at APPA cave + Helmhotz beamline