## Slide 1
The beam halo requirements of CBM
… and what is being done to relax them.
M. Deveaux, Goethe University Frankfurt
on behalf of the CBM collaboration.

## Slide 2: Introduction: Beam damage in the STAR-PXL
Beam
One half of The STAR-PXL detector.
G. Contin, the STAR collaboration, 2016 JINST 11 C12068
Operation experience with the STAR-PXL (2014):
Loss of 14% of sensors (inner layer) within 2 weeks.
Anticipated origin: Impact of heavy beam ions (halo).
Solved by modifying existing protection system.
2014
Related system tests and existing latch-up protection strategy did not avoid incident.

## Slide 3: Outline
The CBM-MVD: Geometry and sensors.
Ion radiation damage in CMOS devices.
MVD sensor protection strategy.
Requirements on the beam.

## Slide 4: The MVD region (not to scale)
Main concern:
Radiation damage in sensors.
Worst case:
Sudden death of sensors.
Main concern:
Secondary reactions
Worst case:
See secondaries instead of physics
Beam pipe
MVD-stations
Vacuum window
Silicon tracking system
Silicon tracking system
Our topic today
Electronics
Beam pipe
z=12 cm
Target

## Slide 5: CMOS Monolithic Active Pixel Sensor (MAPS)
MIMOSA-26
Pixel
Sensitive to integrated radiation damage.
On-chip computer (etc.)
Mostly sensitive to sudden (Single Event) Effects.
Radiation hardening techniques exist in both fields…
… but will not do miracles.
 | MIMOSIS design goal
Spatial resolution | ~5 µm
Time resolution | 5 µs
Pixel Pitch | 30x27µm²
Thickness | 50 µm
Rad. tolerance | ~ 3Mrad
 | 3 x 1013neq/cm²

## Slide 6: Using a MAPS as beam monitor…
Test carried out by the NA61/SHINE collaboration.
SPS primary beam (30 AGeV Pb)
An Au-ion creates ~6200 x more ionization than a proton.
More radiation damage.
More charge at unwanted places (e.g. in memory cells)
1152 pixel, 2.1 cm
574 pixel, 1.1 cm
MIP (proton)
~2 pixels
~2x2 mm
Heavy ion:
~200 pixels

## Slide 7: On “sudden damage”
Impact of ions
Single event effect
Latch up
Integrated damage
Ionizing (TID)
Non-Ionizing
Single event upset
(e.g. bit flip)
“Sudden damage” in digital electronics
“Slow damage” in sensors

## Slide 8: What do we know on latch up?
Latch up:
Ion creates short circuit in vulnerable CMOS-structures.
Reversible, may be cured by power cycling.
No power cycling => Thermal destruction of the device.
Created the STAR-incident.
  Automatic power cycling installed but initially too high reaction threshold.
  Reason: Thin sensors more vulnerable than the thick ones used for test.
Vulnerable structure: e.g CMOS inverter.
Situation at CBM:
MIMOSIS might be immune to this (operates at 1.8V instead of 3.3V).
MVD will be equipped with improved latch-up protection hardware.
Should avoid sensor losses. Still system up-time might be affected.
G. Contin, 2016 JINST 11 C12068

## Slide 9: What do we know about bit-flips?
B Abelev et al and The ALICE Collaboration 2014,
J. Phys. G: Nucl. Part. Phys. 41 087002
What is done about it at CBM:
All important steering units of MIMOSIS will be carried out in triple-vote-logic.
Sensor may detect and correct individual bit flips e.g. by reset.
Data memories are not protected
Data may be corrupted. Impact on over all data quality is marginal.
Should avoid system fail. Still system down-time for recovery may add up… .
Bit flips in CMOS devices
Vulnerability depends on CMOS
process and memory design.
Results for MIMOSIS-like devices
exist for protons.
Tests for ions pending. Expect higher rates.

## Slide 10: “Slow” radiation damage
Impact of ions
Single event effect
Latch up
Integrated damage
Ionizing (TID)
Non-Ionizing
Single event upset
(e.g. bit flip)
“Sudden damage” in digital electronics
“Slow damage” in sensors

## Slide 11: Integrated damage
To be measured and improved: Radiation hardness against…
Ionising radiation:
Energy deposited into the electron cloud.
May ionise atoms and destroy molecules.
=> Damage in transistors and photo diodes.
Non-ionising radiation:
Energy deposited into the crystal lattice.
Atoms get displaced.
=> Damage in photo diodes.
Farnan I, HM Cho, WJ Weber, 2007. "Quantification of Actinide α-Radiation
Damage in Minerals and Ceramics." Nature 445(7124):190-193.
Both damage mechanisms add up.
=> Must validate immunity to each individual damaging mechanism.

## Slide 12: Integrated damage (non-ionizing)
M. A. Xapsos, et al., IEEE TNS
Vol. 51 (2004), P. 3250-3254
Few knowledge, mostly theory calculations for space/satellite community.
CBM energy range not covered, guess work based on extrapolation done (initially for NA61/SHINE).
Results suggests:
Pb-hardness factor .
No empiciral data available (to the best of my knowledge) => Tests needed.
=> Test campaing started together with NA61/SHINE at the CERN/SPS

## Slide 13: Integrated damage (non-ionizing)
Location:
200m upstream
NA61 target.
Radiation tolerant positioning table
MIMOSA-34THR
Tower/Jazz 0.18µm CMOS
Dosimetry:
4x4mm² scintillator
Dose reached:
1.2x1010 Pb/cm² (30A GeV/c)
Result: Conversion factor confirmed (1 Pb-Ion < 300 neq/cm²)

## Slide 14: Integrated damage (ionizing)
Projectile charge
Dose:
Holds for “minimum ionizing particles”, expect higher damage e.g. for target fragments (not covered today).
Idea:
Rely on Bethe-Bloch-Equation.

## Slide 15: Maximum halo rates allowed (normal operation)
Most exposed detector – MVD:
Max. 100 kHz Au-Au or 10 MHz p-Au (collision rate).
=> Beam intensity 107 Au/s, 109 p/s with 1% interaction target.
Integrated damage must not exceed 30% of projected sensor radiation tolerance within 1 year of operation.
 | Protons | Au-ions
Max. flux (to respect ioninzing dose limit). | 60 kHz/mm² | 10 Hz/mm²
Max. flux (to respect non-ioninzing dose limit). | 1.8 kHz/mm² | 60 Hz/mm²
Limit | 1.8 kHz/mm² | 10 Hz/mm²
Must be fulfilled for r=5mm from the nominal beam axis at z=5-12 cm behind the CBM target. Also in case the beam moves!

## Slide 16: Requirement vs. information on beam
Beam diameter 2mm @ 4 AGeV
Assume Gaussian profile.
J. Pietraszko: “CBM+HADES in FAIR Beam Parameter Booklet”, CBM Technical Board, 4. Sept. 2018.
J. Pietraszko, The Slow Extraction Workshop, Darmstadt, 1-3 June 2016
SIS18, HADES beam monitoring.
Note: Option of additional collimation (next talk) ignored.

## Slide 17: Why I got worried…
Sensor
Sensor
Uncertainties:
About factor 3
Radiation from beam
as requested.
Radiation from
CBM physics
Width of sensor
Extrapolation
Radiation doses in both scenarios exceed the limit by orders of magnitude.
Beyond reach of sensor design => Help from accelerator community needed.
Gauß
Scaled to 10 MHz Au beam.

## Slide 18: Beam loss to detector
Beam pipe
MVD-stations
Vacuum window
Beam pipe
Silicon tracking system
Silicon tracking system
Beam
The worry:
Beam steering fail => Detector is hit by full beam.
Consequences => Somewhat unknown (nothing to permanent fail).
Target

## Slide 19: Measures for beam loss protection (beam tuning)
Beam pipe
MVD-stations
Vacuum window
Beam pipe
Silicon tracking system
Silicon tracking system
MVD will be equipped with moving engine:
Power down and move out sensors during beam tuning.
Movement will be slow (few minutes).
Path to safe position should be minimized (major space concern).
100 mm
Target

## Slide 20: Sensors – reaction to beam
MIMOSA-26 operated in direct SPS 30 AGeV Pb beam for ~24h
Observation @few kHz beam intensity:
No obvious loss of functionality.
Observed 3 latch-ups. One persisted several hours before discovery. Chip recovered after power cycling.
Sensor surprisingly robust. But test represents ~1 spill CBM.
=> Need to scale to CBM.

## Slide 21: Beam impact studies (emergency stop)
Idea:
Sensor tolerates charge of one ion at any point.
Assume no charge evacuation (time scale unknown).
Avoid overlaping hits by emergency beam stop.
Open issue:
To what surface is the charge of an ion distributed?
Input:
Rough estimate: Most ion charge is concentrated in r=15µm.

## Slide 22: Beam impact studies (emergency stop)
Assume beam with .
Maximum allowed number of Au - ions:
Shut within 140 µs needed.
Obvious: High uncertainties, includes corse assumptions on
device physics and beam focusing...
Preliminary conclusion: Very fast beam abort system is required.
Note: Collimator, which defocuses/fragments the beam would already help (reduces z)

## Slide 23: Summary and conclusion
Requirements on beam parameters (halo) were presented:
Numbers driven by needs of CBM-MVD (avoid destruction).
Numbers account for design safety features of MVD:
  Advanced tolerance of sensors to integrated damage.
  Latch-up protection system.
  Triple vote logic for important sensor sub-systems.
  Option to move sensors to safe position during beam tuning.
 | Protons | Au-ions
Limit | 1.8 kHz/mm² | 10 Hz/mm²
Resonable precision
Reaction time for beam loss to detector: ~100 µs
Poor precision
Options of the detector community are mostly exhausted
=> Help from accelerator community is required.
Beam halo limits for regular operation (r=5mm from beam axis):
Try to hit the target… and nothing else 

## Slide 24: Radiation damage by ions in CMOS sensors
Impact of ions
Single event effect
Latch up
Integrated damage
Ionizing (TID)
Non-Ionizing
Single event upset
(e.g. bit flip)
“Sudden damage” in digital electronics
“Slow damage” in sensors