## Slide 1: Thermo-mechanical modeling of high energy particle beam impacts
M. Scapin*, L. Peroni*, A. Dallocchio**
* Politecnico di Torino, Corso Duca degli Abruzzi, 24, 10129 Torino, Italy
** Mechanical and Materials Group, Engineering, CERN, CH-1211 Geneva 23, Switzerland

## Slide 2: Contents
Introduction
Problem definition
Material data
Numerical modeling
Results
Results comparison and discussion
Conclusions

## Slide 3: The problem
Objectives:
Numerical simulation of a complex mechanical structure (collimator) subjected to beam impact: energy deposition, shock waves, damage …
Numerical code: LSDyna
General purpose transient dynamic finite element program capable of simulating complex real world problems. It is optimized for shared and distributed memory Unix Linux and Windows platforms.
2D and 3D Lagrangian, Eulerian, ALE, SPH, meshfree
Benchmark model
A Copper bar (5 mm radius, 1 m long) facially irradiated with 8 bunches of 7 TeV/c protons (each bunch comprises 1.11x1011 protons)
2D axisymmetric FEM model
radius
axis of symmetry
beam

## Slide 4: Numerical modeling (I)
The particle beam energy distribution is applied by using a three different case:
all the energy as initial condition E0
a 200 ns ramp (constant power)
a 8 bunches profile (0.5 ns constant power, 25 ns void, 0.5 ns constant power….)
Explicit integration scheme, time step magnitude 0.01 ns
Different mesh were tested in order to investigate the influence of spatial discretization on the results
Since a LSDyna tabular EOS routine is under developing (using the user-def capabilities and the Fortran routine written for SESAME and CTH) a standard Polynomial LSDyna EOS is used to fit tabular data (and try a simplified approach)
time step
3 different energy deposition methods
x
4 different mesh densitiy
x
2 different polynomial interpolations (solid, solid-liquid-plasma)
radius
axis of symmetry

## Slide 5: Numerical modeling (II)
isotherms
isodensity
Isoenergy
isoenergy
Tabular data
Interpolation
ONLY SOLID
SOLID LIQUID PLASMA

## Slide 6: Results (mesh)
BIG2
25x25
50x50
100x100
Pressure (GPa)
Density (kg/dm3)
FEM accuracy
Time step (propagation)
Energy deposition accuracy
200x200
1
2
1
2
□
□

## Slide 7: Results (Eos)
EOS obtained from solid data (polynomial/Gruneisen)
EOS obtained from the whole region of interest

## Slide 8: Results (deposition)
Deposition as initial condition E0
Deposition as 8 bunches profile
00
00
00
00
00
00
(ns)
(ns)
Element 2
Element 1
1
2
1
2
□
□
□
□

## Slide 9: Results comparison
N.A. Tahir et al., Thermo-mechanical effects induced by beam impact on LHC Phase II collimators: preliminary analysis using hydrodynamic approach
Density
BIG2
BIG2
BIG2
LSDYNA
LSDYNA
LSDYNA

## Slide 10: Phenomena evolution

## Slide 11: Conclusions (I)
Numerical simulations of interaction of 7 TeV proton beam that is generated by Large Hadron Collider (LHC) at CERN with a solid copper target were presented.
Study has been done to assess the damage caused by these highly relativistic protons to equipment including collimators, absorbers and others in case of an uncontrolled accidental release of the beam.
The protons energy loss in solid copper is calculated using the FLUKA code and these data are then used as input to the FEM code, LSDYNA, to study the hydrodynamic and structural response of the target.
Hydrostatic behaviour of the target material is treated using a polynomial equation-of-state. Elasto-plasticity with J-C material model.

## Slide 12: Conclusions (II)
When 8 bunches have been delivered, the material will be heated to very high temperature that will generate a very high pressure. This high pressure launches a radially outgoing shock that leads to a substantial density reduction in the central part of the cylinder.
The energy deposited by 8 proton bunches from the LHC is sufficient to severely damage the target: over than 50% of the target is melted and the remaining portion heavy deformed.

## Slide 13: Thermo-mechanical modeling of high energy particle beam impacts
M. Scapin, L. Peroni, A. Dallocchio
Thank you for your attention