## Slide 1: Results on MIMOSIS-0
M. Deveaux, GSI

## Slide 2: MAPS activities at CBM
IPHC Strasbourg
IKF University Frankfurt
CBM host laboratory
Silicon strip R&D
Sensor design
Sensor test
Sensor integration
The CBM-MVD
Sensor test
Sensor integration
Know-how transfer
New task sharing

## Slide 3: Competences @ FAIR/GSI
PCB and DAQ – Design
MAPS – tests:
Experience in operating MAPS.
Experience in rad. tolerance tests.
MAPS – simulation:
Experience in building digitizer models.
Access to heavy ion beams:
Few AMeV to ~1 AGeV.
Proton to 238U.
Sizeable clean rooms/ workshops.
Experience with micro – integration.
Together with

## Slide 4: Where do we want to go?
The CBM – Experiment
Micro Vertex Detector
Ultra thin: 0.3 – 0.5% X0
5 µm spatial resolution.
105 Au+Au collisions.
MAPS based.
Silicon Tracking System (upgrade)
Ver. 1 – Silicon Strip Detectors.
Reduce material budget.
Improve resolution.
Improve rate capability.
Better momentum resolution
Easier tracking
Ideas for additional projects are
welcome.
?

## Slide 5: Results from MIMOSIS-0
MIMOSIS-0
32 columns of 504 pixel.
Priority encoder.
Up to 40V depletion voltage.
No data buffers yet.
1 mm
X-ray picture taken with MIMOSIS-0
Test setup:
Compare amplifier response time with pulse injection time.
Record delay and jitter as function of pulse amplitude.
MIMOSIS-0 pixel
Oscilloscope screen shot
1µs

## Slide 6: Results from MIMOSIS-0 / CREMAPS-0
<5%
>95% of all hits
Preliminary outcome:
Dead time 3µs.
Time precision few 100 ns for >95% of all hits (t.b.c in beam test).
=> Gen. 3 MAPS may reach 1µs time resolution.

## Slide 7: Pixel response
Inject pulses with increasing amplitude at given threshold.
Estimate pixel noise.
Scan for bad pixels

## Slide 8: Pixel response
Analog pixels: underflow
Preliminary result (depends on pixel settings):
Fixed pattern noise (pixel production variation) < 12 e ENC
Thermal noise: 6e (below detection limit)
=> Excellent results in accordance with expectation.

## Slide 9: Response to total ionizing doses
Sensors irradiated with ionizing doses.
Test threshold shift and noise.
+ 1 year room temp. annealing
Preliminary result:
Noise mostly unchanged.
Threshold shift remains in acceptable range
=> Excellent but needs confirmation for non-annealed chips

## Slide 10: Summary and outlook: Test MIMOSIS-1
Next steps (together with IPHC and Uni-Frankfurt):
Basic functionality tests (time response, noise etc.).
Radiation tolerance tests.
Immunity to heavy ion impacts with GSI beams
=> HI impacts: Particularly dangerous for micro-chips.
GSI and IKF of Goethe University Frankfurt have long experience in:
  Sensor testing and operation.
  Radiation tolerance tests.
  Sensor simulation (digitizers).
  Sensor to detector integration.
MIMOSIS-0 tests suggest:
  Excellent noise performance.
  Promising radiation tolerance.
  The potential to reach a time resolution of 1 µs (so far optimized for 5 µs).
  Performance better than expected.
  Results need to be confirmed with MIMOSIS-1.
MIMOSIS-1