## Slide 1
XXXIX PANDA COLLABORATION MEETING GSI-DECEMBER 2011 B. GIRAUDO / D. ORECCHINI
CENTRAL SUPPORT FRAME STRUCTURAL ANALYSIS
FIRST APPROACH AND PRELIMINARY RESULTS
G. Giraudo & D. Orecchini

## Slide 2
- Central Support Frame (CSF) basic idea.
Geometrical prototype
Frame aluminium honeycomb.
Ancillary parts aluminium.
- CENTRAL SUPPORT FRAME STRUCTURAL ANALYSIS -
GSI-DECEMBER 2011: B. GIRAUDO / D. 0RECCHINI
Preliminary basic idea:
Common support for inner devices; (MVD, STT, cross pipe)
Lightweight, stiff and stable structure.
References for external survey.

## Slide 3
TITANIUM
TITANIUM
TITANIUM
SUPPORT FRAME: - CORE, ROHACELL IG51
- SKINS, M55J/LTM110-5
- Central Support Frame (CSF) - foreseen materials
- CENTRAL SUPPORT FRAME STRUCTURAL ANALYSIS -
GSI-DECEMBER 2011: B. GIRAUDO / D. 0RECCHINI

## Slide 4
Central Support Frame (CSF): main dimensions
- CENTRAL SUPPORT FRAME STRUCTURAL ANALYSIS -
GSI-DECEMBER 2011: B. GIRAUDO / D. 0RECCHINI

## Slide 5
TITANIUM (0.5mm Thickness)
TITANIUM (0.5mm Thickness)
STAINLESS STEEL (2mm Thickness.)
STAINLESS STEEL FLANGE
STAINLESS STEEL (0.5mm Thickness)
(OR TITANIUM ??)
TITANIUM (0.2mm Thickness)
CROSS-PIPE: foreseen materials,
(From document: Vacuum-Target-CJT_V2010kw48) Ref. EDMS Doc 1107870-872 v.1 .
- CENTRAL SUPPORT FRAME STRUCTURAL ANALYSIS -
GSI-DECEMBER 2011: B. GIRAUDO / D. 0RECCHINI

## Slide 6
- CENTRAL SUPPORT FRAME STRUCTURAL ANALYSIS -
GSI-DECEMBER 2011: B. GIRAUDO / D. 0RECCHINI
Cross-Pipe: MAIN DIMENSIONS
From document, Vacuum-Target-CJT_V2010kw48)
Cross-Pipe: I.P. area

## Slide 7
“CF” & “CROSS PIPE” GRAVITY LOAD
MVD’s GRAVITY LOAD
STT’s GRAVITY LOAD
- CENTRAL SUPPORT FRAME: Loads input
810N
330N
260N
- CENTRAL SUPPORT FRAME STRUCTURAL ANALYSIS -
GSI-DECEMBER 2011: B. GIRAUDO / D. 0RECCHINI
90N
183N

## Slide 8
Vertex support system and related moment
VERTEX SUPPORT SYSTEM
BACKWARD PIPE LONG ARM
Backward Pipe and related moment
- CENTRAL SUPPORT FRAME: Loads conditions
260N
260N
- CENTRAL SUPPORT FRAME STRUCTURAL ANALYSIS -
GSI-DECEMBER 2011: B. GIRAUDO / D. 0RECCHINI

## Slide 9
CENTRAL SUPPORT FRAME: Constraint conditions
TARGET : ACCEPTABLE MAX DISPLACEMENT: 0.05mm -
CONSTRAINT CONDITIONS
- CENTRAL SUPPORT FRAME STRUCTURAL ANALYSIS -
GSI-DECEMBER 2011: B. GIRAUDO / D. 0RECCHINI

## Slide 10
Translational values – Magnitude: Max 0.14mm
4xM55J + Rohacell + 4xM55J
The Cross-pipe has been considered as load.
1° FEM STEP: Geometry as the prototype
TARGET : ACCEPTABLE MAX DISPLACEMENT: 0.05mm -
- CENTRAL SUPPORT FRAME STRUCTURAL ANALYSIS -
GSI-DECEMBER 2011: B. GIRAUDO / D. 0RECCHINI

## Slide 11
- CENTRAL SUPPORT FRAME STRUCTURAL ANALYSIS -
GSI-DECEMBER 2011: B. GIRAUDO / D. 0RECCHINI
4xM55J + Rohacell + 4xM55J
- TARGET : ACCEPTABLE MAX DISPLACEMENT: 0.05mm -
The Cross-pipe has been considered as load.
Translational values – Magnitude: Max 0.12mm
2° FEM STEP: The central window has been closed

## Slide 12
3° STEP: All the windows has been closed
- CENTRAL SUPPORT FRAME STRUCTURAL ANALYSIS -
GSI-DECEMBER 2011: B. GIRAUDO / D. 0RECCHINI
4xM55J + Rohacell + 4xM55J
TARGET : ACCEPTABLE MAX DISPLACEMENT: 0.05mm -
The Cross-pipe has been considered as load.
Translational values – Magnitude: Max 0.1mm

## Slide 13
4° FEM STEP:
- A)- All the windows has been closed.
- B)- Frame skins has been changed: plies added.
- C)- The Cross-pipe has been integrated as part of the FEM model
trying to evaluate its behaviour under strains.
- CENTRAL SUPPORT FRAME STRUCTURAL ANALYSIS -
GSI-DECEMBER 2011: B. GIRAUDO / D. 0RECCHINI

## Slide 14
Translational values – Magnitude:
Max 0.0197mm
8xM55J + Rohacell + 8xM55J
The Cross-pipe has been considered as part of the FEM model.
4° FEM STEP: Results
- CENTRAL SUPPORT FRAME STRUCTURAL ANALYSIS -
GSI-DECEMBER 2011: B. GIRAUDO / D. 0RECCHINI
TARGET : ACCEPTABLE MAX DISPLACEMENT: 0.05mm -

## Slide 15
Translational values
Z component:
Max 0.018mm
Translational values
X component:
Max 0.0158mm
- CENTRAL SUPPORT FRAME STRUCTURAL ANALYSIS -
GSI-DECEMBER 2011: B. GIRAUDO / D. 0RECCHINI
4° FEM STEP: Results

## Slide 16
Von Mises: Max 3.75MPa
- CENTRAL SUPPORT FRAME STRUCTURAL ANALYSIS -
GSI-DECEMBER 2011: B. GIRAUDO / D. 0RECCHINI
4° FEM STEP: Results

## Slide 17
TITANIUM (Grade 5) MECHANICAL PROPERTIES:
- Density: 4400 Kg/m3
- Tensile Strength - Yield: 828 MPa
- Tensile Strength – Ultimate: 895 MPa
- Young Modulus: 106 GPa
- CENTRAL SUPPORT FRAME STRUCTURAL ANALYSIS -
GSI-DECEMBER 2011: B. GIRAUDO / D. 0RECCHINI
4° FEM STEP: Results
Von Mises: Max 3.75MPa

## Slide 18
1Nm
1Nm
CENTRAL SUPPORT FRAME: Loads conditions.
5° FEM STEP:
The torque due the insertion of the “Pellets pipes” has been considered in the FEM model.
INSERTION TORQUE
- CENTRAL SUPPORT FRAME STRUCTURAL ANALYSIS -
GSI-DECEMBER 2011: B. GIRAUDO / D. 0RECCHINI

## Slide 19
Translational values – Magnitude:
Max 0.0212mm
8xM55J + Rohacell + 8xM55J
The Cross-pipe has been considered as part of the FEM model.
- 5° FEM STEP: Results (Gravity loads + torque)
- CENTRAL SUPPORT FRAME STRUCTURAL ANALYSIS -
GSI-DECEMBER 2011: B. GIRAUDO / D. 0RECCHINI
TARGET : ACCEPTABLE MAX DISPLACEMENT: 0.05mm -

## Slide 20
Translational values – Z component:
Max 0.00794mm
- CENTRAL SUPPORT FRAME STRUCTURAL ANALYSIS -
GSI-DECEMBER 2011: B. GIRAUDO / D. 0RECCHINI
- 5° FEM STEP: Results (Gravity loads + torque)
Translational values – X component:
Max 0.0177mm

## Slide 21
Von Mises: Max 4.50MPa
- CENTRAL SUPPORT FRAME STRUCTURAL ANALYSIS -
GSI-DECEMBER 2011: B. GIRAUDO / D. 0RECCHINI
- 5° FEM STEP: Results (Gravity loads + torque)

## Slide 22
Von Mises, without torque: Max 3.75MPa
Von Mises, with torque: Max 4.50MPa
- CENTRAL SUPPORT FRAME STRUCTURAL ANALYSIS -
GSI-DECEMBER 2011: B. GIRAUDO / D. 0RECCHINI
- 5° FEM STEP: Results (Gravity loads + torque)
TITANIUM (Grade 5) MECHANICAL PROPERTIES:
- Density: 4400 Kg/m3
- Tensile Strength - Yield: 828 MPa
- Tensile Strength – Ultimate: 895 MPa
- Young Modulus: 106 GPa

## Slide 23
“CSF” GRAVITY LOAD
CENTRAL SUPPORT FRAME OPENED SCENARIOS: Constraint conditions.
6° FEM STEP:
“CSF” POSSIBLE PROBLEMS DURING HANDLING.
- CENTRAL SUPPORT FRAME STRUCTURAL ANALYSIS -
GSI-DECEMBER 2011: B. GIRAUDO / D. 0RECCHINI

## Slide 24
Von Mises: Max 4.00MPa
- CENTRAL SUPPORT FRAME STRUCTURAL ANALYSIS -
GSI-DECEMBER 2011: B. GIRAUDO / D. 0RECCHINI
6° FEM STEP: Results (Handling)
8xM55J + Rohacell + 8xM55J
Translational values – Magnitude:
Max 0,109mm

## Slide 25
“CSF” GRAVITY LOAD
- CENTRAL SUPPORT FRAME STRUCTURAL ANALYSIS -
GSI-DECEMBER 2011: B. GIRAUDO / D. 0RECCHINI
7° FEM STEP:
“CSF” POSSIBLE PROBLEMS DURING HANDLING.
CENTRAL SUPPORT FRAME OPENED SCENARIOS: Constraint conditions.

## Slide 26
- 7° FEM ATTEMPT: Results
- CENTRAL SUPPORT FRAME STRUCTURAL ANALYSIS -
GSI-DECEMBER 2011: B. GIRAUDO / D. 0RECCHINI
8xM55J + Rohacell + 8xM55J
Translational values – Magnitude:
Max 0,150mm
Von Mises: Max 1.63MPa

## Slide 27
- CENTRAL SUPPORT FRAME STRUCTURAL ANALYSIS -
GSI-DECEMBER 2011: B. GIRAUDO / D. 0RECCHINI
CENTRAL SUPPORT FRAME AFTER FEM ANALYSIS
The external geometry has not changed.
All the “windows of lightening” has been closed.
The connection area for the “MVD” and the “STT” are defined.
The “Cross-Pipe” connections must be defined and fixed.

## Slide 28
- CENTRAL SUPPORT FRAME STRUCTURAL ANALYSIS -
GSI-DECEMBER 2011: B. GIRAUDO / D. 0RECCHINI
NEXT STEPS:
1) DEFINITION OF THE INTERFACE BETWEEN THE “CSF” AND THE CROSS-PIPE
2) CONTACTS WITH SPECIALIZED COMPANIES:
- definition of technological details.
- design optimization.
-THE DESIGN REACHES THE GIVEN TARGETS. (FEM analysis)
THE DEVELOPMENT OF THE “CROSS-PIPE” IS A BASIC KEY FOR THE
FINAL DEFINITION OF THE INTERFACES BETWEEN THE CSF AND THE CROSS-PIPE.
SERVICES CONTRIBUTIONS NOT COMPLETELY DEFINED.
CONCLUSIONS