## Slide 1: Transmission Dynodes: Enhancing Vacuum Photodetectors
J. Lapington, D. Cussans, T. Conneely, N. Fox, G. Jones, M. Kreps, J. Milnes, W. Oughton, and A. Romano

## Slide 2: Outline
MCP-PMT – positive characteristics
MCP-PMTs – disadvantages
Technology to overcome MCP-PMT limitations
Diamond transmission dynode
Proof-of-concept hybrid detector
Long term vision
Project team
Summary

## Slide 3: MCP-PMT Characteristics
Single photon counting
Picosecond time resolution – σ < 30 ps
Low dark noise – typically < 1 kHz/cm2 – photocathode limited
Radiation tolerant – MCPs themselves radiation hard
High spatial resolution – readout dependent, MCP pore limited
Large format available – LAPPD up to ~ 20 x 20 cm2
Large wavelength sensitivity – 8 keV (0.16 nm) to 1200 nm – photocathode dependent
Despite complexity of manufacture, operational fragility, need for HV:
Impressive performance – technology of choice in many fields

## Slide 4: MCP-PMTs – the disadvantages
Gain Characteristics
Single photoelectron pulse height distribution
  Characteristics of the microchannel plate design:
    MCP glass has moderate secondary electron emission  large variance in gain per collision
    Pore geometry and continuous dynode arrangement  varying electron trajectories
    Varying gain per step and number of gain steps  high overall gain variance

## Slide 5: MCP-PMTs – the disadvantages
Gain Characteristics
Single MCP (~103 gain) – negative exponential distribution
Two or more MCPs (106 + gain) – pulse height saturation as gain increases
Pulse height saturation > 100% FWHM even at 106 gain
poor single photoelectron resolution even at high gain
Compare with SiPM single photoelectron resolution!

## Slide 6: MCP-PMTs – the disadvantages
Gain Characteristics
Single MCP (~103 gain) – negative exponential distribution
Two or more MCPs (106 + gain) – pulse height saturation as gain increases
Pulse height saturation > 100% FWHM even at 106 gain
poor single photoelectron resolution even at high gain
Compare with SiPM single photoelectron resolution!
Cf. SiPMs – can resolve single photoelectrons

## Slide 7: MCP-PMTs – the disadvantages
Lifetime Characteristics – negative effects of high gain
Electron avalanche in MCP mediates contaminant desorption
  Desorption increases nonlinearly with MCP gain

## Slide 8: MCP-PMTs – the disadvantages
Lifetime Characteristics – negative effects of high gain
Electron avalanche in MCP mediates contaminant desorption
  Desorption increases nonlinearly with MCP gain
  Desorbed material ionized and drifts towards MCP input
   Known as ion feedback
  Ion collisions can instigate secondary event (afterpulsing)
J Va’vra 2020 J. Phys.: Conf. Ser. 1498 012013

## Slide 9: MCP-PMTs – the disadvantages
Lifetime Characteristics – negative effects of high gain
Ions which escape from MCP accelerate towards photocathode
  Ion collision with photocathode damages photocathode
   Degradation of photocathode quantum efficiency, QE (dependent on total extracted signal charge)
   QE drops off faster at higher gain (for given detected event rate)

## Slide 10: MCP-PMTs – the disadvantages
Count Rate Characteristics – negative effects of high gain
Maximum signal current - 10-20% of MCP strip current,
Strip current determined by MCP resistance and HV,
Maximum count rate
But minimum MCP resistance limited by thermal runaway (-ve coeff. of resistance)
Maximum count rate gain-1

## Slide 11: MCP-PMTs – the disadvantages
Count Rate Characteristics – negative effects of high gain
Saturated PHD with distinct valley required for thresholding and good photon counting statistics
Typically:
 Minimum gain required >>105

## Slide 12: MCP-PMTs – the disadvantages
Dynamic range – negative effects of high gain
At high rates:
  Signal current limited by MCP strip current,
  Maximum count rate gain-1
At low rates:
  Minimum signal set by threshold level
  Minimum gain (>105) required for saturated PHD with valley
Dynamic range set by gain required for PHD saturation

## Slide 13: How do we escape MCP-PMT limitations?
Operation at reduced gain (without performance loss)
   Increased lifetime, maximum count rate, dynamic range
Improve (narrow) pulse height distribution (without gain increase)
  Possibility to run at lower overall gain
  Lower gain increases maximum count rate
  Lower gain also reduces ion feedback, increasing lifetime
  Narrow PHD also improves SPE resolution and dynamic range
Physical technique to limit/prevent ion feedback to photocathode
  Further improvement in lifetime
  How to simultaneously achieve these objectives???

## Slide 14: Technology Objectives
Must produce electron gain in vacuo
  Operates via secondary electron emission (SEE)
  Technology choice: reflection or transmission dynode
Impermeable to ion feedback
  Reflection dynode – porous structure 
  Transmission dynode – planar membrane 
High gain first stage
  Poisson statistics  narrower distribution () as increases
  Performance determined by material choice and device geometry

## Slide 15: Recap: Secondary Electron Emission
Four processes:
Excitation – of energetic photoelectron
Thermalisation – to maximise # of secondary electrons
Transport – to dynode output
Emission – to vacuum

## Slide 16: Recap: Secondary Electron Emission
Four processes:
Excitation – of energetic photoelectron
  Generation of secondary electrons by interaction of primary electron
  Absorption depth and number of secondaries related to primary electron energy and band gap
Thermalisation – to maximise # of secondary electrons
  Thermalisation of initial energetic secondaries to ~conduction band minimum (CBM) energies
Transport – to dynode output
  Transport efficiency dependent on scattering, trapping, and escape depth
  Scattering: band gap influences number of conduction band electrons causing scatter
  Trapping: dependent on crystallinity – defects cause traps, degrade efficient transport
  Escape depth depends on primary energy and device geometry
Emission – to vacuum
  Majority of secondary electrons thermalised – energies close to CBM
  Dynode surface modification  Negative Electron affinity (NEA)
  NEA allows electrons near CBM to be ejected into vacuum

## Slide 17: Band Structure of a Transmission Dynode

## Slide 18: Reflection and Transmission Dynodes
Conventional PMTs
  discrete dynodes in reflection mode
MCPs
  continuous dynode in reflection mode
  variable dynode length and number
  large range of trajectories
Transmission dynode
  Requires a thin membrane
  Linear geometry – confined trajectories
  Membrane is impermeable

## Slide 19: How to improve the MCP-PMT?
Primary Design Goals
Prevent ion feedback reaching PC  overcome PC lifetime limitation
Reduce gain  maximise maximum count rate (MCP-limited)
Achieve tighter PHD  Better efficiency, counting statistics, electronics
How to achieve these simultaneously?
First gain stage impermeable to ion feedback
First gain stage achieves tight PHD by means of higher gain
Utilise discrete dynode in transmission mode (impermeable to ion feedback)
High gain by using high secondary electron yield material (diamond)
Implement a high gain diamond transmission dynode as first gain element

## Slide 20: Diamond – a Suitable Dynode Material
High Band Gap (5.47 eV) and Mobility (4500 cm2/Vs)
  High band gap  low # of charge carriers in conduction band at RT
  Low scattering  better electron transport characteristics (SCD)
  Better transport properties  allows use of thicker transmission dynode
  # thermalised secondary electrons 1/band gap – offset by better transport & NEA
Surface Termination to produce NEA surface
  Various surface terminations provide NEA in diamond e.g. X-O dipole
  Important: NEA stability with charge extraction
Diamond can be doped
  Required for electrical contact  signal recharge
  Doping  internal E-field – aid to secondary electron transport and emission
Diamond – mechanical properties
  Ability to fabricate thin membranes for transmission dynode

## Slide 21: Previous work with diamond
Measured a high secondary electron yield – reflection mode only
Manufactured thin nanocrystalline diamond membranes– but transmission mode did not yield such good results
First tests using available polycrystalline diamond (PCD) material
Diamond SEE measurement

## Slide 22: Previous work with diamond
PCD - graphitic grain boundaries which compromise electron transport
  Problem for thin membranes
Transmission diamond dynodes require single crystal diamond (SCD)
  No grain boundaries, defects, traps – large improvement in transport properties
SCD was not readily available
Gain Advantage of Diamond
Measured diamond secondary electron yield (reflection)
Traditional dynode materials

## Slide 23: Recent Developments in Diamond
New growth techniques developed for large scale single crystal diamond (SCD)
Commercially available SCD material – several sources, cost-effective
New doping methods produce improvements in - and -type materials
New termination processes/ materials producing stable NEA surfaces have been developed
© Fraunhofer USA CMW

## Slide 24: Proof-of-Concept Hybrid Detector

## Slide 25: Proof-of-Concept Hybrid Detector
Initially trial a conservative approach
Transmission diamond dynode
  between photocathode and MCP
Provides a barrier for ion backflow
   longer photocathode lifetime
Provides electron gain
   Tight PHD at low gain
   Higher maximum count rate
Thin diamond membrane
  100’s nm – few μm thick
  High OAR support structure
Diamond with NEA surface
  Efficient charge extraction
Single MCP provides further amplification
   but maintain overall low gain
Toy model of PHD for diamond-MCP-PMT for at range of diamond dynode gains

## Slide 26: Proof-of-Concept Hybrid Detector
Initially trial a conservative approach
Transmission diamond dynode
  between photocathode and MCP
Provides a barrier for ion backflow
   longer photocathode lifetime
Provides electron gain (10-20 gain)
   Tight PHD at low gain
   Higher maximum count rate
Thin diamond membrane
  100’s nm – few μm thick
  High OAR support structure
Diamond with NEA surface
  Efficient charge extraction
Single MCP provides further amplification
   but maintain overall low gain and timing
A single MCP can achieve excellent time resolution in multi-photon mode – analogous to operation in hybrid detector
Va’vra 2020 J. Phys.: Conf. Ser. 1498 012013

## Slide 27: Long Term Vision
A technology to supercede MCPs
Monolithic stack of diamond transmission dynodes (3-5 dynodes)
Very low ion feedback – long lifetime
Gain of ~103–105 with narrow PHD for single photon counting
Linear dynode geometry  time resolution 10 ps
Integrated with an active pixel sensor e.g. Medipix, Timepix, TDCpix, etc.
Choice of readout ASIC allows customisation of performance
 Picosecond timing; high count rate; long lifetime; high spatial resolution ..

## Slide 28: Project Team
University of Leicester – long heritage in space science inc. MCP-PMTs, development of alternative detector technologies inc. diamond dynodes
University of Bristol - expertise in diamond manufacture and use in energy applications, and detector development for high energy physics
University of Warwick - expertise in detector development for high energy physics with focus on photo-detector characterisation
University of Birmingham - expertise in detector development, characterisa-tion, technology survey, and comparison with state-of-the-art MCP-PMTs
Photek - one of the leading worldwide manufacturers of vacuum tube devices with more than 25 years of custom detector design and fabrication expertise
This project is part of the Vacuum-based Photodetectors programme within DRD4 WP4.2

## Slide 29: Summary
Major MCP-PMT limitations – lifetime, count rate – difficult to overcome for future high-rate applications
Diamond has much promise as a high gain dynode material
Transmission dynode geometry offers significant advantages
Advances in diamond production and processing make this a realistic prospect
Initial conservative objective: MCP-PMT augmented with a single diamond transmission dynode (DTD)
Longer term goal: DTD stack to replace MCPs and integrate with readout ASICs:
 radiation-hard single photon imager; up to 10 GHz count rate;10 ps time resolution; 1 Mpixel resolution