## Slide 1
G. Giraudo
GSI-Darmstadt 24-06-2013
MVD updates
    Thermal properties improvement
    Cooling circuit test (Torino)
    Integration (Jülich)

## Slide 2
G. Giraudo
GSI-Darmstadt 24-06-2013
Updates for stave – Improvements for thermal properties
Changes:
  carbon foam  carbon paper
  carbon foam  Rohacell 31 IG
Thermagraph FGS |  | 
Properties | Unit | Data
Thickness | mm | 0.03
Density | g/cm3 | 1.6
Thermal Conductivity Through Plane | W/m·K | 1500
Thermal Conductivity Through Thickness | W/m·K | 15
Poco Foam/HTC |  | 
Properties | Unit | Data
Thickness | mm | <25.4
Density | g/cm3 | 0.6/0.9
Thermal Conductivity Through Plane | W/m·K | 135/245
Thermal Conductivity Through Thickness | W/m·K | 45/70
REFERENCE:
http://www.amecthermasol.co.uk

## Slide 3
Position and detectors distribution of Layer 1 & Layer 2 UNCHANGED
Rohacell
Carbon Paper
Thermal filler
G. Giraudo
GSI-Darmstadt 24-06-2013

## Slide 4
CARBON FOAM PROJECT
ADVANTAGES: CF plane workable
DRAWBACK: CF gluing uniformity
CARBON PAPER PROJECT
Carbon Paper
Carbon Foam
ADVANTAGES: minor Temperature; less material
DRAWBACK: plane precision
Si=0,1mm
Glue=0,1mm
CF=1mm
Glue=0,1mm
Ω=0,3mm
Glue=0,1mm
MP35N=0,08mm
Si=0,1mm
Glue=0,1mm
MP35N=0,08mm
Glue=0,1mm
CP=0,05mm
Glue=0,1mm
Ω=0,3mm
TEST ARE NEEDED
Tmax=35°C
Tmax=33°C

## Slide 5
G. Giraudo
GSI-Darmstadt 24-06-2013
Hydraulic circuit test – 2 lines
First step – not remote controlled

## Slide 6
G. Giraudo
GSI-Darmstadt 24-06-2013
Central frame (Prototype) completed in Frascati last 15thMay
Bosses for MVD suspension added
Ready to be sent in Jülich a.s.a.p.

## Slide 7
G. Giraudo
GSI-Darmstadt 24-06-2013