## Slide 1: Characterization of atomic hydrogen beams for future neutrino mass experiments
David Frese, Genrich Zeller, Caroline Rodenbeck

## Slide 2: Tritium based neutrino mass measurements
Measure shape of the endpoint region of the spectrum
)))
(((
More details in the slides of:
Juliana Stachurska
Francesca Maria Pofi
Christian Weinheimer
Sonja Schneidewind
Karo Erhardt

## Slide 3: Increasing sensitivity for future neutrino mass experiments
Credit: S. Heyns
Sensitivity study by S. Heyns

## Slide 4: Improving sensitivity for future neutrino mass experiments
Sensitivity study by S. Heyns
Development of new technologies is necessary to reach below inverted mass ordering
Differential detector
Atomic tritium
More details in the slides of:
Juliana Stachurska
Francesca Maria Pofi
Christian Weinheimer
Svitlana Hoienko
Jan Küpperbusch
Lorenzo Calza
Raghav Pandey

## Slide 5: Improving sensitivity with atomic tritium
Sensitivity study by S. Heyns
)))
(((
Intrinsic broadening of ground state (FWHM 1 eV)

## Slide 6: Steps toward an atomic tritium source
  Aim: Generate a source of mK-cold tritium atoms with high activity (ultimately >1011Bq ≈ KATRIN)
  Efficiency of each processing step needs to be optimized to achieve a high total efficiency
  Solve challenges together! Ongoing collaborative effort: Karlsruhe Mainz Atomic Tritium Experiment: KAMATE
Established technology at TLK
Future
Slide from C. Rodenbeck

## Slide 7: Milestones within KAMATE
KAMATE 0.5
KAMATE 1.0
KAMATE 2.0
KAMATE 3.0
  Identify the best dissociation technology
  Thermal dissociator
  Plasma dissociator
  Using nonradioactive hydrogen
  Tritium operation.
  Operate KAMATE 0.5 setup at TLK with tritium.
  Cooling I.
  Add accommodator to achieve atoms of O(100K).
  Cooling II.
  Add nozzle to achieve atoms of O(1 K).
  Add beam-temperature measurement setup using time of flight.
Slide adapted from C. Rodenbeck

## Slide 8: Techniques to characterize atomic hydrogen beams
Laser ionisation
Quadrupole Mass Spectrometer (QMS)
Calorimetric methods
Hydrogenation of graphene (H-Gr)
Advantages of H-Gr:
Large beam coverage possible
Sensitivity to single atom adsorption possible
Adsorption of tritium demonstrated
F. Schedin et al. Nature Materials 6(9):652-5 (2007)
Astaschov, M., et al. Eur. Phys. J. D 79, 60 (2025)
Hydrogenated graphene
Graphene exposed to a plasma
Killian et al. (GRASIAN) Eur. Phys. J. D 77, 50 (2023)
Zeller et al, Nanoscale Adv.,2024

## Slide 9
2D material consisting of C in honey comb structure
Adsorption is selective to atomic/ionic hydrogen
Two type of defects occur mainly during exposure to H-beams
Diagnostic methods:
In-situ: Sheet resistance measurement
Defect production removes a charge carrier
Ex-situ: Raman Microscopy
Complex dedicated optical setup for Raman microscopy
desired: -type defects
undesired: vacancy-type defects
Hydrogenation of graphene: H-Gr
Neumann and Stampfer, Springer, 2018
pristine graphene
defective graphene
Barrero et al. Sensors 2022, 22(24),101013

## Slide 10: Ex-situ diagnostic: Raman spectroscopy
2D/G intensity ratio: existence of graphene
D/D‘ intensity ratio: defect type
D/G intensity ratio: defect density is determined from theoretical (=idealized) calculations
Neumann and Stampfer, Springer, 2018
defective graphene
T Fournier et al., Carbon 244 (2025) 120657
Interpretation of Raman spectra can be non trivial

## Slide 11: Experimental setup
H-gas inlet
Dissociator
Hydrogen beam
Graphene samples
Thermal cracker
Plasma-based dissociation
substrate
Quartz substrate
Graphenea.com

## Slide 12: Measurement: Sheet resistance
Preliminary
substrate
Plasma source
Thermal cracker
gas
Zeller et al, Nanoscale Adv.,2024
Preliminary
substrate
H from thermal on quartz substrate

## Slide 13: Results: Sheet resistance
Logistic growth:
Plasma damages and removes the graphene (confirmed with Raman)
Local maximum observed in the beginning of the loading
Saturation seems to depend on substrate
Relative time (h)
Relative time (h)
( )
( )
Bin width: 1h
Preliminary
Preliminary
Relative time (h)
( )
Preliminary
Preliminary
Relative time (h)
( )
Richards, Journal of Experimental Botany, 10.1093, pp. 290–301 (1959)
Data
Fit
H from Plasma
gas
H from thermal
H from thermal on quartz

## Slide 14: Raman results: Defect type & Defect density
(hydrogenated)
(vacancy defects)
(mix of defect types)
Preliminary
Loading with plasma
Loading time: 53 min
Very little hydrogenation
Many vacancies
Beam profile visible in defect density
Loading with thermal cracker
Loading time: 48 h
Much more hydrogenation
Beamprofile-like structure visible in defect type
Defect density
Defect type
Comparison to literature:
Theory:
Hydrogen coverage < 1 %
Experiment:
Hydrogen coverage ~ 15%  Effective Adsorption rate Atoms/s  Efficiency ~ %
Son et al., Nat Commun 7, 13261 (2016)
T Fournier et al., Carbon 244 (2025) 120657

## Slide 15: Raman results of loading with plasma: Beam profile in defect density
Observe beam profile in the defect density
Increase beam coverage with multiple samples
Fit three empirical models
Determine beam profile properties
Lorentzian fit

## Slide 16: Summary & Outlook
Relative time (h)
( )
Bin width: 1h
Preliminary
Data
Fit
H from Plasma
gas
H from thermal
H from thermal on quartz
A sub-K atomic tritium source is needed for future neutrino mass experiments
KAMATE aims to develop diagnostics to characterize atomic tritium beams
Graphene is succesfully used to characterize hot atomic hydrogen beams (Paper in preparation)
Next up: Will this also work for cold beams?
Preliminary

## Slide 17: Backup

## Slide 18: Experimental setup key facts
Vacuum background pressure:
Operating flow:
Temperatures:
  Thermal dissociator:
  Plasma dissociator:

## Slide 19: Graphene as an atomic hydrogen sensor – In-situ diagnostic
Idea
Sheet resistance increases with hydrogenation
Thermal annealing to 300°C to distinguish defect type
Realisation
Sheet resistance via Van der Pauw (VdP) method
  4 wire contact method
  Averaging of all contacting permutations
  Independent of contacting quality and geometry
Engineering balance between:
  Fullfilling VdP contacting requirements
  Contacting robust against heating of 300°C
  UHV compatible
  Tritium compatible
Cha et al, Appl.Phys Express 15.1, 2022

## Slide 20: Ex-situ diagnostic: Raman spectroscopy
Graphene-structure-dependend wavelength shift of 532 nm laser
Neumann and Stampfer, Springer, 2018
defective graphene
pristine graphene

## Slide 21: Loading experiments: Dissociator comparison – plasma
Full loading with plasma removed graphene  existence of high energy species
Defect type for loading time: 45 min
Loading time: 17h
Loading time: 45 min
Plasma source
substrate
(mix of defect types)
(hydrogenated)
(vacancy defects)
Loading time: 45 min
Mixture of vacancies and -type defects  Very few atoms
Defect density

## Slide 22: Loading experiments: Substrate comparison
Preliminary
substrate
Quartz substrate
Plasma source
Thermal cracker
gas
Zeller et al, Nanoscale Adv.,2024
Sheet resistance indicates increased hydrogen coverage. Confirmed by first Raman scans (coverage >20%)
Preliminary

## Slide 23: Outlook: Implementation of PTFE tube
H-gas inlet
Graphene sample
dissociator
skimmer
PTFE tube
4 wire resistance of DAQ
Start loading

## Slide 24: Graphene for cold atoms?
Exact adsorption potential unclear
Classical chemisoprtion probably not possible due to potential well of ~0.1 eV
Investigate adsorption mechanisms by measuring at different beam temperatures
Wu et al. Nuclear Engineering and Technology 54 (2022) 4022e4029
Calculations T with Gr
Gr temperature
Easy experimental realization…

## Slide 25: Low-energy particle beams
Low energy: average kinetic energy of sub eV
Particles: ions, molecules, atoms
Fields that are interested:
Thin film deposition
Satish, M. J Bio Tribo Corros 9, 35 (2023)
A D Lambert et al 1999 Semicond. Sci. Technol. 14 L1
Atomic tritium research
Surface cleaning
Basic beam properties:
Beam alignment
Opening angle

## Slide 26: Raman spectroscopy limitations
Width determines defect stage
  Stage 1:
  Stage 2:
      No assignment for defect type!
Eckmann et al. Nano Lett. 12.8, 2012
T Fournier et al., Carbon 244 (2025) 120657
L.G. Cancado et al., Nano Letters11.8 (2011)

## Slide 27: Observed defect types
D/D‘ intensity ratio histogram
Eckmann et al. Nano Lett. 12.8, 2012
Raman spectrum of defective Graphene
hydrogenation: -type defects
vacancy-type defects
(mix of defect types)
(hydrogenated)
(vacancy defects)
Defect type in the D/D‘ intensity ratio
Mixture of vacancies and -type defects
D/D‘ intensity ratio

## Slide 28: Beam profiles

## Slide 29: Empirical beam profile models
Choose models empirically
Three models evaluated:
  Gaussian and
  Generalized Normal with p = free parameter and
  Lorentzian
Beam profile parameters

## Slide 30: Fit results – 3 models
Goodness of the fit :
And reduced :
Successful development of graphene chips as a new beam diagnostic tool
Compare data and lorentzian fit
Beam center
 | Lorentzian | Generalized normal | Gaussian
 | Lorentzian | Generalized normal | Gaussian
Residuals:
Degrees of freedom

## Slide 31: Determination of beam profile parameters - Model comparison
Determine from and for model comparison
Model | Conversion factor
Lorentzian | 2
Generalized normal | 1.98
Gaussian | 1.62
Models are compatible in the determination of beam profile position and size
Beam profile (BP) parameters

## Slide 32: Beam profile models
Choose models empirically
Three models evaluated:
  Gaussian and
  Generalized Normal with p = free parameter and
  Lorentzian
Beam profile parameters

## Slide 33: Fit parameter uncertainty
Beam profile (BP) parameters
Uncertainty of the D-G ratio of every pixel:
  from the fit of the D and the G peak
  from intensity calibration of the Confocal Raman Microscope
  Propagation via approximation of the Hessian matrix of the -function
Uncertainty yielding from variations in the mapping of the Raman scans to the photo.
  Monte Carlo uncertainty propagation
  Shifting the graphene samples by random value from a uniform distribution with limits:
      x-position :
      y-position :
      Rotation:
    Perform 1000 fits

## Slide 34: - Monte Carlo based uncertainty estimation for the lorentzian model
Beam profile (BP) parameters
= std. dev. of parameter 𝜃

## Slide 35: Correlation of parameters - Lorentzian
Beam profile (BP) parameters

## Slide 36: Hydrogenation of graphene
Jonathan Guillemette PHD Thesis (2014)
Hydrogen bonds covalently with electron of carbon atom
-bond misses an electron
Band gap forms

## Slide 37: Correlation of sheet resistance (in-situ) and D-G intensity ratio from Raman scans (ex-situ)
D-G intensity ratio is proportional to the defect density
correlates positively with R
and R correlate positively with loading time t and plasma driving power
Raman spectrum of defective Graphene
Gen. 3 pristine
Gen. 3 plasma exposed and heated
Gen. 4 pristine
Gen. 4 plasma exposed and heated
Generation | t in minutes | in W | in sccm
2 | 237 | 250 | 0.5
 | 1058 | 350 | 1.0
3 | 56 | 350 | 0.5
4 | 30 | 50 | 0.5
 | 13 | 250 | 0.5
Generation | t in minutes |  | 
2 | 237 | 250 | 0.5
 | 1058 | 350 | 1.0
3 | 56 | 350 | 0.5
4 | 30 | 50 | 0.5
 | 13 | 250 | 0.5
Sheet resistance R is an indicator for defect density
Neumann and Stampfer, Springer, 2018
Sheet resistance in k□
R

## Slide 38: Hydrogenation of graphene
Defect density depends on the defect type
Distinguish sp³-defects (hydrogenation) from vacancies by D-D‘ intensity ratio
Raman spectrum of defective Graphene
Gen 3 –
Gen 4 –
Eckmann et al. Nano Lett. 12.8, 2012
data gen 3
data gen 4
Generation 3 contains mainly vacancies → assign defect density =5.5 nm
sp³-defects decrease and vacancies increase with loading time
Neumann and Stampfer, Springer, 2018