## Slide 1
Eugenia Toimil-Molares
GSI Darmstadt
On behalf of the MAT collaboration
MATerials Research at FAIR

## Slide 2: Materials Research at GSI and FAIR
Operation of the MAT facilities:
flexible beam conditions
various ion species, energies, fluxes….
6 beamlines ( 7)
> 10 target stations ( 12)
online and in-situ analysis
Ion-track nanotechnology, irradiation effects, materials under extreme conditions
~ 200 MAT collaboration members from 27 countries
~ 40 groups served per beamtime
~ highly interdisciplinary (materials science, chemistry, geology, biology, nanosciences, …)
Highest ion energy loss
Large ion penetration range
Highly charged ions
at low kinetic energies
Highest intensities
Higher energies

## Slide 3: Materials Research at GSI and FAIR
Ion-track nanotechnology
Fabrication, characterization and application of novel nanostructures
Heavy ion-induced modifications
From bulk to nanoscale
Simulation of cosmic radiation
Materials under multiple extremes
Combining high pressure, radiation and temperature
High-pressure irradiation
Radiation hardness of functional materials
ion
beam
50 GeV
200 MeV/u
ion penetration range
energy loss
3 - 11 MeV/u
3 - 11 MeV/u
Cave A  APPA Cave

## Slide 4: MAT science at existing facilities
Highest ion energy loss and in-situ and online analysis
ion-track nanotechnology
ion-induced materials modifications: from bulk to nano
radiation hardness functional materials (including fusion and accelerator materials)
heavy ion microprobe for sub-µm targeting with single ions (space electronics and detectors)
astrochemistry
ions
UNILAC (3-11.4 MeV/u)
Ion range up to 100 µm
UNILAC
SIS18

## Slide 5: MAT facilities in 2030-31 (3 - 11.4 MeV/u)
HSI
SIS 18
North
HSI
South
HSI
X0 & M-branch
cw-beam HELIAC
UNILAC (10 Hz, 1 ms)
18GHz ECR
28GHz ECR
HELIAC: cw beams suitable for most of MAT activities (tunable intensity and energy), more efficient and stable irradiations (transfer technology)
UNILAC: pulsed beams allow only ~35% of program; unique for testing performance limits of materials in e.g. inertial confinement fusion and accelerators
Dual-beam experiments become possible  new research possibilities

## Slide 6: MAT science at existing facilities
Highest ion energy loss and in-situ and online analysis
SIS18 (80-1000 Mev/u)
Ion range ~mm-cm
High energy / ion range
irradiation of thick bulk samples
irradiations at high-pressures
radiation hardness of materials
UNILAC (3-11.4 MeV/u)
Ion range up to 100 µm
UNILAC
SIS18
CRYRING MAT-station
Highest ion charge states
at various kinetic energies
ions

## Slide 7: MAT science at APPA cave
Materials under extreme conditions
Temperature
High pressure
Ion Irradiation
High-pressure irradiation platform
APPA cave
Cave A to APPA cave:
Energy up to 10 GeV/u
Higher beam intensity
Cave suitable for experiments with more intense beams
Beam diagnostics for fast and slow extraction
Multipurpose-target station with in-situ and online analytics
APPA cave
MAT stations
HED@FAIR
SPARC
BIOMAT beamline

## Slide 8: Coupling extreme conditions
Pressures of up to ~100 GPa
Ion fluence up to 1013 i/cm2
Penetration depth (mm)
Enormous amount of energy in very localized volumes and in very short times
Ion Irradiation
Energy density ~ eV/atom
High energy
Au, Pb, U ions
Temperature
High pressure
Ion Irradiation
Zircon
Nanowires
Molecular compounds
Study of phases in Earth’s & rocky planet’s interiors
Formation and stabilization of high-pressure phases - new properties!
New thermodynamic paths for phase-transitions of bulk materials and nanomaterials

## Slide 9: Formation /stabilization of high-pressure phases
Phys. Rev. Lett. 96 (2006) 19570
Nature Materials 8 (2009) 793
ZrSiO4
14 GPa
Ion Irradiation
+
Pressures of up to ~100 GPa
Ion fluence up to 1013 i/cm2
High-pressure phase reidite:
  forms below critical transition pressure
  is stable upon pressure release
  nanocrystal formation at very low ion fluences
After irradiation and decompression
reidite
Penetration depth (mm)

## Slide 10: Formation /stabilization of high-pressure phases
Bi-NWNW (35 nm)
238U
Bi-I
Bi-I
In-situ Raman – Bi NWNW (35 nm)
Bi-II
2.4 GPa
238U @245 MeV/u ~30 MeV/u @ sample position
Schroeck et al. Phys. Rev B 112 (2025) 014111

## Slide 11: Formation /stabilization of high-pressure phases
238U @325 MeV/u
f = 3e13 i/cm2
f = 3e13 i/cm2
18.9 GPa
quenching
Bi microcrystal
J. Phys. Chem. C 124 (2020) 6659
Bi-III phase is
superconducting
with Tc ~6-8 K

## Slide 12: Ion-induced phase transitions in molecular solids
Liang, Tzifas, Winkler et al. PCCP (2026)
Tzifas et al, Phys. Rev. Res. 8 (2026) 023054
1.1 GPa
7.1 GPa
Efficient breakage of sulfur S8 rings drive system toward more ordered polymeric state, expected to exhibit superior thermal, electrical and chemical properties
a-S25
SII
S8
p-S
SHI irradiation under high pressure induces chemical reactions in molecular solids, evidenced by the polymerization of CO and sulfur, and urea decomposition

## Slide 13: Operational platforms in cave A
Diamond anvil cells (DAC)
Paris-Edinburgh cell (PEC)
sample size ~ mm
pressure up to ~12 Gpa
Tmax ~ 600 °C
sample size ~ 10-50 µm
pressure up to ~100 Gpa
room temperature

## Slide 14: Extension to low- and high-temperatures
Research goals
Irradiation of space ices under pressure at cryogenic temperatures to understand physicochemical processes
Study response of rocky planet materials under irradiation, pressure and high temperatures and explore how extreme conditions affect structural and chemical changes
Conduct temperature-dependent in-situ electrical measurements to correlate structural and electrical properties of novel material phases
Elucidating the role of temperature and temperature/pressure rates in ion-induced phase transformations under high-pressure
P
pressure
High T
Low T
Ions
ices
gas giants
nanomaterials
minerals
Extension of high-pressure research to low and high-temperatures
Materials of interest: ices, minerals, nanomaterials and molecular compounds
Platform upgrade funded by BMFTR ErUM-Pro (2025-2028) (B. Winkler, Goethe University Frankfurt)

## Slide 15: Static vs. dynamic compression (Bi)
Static → Dynamic-DAC (10⁰–102 s⁻¹) → FdC → Laser-driven shock (105–10⁸ s⁻¹)
Bi-III absent
Bi-V starts at lower pressures with unidentified phase Bi-M
Bi-IIIBi-V shifts to higher P at higher compression rates
Cubic
h
g:
Bi-I Bi-II  Bi-III  Bi-V
Range 0.01–780 GPa/s
Time-resolved XRD
at DESY P02.2
4 KHz
Investigation of influence of compression rate on bismuth phase transitions and
elucidate bismuth transformations at intermediate compression rates (µs)
Gorman et al., Sci. Rep. 8 (2018) 16927
Schröck et al. Phys. Rev B 112 (2025) 014111
Husband et al., Sci. Rep. 11 (2021) 14859

## Slide 16: Dynamic compression of Bi at µs-timescales
Compression rates up to ~60 TPa/s (≈60× faster than previous dDACs)
Strain rates ~102 – 103 s-1
MHz-XRD enabled by EuXFEL pulse train  µs structural tracking
Accessing a strain‑rate regime between classical dDAC and shock
Static → Dynamic-DAC (10⁰–103 s⁻¹) → FdA→ Laser-driven shock (105–10⁸ s⁻¹)
Time (µs)
Difraction angle 2q (deg.)
Eu-XFEL
O’Bannon, Appel, Schröck, Tzifas, Toimil-Molares, Pepin et al. Nature Communications Materials (2026)
Time (µs)

## Slide 17: Microsecond compression reveals kinetic suppression of Bi‑III
O’Bannon, Appel, Schröck, Tzifas, Toimil-Molares, Pepin et al. Nature Communications Materials (2026)
Static sequence preserved: Bi‑I → Bi‑II → Bi‑III → Bi‑V
Bi‑V nucleates 2 - 4 GPa lower than in static DAC
Bi‑III stability field shrinks with increasing rate  complex host-guest arrangement kinetically hindered
Transition onset depends on compression rate
At sufficiently fast loading, Bi‑III may be bypassed entirely  shock‑compression observations
Time (µs)
Difraction angle 2q (deg.)
Eu-XFEL
Time (µs)

## Slide 18
High pressures
Diamond anvil cells
Pressures of up to ~100 GPa
Ion fluence up to 1013 i/cm2
Penetration depth (mm)
Ion Irradiation
Energy density ~ eV/atom
GeV heavy ions deposit enormous amount of energy in very localized volumes and in very short times
High energy
Au, Pb, U ions
Coupling extreme conditions
Temperature
High pressure
Ion Irradiation
Notes: High-static pressures are achieved by inserting the materials of interest (x, y, z) in diamond anvil cells, where pressures of upto 100 Gpa can be reached
The heavy ion beams, as we have seen, deposit enormous amount of energy in very localized volumes and in very short times.
So, at GSI, Materials will be pressurized between the two diamonds of a diamond anvil cell to tens of GPa, and subsequently exposed to the ion beams.
A special characteristic of swift heavy ions is that they deposit the maximal energy at the end of the trajectory. So the high energy ions of the synchrotron accelerator can penetrate the cell (either though the diamonds or though the gasket and deposit the maximal amount of energy on the pressurized material.

## Slide 19: Functional materials response to radiation
Degradation of thermal conductivity
Monitoring of ion-pulse induced stress waves
Applications:
High-power accelerators:
(targets, collimators and beam dumps)
High temperature reactors
Space materials
Shock and Vibration (2021) 8884447
Pretreated copper targets for ion-beam desorption experiments
Acta Materialia 184 (2020) 187
Vacuum 194 (2021) 110608
APPA cave:
Fast extraction of high-intensity pulsed beams (higher intensities up to 1011 pps)
High energy – larger volumes of radiation damaged and thermally excited material
New facility to study dynamic response of beam-facing materials on site

## Slide 20: Astrochemistry at APPA cave
µm thick cryogenic film
on IR transparent window
ion beam
How are complex molecules created in space?
Ion beam
APPA cave:
Extension of available ion energies for determination of molecules formation and destruction yields
Irradiation of molecules inside bulk materials simulating space conditions
Chemical processes, sputtering, temperature effects,…
Multipurpose chamber with in-situ and online analysis techniques
GSI
FAIR
Galactic Cosmic Rays
Astronomy & Astrophysics A&A 623, A134 (2019)
Astronomy and Astrophysics, 599, A130 (2017)
NIMB 365 (2015) 477–481

## Slide 21: Summary
APPA cave
MAT-collaboration meeting
SPARC
BIOMAT stations
HED
New experimental opportunities for Materials Research at CRYRING and in APPA cave with FAIR beam parameters and diagnostics
High-pressure irradiation platforms being extended and ready for Day 1
Chambers for radiation hardness tests and astrochemistry being planed
Platforms are mobile and can be used at various locations
GSI-MAT
Thank you for your attention!

## Slide 23: International competitiveness
worldwide only very few large-scale high-energy heavy-ion accelerators with dedicated beamlines for material science
Facility | Capabilities / limitations | Rating
GSI/FAIR | Most comprehensive facility: full ion/energy/flux range, ex-situ, in-situ & online analysis, onsite expertise. | Excellent
GANIL/CIMAP | Several in-situ techniques; focus 0.5–4 MeV/u, max E ~29 MeV/u for Pb. | Limited
IMP/CAS | Dedicated materials beamlines; limited ion flux. | Limited
HIAF/CAS | Materials research beamlines not yet available — expected in future. | No current activities
JINR & Univ. of Jyväskylä | Beams up to UNILAC energies; no in-situ analysis. | Limited
CERN | HiRadMat beamline for pulsed beams — only protons. | No current activities
NICA & RAON | Plan activities; limited experience with heavy ions so far. | No current activities
Riken, MSU, BNL | Very few activities; no material-science user facility. | No current activities

## Slide 24: EXTRAS

## Slide 25: MAT science at CRYRING
CRYRING (0.3 – 14 MeV/u)
MAT station @ CRYRING
Physics topics
ion solid interaction at highest charge states and low kinetic energies
surface and sputtering processes
defect enginnering in 2D materials
Highest ion charge states
2021: comissioning of UHV-irradiation chamber with 107Ag47+ @ 5.9 MeV/u
2025: installation and commissioning of in-situ Raman spectrometry and first experiments

## Slide 26
Chart: MAT country distribution
| Australia | Austria | Belgium | Brazil | China | France | Germany | India | Italy | Japan | Russia | USA | Others
 | 4 | 6 | 4 | 7 | 12 | 21 | 70 | 4 | 4 | 7 | 7 | 16 | 26