## Slide 1
Status of the CBM Micro Vertex Detector
M. Deveaux, Goethe University Frankfurt

## Slide 2: Outline
Some propaganda slides on MAPS
Some science behind the propaganda
DAQ concept and beam test results
Toward detector construction
MVD
STS
2.5°
25°
Beam

## Slide 3: Open charm reconstruction: Concept
Primary Beam: 25 AGeV Au Ions (up to 109/s)
Primary
vertex
Secondary
vertex
Short lived particle
D0 (ct = ~ 120 µm)
Detector 1
Detector2
Target
(Gold)
z
Reconstruction concept for open charm
Central Au + Au collision (25 AGeV)
A good time resolution to distinguish
the individual collisions (few 10 µs)
Very good radiation tolerance
(>1013 neq/cm²)
Reconstructing open charm requires:
Excellent secondary vertex
resolution (~ 50 µm)
=> Excellent spatial resolution (~5 µm)
=> Very low material budget (few 0.1 % X0)
=> Detectors in vacuum

## Slide 4: Performances of MAPS (2003)
 | Required | Hybrid pixels
Single point res. [µm] | ~ 5 | ~ 30
Material budget [ X0 ] | ~ 0.3% | 1%
Time resolution [µs] | few 10 | 0.025
Rad. hardness [n/cm²] | > 1013 | >> 1014
CCD
~ 5
~0.1%*
~100
<< 1010
MIMOSA-5 (2001)
3.5
~0.1%*
~25000
~ 1012
*Sensor only
MAPS provide an unique compromise between:
sensitivity
high rate capability
R&D is needed on radiation tolerance and read-out speed.

## Slide 5: Speed of MAPS vs. needs of CBM
MIMOSA-5
MIMOSA-20
MIMOSA-26
ASTRAL*
*predicted
CBM minimum
CBM maximum

## Slide 6: Tolerance to ionizing radiation
Mimosa-4
Mimosa-15
Mimosa-32
CBM minimum
Mimosa-1

## Slide 7: Tolerance to non-ionizing radiation
MIMOSA-1
MIMOSA-11
MIMOSA-26AHR
MIMOSA-18AHR
CBM minimum

## Slide 8: Performances of MAPS (2014)
 | Required | Hybrid pixels
Single point res. [µm] | ~ 5 | ~ 30
Material budget [ X0 ] | ~ 0.3% | 1%
Time resolution [µs] | few 10 | 0.025
Rad. hardness [n/cm²] | > 1013 | >> 1014
CCD
~ 5
~0.1%*
~100
<< 1010
ASTRAL³ (2014E)
~5
~0.05%*
15-20
> 1013
*Sensor only
²Best of specialized sensors
MAPS² (2013)
3.5
~0.05%*
32
> 3x1014
³Estimate (submitted)

## Slide 9: Sensor R&D: The operation principle
Reset
+3.3V
+3.3V
Output
SiO2
SiO2
SiO2
N++
N++
N+
P+
P-
P+
15µm
50µm

## Slide 10: Radiation tolerance vs. pixel pitch
Better CMOS-technology – better performance
Undepleted sensor
Partially depleted sensor

## Slide 11: Limitations of traditional MAPS
Reset
+3.3V
+3.3V
Output
SiO2
SiO2
SiO2
N++
N++
N+
P+
P-
P+
15µm
50µm
N+
P
P
No PMOS transistors => No discriminators on pixel => “slow”
PMOS Transistor

## Slide 12: Today: 2.5D-MAPS
Reset
+3.3V
+3.3V
Output
SiO2
SiO2
SiO2
N++
N++
N+
P+
P-
P+
15µm
50µm
N+
P
P
Modern 0.18µm process was identified:
Deep P-well isolates sensor from electronics
PMOS transistor available
deep P-well
Sensor design: PICSEL Group, IPHC Strasbourg, et al.

## Slide 13: The science behind the propaganda
Reset
+3.3V
+3.3V
Output
SiO2
SiO2
SiO2
N++
N++
N+
P+
P-
P+
50µm
N+
P
P
deep P-well
Question:
Does deep P-well really
separate electronics and
sensor?
Fe-55, 5.9 keV
Answer: Yes, it does.
D. Doering, B. Linnik

## Slide 14: The science behind the propaganda
Reset
+3.3V
+3.3V
Output
SiO2
SiO2
SiO2
N++
N++
N+
P+
P-
P+
50µm
N+
P
P
deep P-well
Qestion:
Does the charge collection
still work?
d
Answer:
d= 6µm => reduced
d=10µm => ok
D. Doering, B. Linnik

## Slide 15: The science behind the propaganda
Reset
+3.3V
+3.3V
Output
SiO2
SiO2
SiO2
N++
N++
N+
P+
P-
P+
50µm
N+
P
P
deep P-well
Qestion:
Any impact on the noise?
(Expect reduced noise)
Answer:
Ouups…
…lets have a closer look…
D. Doering, B. Linnik
new 0.18µm
old 0.35µm

## Slide 16: The science behind the propaganda
Observation (measurement + literature):
Pre-amps of individual pixels suffer from RTS-Noise
  in input transistors.
May be cured by enlarging the gate of affected transistors

## Slide 17: The science behind the propaganda
From: ALICE TDR for the
upgrade of the ITS (Nov. 2013)
Reported in Strasbourg
Reported on ALICE-ITS meeting
(March 2013)
Migrating a technology to a different CMOS process comes
with many challenging details.
It works best, if many experiments contribute (financially).
HIC for FAIR has some outreach…
Gate: 0.35µm in 0.18µm CMOS
Gate: 0.2µm
250k€
Submitted to JINST

## Slide 18: Pixels of the past, pixels of the future…
Pixel of MIMOSA-11
2 transistors
Signal handling outside
1x
??? transistors
Signal discrimination inside
Digital data transport on chip
=> Much more speed
Pixel of AROM-0

## Slide 19: “If I give you the data…
CBM-MAPS
~ 2 Gbit/s per chip
Conventional phone
~ 56 kbit/s
= 36 000 x
= 320 x
… you are going to have (to deal with) it.”

## Slide 20: Cluster compression (Q. Li)
 | * |  | * | 
 |  | * * |  | 
Plausible cluster
Unplausible cluster
Idea:
There are plausible clusters
There are not so plausible clusters
>90%
Data: MIMOSA-26AHR
Beam test @SPS 2012
0 = overflow/fail
Don‘t encoding full window (25bit),
define shape code (10bit)
Observation (real data):
99.99% of all clusters
are successfully encoded

## Slide 21: Possible cluster encoding (Q. Li)
0 | … | 9 | 10 | … | 20 | 21 | … | 30 | 31
Bit(0-9) |  |  | Bit(0-10) |  |  | Bit(0-9) |  |  | Bit0
Row Address |  |  | Column Address |  |  | Index of the ShapeCode |  |  | OVF
Header
Framecpt
ClusterNum
Trailer
Cluster1
ClusterN
N=ClusterNum
Real data:
MVD prototype@CERN SPS
Result:
Encode cluster in 32bit
Grouping done on FPGA (implementation ongoing)
Data reduction: Factor 2 (SPS beam test data)

## Slide 22: Beam test of the MVD-prototype
After fine analysis: Nominal resolution of
MIMOSA-26AHR (3.5µm) reproduced.

## Slide 23: Refined results on the prototype
Observation:
Background is generated by
very limited number of noisy
pixels.
Observation:
Device under test moved…
…with 3nm / min…
…(30 atom layers/min)…

## Slide 24: A word on integration
The CBM – MVD should
Have 3-4 layers
~0.3% X0 (first station)
~0.5% X0 (other stations)
Operate in target vacuum
Cooling <1 W/cm²
Bending radius: ~30 cm
Size: 21.2 x 10.6 mm2

## Slide 25: Integration concept of the MVD
Discri
Sensor
Discri
Sensor
Discri
Sensor
Discri
Sensor
Discri
Sensor
Discri
Sensor
Discri
Sensor
M. Deveaux
25
T. Tischler
MIMOSIS-1B
MIMOSIS-1A
Discri
Sensor
Discri
Sensor
Discri
Sensor

## Slide 26: Why cables?
Together with R. Visinka (GSI), A. Meier, F. Völklein (Hochschule RheinMain, IMtech)
Cables are material…
… material is evil…
Try to avoid cables.
Idea: Put traces directly
on the CVD diamond.
Status: Demonstrator produced, tests underway.
C. Müntz

## Slide 27: Test of the sensor before integration
The challenge:
Take 50µm thin sensor
Connect ~50 pins with a probe
Operate the sensor via the probes
Test the sensor…
M. Koziel, B. Milanovic

## Slide 28: Probe testing of MIMOSA-26AHR
50µm thick MIMOSA-26AHR operated successfully
Software for detailed tests is being developed
M. Koziel, B. Milanovic

## Slide 29: Vacuum compatibility
First tests on vacuum:
Goal: Absence of air
Issues:
Outgasing
Mech. stress due to cavities
Observations with 50µm dummies:
No significant outgasing (test not very sensitive)
Cavities of ~0.5mm can be tolerated
M. Koziel, G. Kretzschmar, T. Tischler

## Slide 30: Vacuum operation
Yesterday:
18:38… a reference station of the MVD prototype is
switched on within the vacuum vessel…
19:12… System tolerates pumping to 7mBar…
(Smoke test passed… still high noise).
To be continued…

## Slide 31: Conclusion
Sensor R&D in schedule:
  All requirements individually demonstrated
  Expect first full prototype in 2014
  Sensor might exceed initial performance expectations
Beam test of the prototype successful:
  Reached nominal sensor resolution (3.5 µm)
  Reached >99% detection efficiency for MIPs
  Dark rate << 104
  Still open: DUT moved by 3nm/min
DAQ concept demonstrated with beam data…
Studies on sensor QA, vacuum operation, … in schedule
There are thousand open issues remaining,
but I dare to predict…

## Slide 32: Conclusion
The MVD will fly…

## Slide 33: Instances of the processing chain
MIMOSA-Sensor:
Rolling shutter readout
On-chip noise discrimination
On-chip group finding
Output: High level protocol
 |  | 0 | 1 | 2 | 3 | 4 | 5 | 6 | 7 | 8 | 9 | 10 | 11 | 12 | 13 | 14 | 15
1 | Header | 0x5555 |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
2 | Header | 0x5555 |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
3 | Framenr | Frame Number 1 |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
4 | Framenr | Frame Number 2 |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
5 | Datalength | Data Length a |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
6 | Datalength | Data Length b |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
 | State Row | Of | Address line |  |  |  |  |  |  |  |  |  |  | States per line |  |  | 
 | State Col |  |  |  | Address column |  |  |  |  |  |  |  |  |  |  | NN | 
N-1 | Trailer | 0x8001 |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
N | Trailer | 0x8001 |  |  |  |  |  |  |  |  |  |  |  |  |  |  | 
Native MIMOSA-26 data word

## Slide 34: Instances of the processing chain
TRBv3 - FPGA:
Sensor control
Test for data consistency
SEU – detection and sensor restart
MVD synchronization
Time stamping
Add absolute system time
Data reduction
Idle bit removal
Data compression