## Slide 1: Summary HiLuMI LHC Collimation Materials Irradiation Damage Study at BNL EuCARD
N. Simos
Effort consists of:
IRRADIATION
200 MeV proton irradiation at BNL Linear Isotope Producer (BLIP) of 4 candidate materials (Molybdenum, Glidcop, Mo-Graphite and Cu-CD (copper-diamond). Irradiation parameters: 8-weeks at 110 uA
Neutron irradiation of Cu-CD from 118 MeV protons
28-MeV proton irradiation of Mo (including spallation neutron irradiation of Mo, Glidcop, Cu-CD and Mo-GR)
PIE
X-ray diffraction studies at NSLS X17B1/X17A beamlines (completed)
X-ray diffraction studies at NSLS II XPD beamline (proposed)
Comprehensive macroscopic analysis at BNL Isotope extraction facility (initiated)
Spectral Analysis (initiated)
Nano- micro-structural characterization at Center of Functional Nanomaterials (initiated)

## Slide 2
Irradiated LHC HiLuMi Collimation materials
Preliminary Assessment:
200 MeV heavily bombarded LHC array is still in cool-down mode due to extremely high dose levels.
One of the two Molybdenum (Mo) capsules has been opened for visual examination. Mo samples appear to be fully intact.
In coming weeks the proton irradiated array will be opened and examined (followed by transport to the PIE hot cells for sorting and studies)
Neutron irradiated Cu-CD has seen no structural degradation
28 MeV protons and spallation neutrons at Tandem have not affected the structural integrity of the LHC HiLuMI array

## Slide 3
200 MeV Proton Irradiation

## Slide 4
Spallation Neutron Irradiation - Cu-CD
Neutron spectrum downstream of isotope target array

## Slide 5
28 MeV Proton (plus spallation neutron) irradiation at Tandem
Mo – direct 28 MeV protons
Mo/MoGR/CuCD/Glidcop: spallation neutrons
28 MeV (1 uA, 200 x 200 um x um) protons

## Slide 6
X17A (monochromatic x-rays)
X-Ray ring
(3 GeV)
X17B1
X-ray diffraction studies at NSLS
Monochromatic 70 KeV beam (X17A beamline)
White beam 200 KeV, X17B1 beamline
Mo-GR
Glidcop (SLAC LHC rotating collim)
Glidcop (HiLuMI)

## Slide 7
incident
collimation
system
Transmission
detector
(radiography)
Ge-Detector
specimen
Diffraction
volume
2
k
“White Beam”
STRAIN MAPPING
Energy Dispersive Diffraction Mode
1m diff. coll.

y
X-17B1
3-12o~
Like having imbedded inter-atomic strain gauges !!!!
10-50 m

## Slide 8
From concept to a versatile experimental stage at X17B1 beamline at NSLS
Multi-functional stage capable of handling
  Real size irradiated specimens, under vacuum and four point bending state of stress
  and eventually
  Heating/annealing via a portable, collimated laser beam
  Tensile stress-strain test

## Slide 9
stress
strain

## Slide 10
EXCELLENT matching with the experimental data at X17B1 using x-rays and loading to assess the displacement.
Load 1
Load 2
GOAL: LATTICE strain and global strain are very different in magnitude

## Slide 11
STATE of PIE
8-week proton Irradiation at BLIP
Target Capsules (still extremely hot) were transported to the Hot Cell Facility for opening and sorting;
Capsules opened so far:
Two proton irradiated Mo
Proton irradiated Glidcop
Proton Irradiated Cu-CD
Low-dose proton irradiated Mo-GR
Neutron irradiated Cu-CD

## Slide 12
Status of HiLuMI LHC Irradiation Damage Studies at BNL
BLIP
200 MeV proton irradiation (8 weeks): COMPLETED
Neutron irradiation from 112 MeV protons COMPLETED
Cooling of highly radioactive samples in Hot Cell Lab 66: ON-GOING
TANDEM VAN DER GRAAF
28 MeV proton irradiation: COMPLETED
X-ray Diffraction Experiments at NSLS
X-Ray diffraction studies for phase and strain mapping of some cold and irradiated samples: COMPLETED (to be continued in NSLS II in late 2015)
Data analysis: ON-GOING
X-ray Diffraction Experiments at NSLS II (XPD Beamline)
Beamtime proposal preparation at XPD (due Feb. 2, 2015)
CFN (BNL Center of Functional Nanomaterials)
Annealing and Electron Microscopy analysis: NOT STARTED (foreseen for beginning 2015)
IEF (BNL Isotope Extraction Facility)
Activity and dose measurements per sample: COMPLETED
γ-spectra for selected samples: PARTIALLY COMPLETED

## Slide 13
Mo #1
Mo #2

## Slide 14
Mo-GR Irradiated with 200 MeV protons full beam for 2 hours at BLIP before it was removed from beam due to overheating and closing the cooling channel
Shows signs of distress even with minimum beam

## Slide 15
Mo X-ray Diffraction Studies (preliminary)

## Slide 17
X-ray Diffraction of Mo Irradiated with 28 MeV focused PROTON beam at TANDEM

## Slide 18
Cu_CD_unirrad
Cu_CD_Irradiated with FAST neutrons at BLIP

## Slide 19
Mo-GR_unirrad
Mo-GR: Irradiated with modest FLUENCE of protons at BLIP
Mo-GR: Irradiated with modest FLUENCE of neutrons at TANDEM

## Slide 20
Mo-Gr (unirradiated)
Mo-Gr (irradiated at Tandem with neutron flux)

## Slide 21
Graphite <002>
Mo-Gr Irradiated at BLIP with 200 MeV Protons and very modest fluence
Scanning across the irradiated zone

## Slide 22
SUMMARY
An extensive PIE (both macroscopic at the BNL Hot Cells and Microscopic using X-rays at the new Synchrotron and the XPD beamline and CFN for unirradiated materials studies)
The large volume of experimental data to-date from the different irradiations and X-ray diffraction as well as baseline studies will continue to be analyzed
THE CRUCIAL steps are those associated with the HEAVILY IRRADIATED array of Mo, Mo-Gr, Cu-CD and Glidcop at BLIP
Complete opening all capsules and sort all of them
  Conduct all the macroscopic studies (including photon spectra)
  Anticipate cool-down below levels that they can be studied at the XPD beamline of NSLS II (proposal under preparation)
ASSESS what materials from array should be looked further and which should not

## Slide 23
PRELIMINARY ASSESSMENT on LHC Collimator Materials of PHASE I
2-D Carbon/Carbon Composites
Graphite
Glidcop
PARENTHESIS

## Slide 24
Glidcop – Irradiated with 200 MeV protons
Irradiated
Unirradiated

## Slide 26
Effects of Proton irradiation (180 MeV) on graphite and C/C composite
X-ray diffraction studies at NSLS
Unirradiated GRAPHITE
irradiated GRAPHITE

## Slide 27
Effects of Proton irradiation (180 MeV) on graphite and LHC C/C composite

## Slide 28
Global volumetric changes vs. crystal-level changes
Activation Energy

## Slide 29
Irradiation and Thermal “anomalies” of Tungsten – Possible Similarities to Mo