## Slide 1: STORAGE RINGS MEETING
RESIDUAL ACTIVITY
Ing. Peter KATRIK
[ P. Katrik1,2 | E. Mustafin1 | D. Hoffmann1,2 | I. Strasik1 | M. Pavlovic3 ]
1GSI Darmstadt, Germany | 2TU Darmstadt, Germany | 3STU Bratislava, Slovakia
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]
INDUCED BY HEAVY-ION BEAMS IN MATTER
GSI Helmholtz Center for Heavy Ion Research, Darmstadt

## Slide 2
Content
RESIDUAL ACTIVITY INDUCED BY HEAVY-ION BEAMS IN MATTER.
. motivation
. activation of the material
. experimental settings
. depth-profiling
. beam loses criteria
. review of previous results | FLUKA 2008.3.6
. new results | FLUKA 2011.2b.5
. conclusion
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 3
Motivation
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]
SIMULATIONS & EXPERIMENTS.
. Beam-loss criteria
. „Hands-on“ maintenance
. FLUKA verification
. Previous experiments at GSI
. Preparation work at FAIR

## Slide 4
Motivation
SIMULATIONS & EXPERIMENTS.
. Beam-loss criteria
. „Hands-on“ maintenance
. FLUKA verification
. Previous experiments at GSI
. Preparation work at FAIR
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]
Target | Beam energy | Beam
Stainless steel | 1GeV/u | U
Stainless steel, Cu, Al, Pb | 950 MeV/u | U
Stainless steel, Cu, Al, Pb , Graphite, Carbon-composite | 500 MeV/u | U
Pb | 345 MeV/u | U
Al | 300 MeV/u | U
Al, Cu | 200 MeV/u | U
Al, Cu | 125 MeV/u | U
Carbon-composite | 100 MeV/u | U
Cu, Al, Pb | 500 MeV/u | Ta
Al | 300 MeV/u | Xe
Cu | 100 MeV/u | Xe
Cu | 700 MeV/u | N
Cu, Al, Pb | 500 MeV/u | N
Cu, Al | 1 GeV/u | Ar
Cu, Al | 500 MeV/u | Ar

## Slide 5
238U
Energy = 200 MeV/u
Activation
Fragment of target atom
Fragment of primary ion
Fragment of primary ion
Scattered neutrons

## Slide 6
Atoms of U, Al and Fragments
BEAM-LOSS.
. motivation

## Slide 7
Interactions of neutrons with matter
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]
incident
neutron
target
nucleus
compound
nucleus
A
Z*
α
emitted
charged particle
final
nucleus
C
. illustration of (n, a) reaction
incident
neutron
target
nucleus
compound
nucleus
A
Z*
E
D
fission fragment
fission fragment
fission neutrons
. illustration of fission reaction
incident
neutron
target
nucleus
compound
nucleus
A
Z*
. illustration of (n,g) reaction
final
nucleus
Z
gamma
rays
incident
neutron
target
nucleus
compound
nucleus
A
Z*
. illustration of inelastic neutron scattering
gamma
rays
A
scattered neutron
excited nucleus
A*
ground-state nucleus
incident
neutron
target
nucleus
compound
nucleus
A
Z*
scattered neutron
ground-state
nucleus
A
. illustration of elastic neutron scattering
. the compound nucleus is unstable
. can disintegrate into various products
. can emit gamma rays

## Slide 8
Activation
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]
. simulated by SRIM
Experimental target
HEAVY-ION BEAM PENETRATION.
. Δx - the range
. E0 - the initial kinetic energy of the particle
. S(E) - the stopping power
Stopping power, dE/dx
Kinetic energy, E(x)
Depth
dE/dx
E(x)
Range
. combination of the foils and discs
. different thickness | resolution of the depth-profiling

## Slide 9
Experimental station
IRRADIATION.
. remote control from MCR
. 3 analog cameras
. 2 moving platforms for ~ 5÷10 targets
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]
HHD cave

## Slide 10
Experimental station
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]
AFTER IRRADIATION.
. detector Canberra® HPGe – GC3518
. spectrometer ORTEC® DESPEC LF TM
. software GammaVision ®
Energy resolution ~ 1.8keV FWHM at the 1332 keV 60Co line
Model A66-B32

## Slide 11
Organic foils
BEAM SPOT MEASUREMENT.
. radiation sensitive material
. polycarbonate
. kapton
. pokalon
. bisphenol
. important for simulation | dose distribution calculations
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 12
Focusing issue
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 13
Depth-profile
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]
Experimental target

## Slide 14
Depth-profile
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]
. better resolution of depth profile = more foils
. more foils = longer total time of measurement of whole target
. better measurement statistic = longer measurement time
. short-living isotopes = short time till all nuclides die

## Slide 15
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 16
Depth-profile
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]
Chart: Depth [mm]
| 0.25 | 0.75000000000000011 | 1.25 | 1.7500000000000002 | 2.25 | 2.75 | 3.05 | 3.15 | 3.25 | 3.3499999999999996 | 3.4499999999999997 | 3.5500000000000003 | 3.6500000000000004 | 3.7500000000000004 | 3.85 | 3.95 | 4.0500000000000007 | 4.1499999999999995 | 4.25 | 4.3499999999999996 | 4.4499999999999993 | 4.5499999999999989 | 4.8499999999999988 | 5.3499999999999988 | 5.8499999999999988 | 6.3499999999999988 | 6.8499999999999988 | 7.3499999999999988 | 7.8499999999999988 | 8.3500000000000014 | 9.3500000000000014
7Be - Experiment (1st) | 5.5921e-11 | 6.2838e-11 | 6.4283e-11 | 7.0565e-11 | 6.9221e-11 | 6.9956e-11 | 8.6016e-11 | 9.3783e-11 | 2.0888e-10 | 3.6378e-10 | 1.5861e-10 | 6.7523e-11 | 4.3837e-11 | 4.5687e-11 | 2.7145e-11 | 4.3785e-11 | 3.4118e-11 | 4.0155e-11 | 2.6728e-11 | 3.3686e-11 | 3.319e-11 | 5.7004e-11 | 5.685e-11 | 5.6602e-11 | 4.432e-11 | 6.353e-11 | 3.427e-11 | 3.4247e-11 | 4.5303e-11 | 1.6121e-11 | 1.5603e-11
7Be - Experiment (2nd) | 5.8572e-11 | 6.1848e-11 | 6.2538e-11 | 7.0076e-11 | 7.3934e-11 | 6.8646e-11 | 7.329e-11 | 7.6228e-11 | 8.2893e-11 | 1.0723e-10 | 4.4036e-11 | 3.4202e-11 | 3.8361e-11 | 3.8548e-11 | 4.5413e-11 | 4.281e-11 | 3.4457e-11 | 3.5876e-11 | 2.5619e-11 | 3.134e-11 | 3.2197e-11 | 4.3741e-11 | 4.2263e-11 | 5.7148e-11 | 4.8353e-11 | 4.1959e-11 | 3.143e-11 | 3.3394e-11 | 2.5562e-11 | 1.6462e-11 | 1.079e-11
7Be - Experiment (3rd) | 5.8187e-11 | 6.381e-11 | 6.9366e-11 | 7.3129e-11 | 7.3377e-11 | 6.6967e-11 | 7.371e-11 | 6.4671e-11 | 5.6048e-11 | 5.8743e-11 | 3.6946e-11 | 3.3111e-11 | 3.0263e-11 | 1.8956e-11 | 3.0413e-11 | 3.689e-11 | 2.7243e-11 | 3.0794e-11 | 1.761e-11 | 2.3423e-11 | 2.197e-11 | 3.2899e-11 | 4.0425e-11 | 4.279e-11 | 4.4745e-11 | 3.2108e-11 | 2.7313e-11 | 2.2678e-11 | 1.261e-11 | 6.2632e-12 | 9.9688e-12
7Be - Simulation (1d) | 5.7322e-11 | 6.2044e-11 | 6.0186e-11 | 5.5584e-11 | 5.4486e-11 | 7.6335e-11 | 8.8202e-11 | 1.0513e-10 | 9.9777e-11 | 1.027e-10 | 9.1862e-11 | 7.8916e-11 | 7.3609e-11 | 6.7936e-11 | 5.8054e-11 | 5.9747e-11 | 5.6362e-11 | 5.3022e-11 | 5.014e-11 | 4.9042e-11 | 4.3882e-11 | 4.0684e-11 | 3.8611e-11 | 3.5528e-11 | 3.0596e-11 | 2.9681e-11 | 2.529e-11 | 2.27e-11 | 2.2609e-11 | 2.0138e-11 | 1.9287e-11
Chart: Depth [mm]
| 0.25 | 0.75000000000000011 | 1.25 | 1.75 | 2.25 | 2.75 | 3.05 | 3.15 | 3.25 | 3.3499999999999996 | 3.4499999999999997 | 3.5500000000000003 | 3.6500000000000004 | 3.7500000000000004 | 3.85 | 3.95 | 4.0500000000000007 | 4.1499999999999995 | 4.25 | 4.3499999999999996 | 4.4499999999999993 | 4.5499999999999989 | 4.8499999999999988 | 5.3499999999999988 | 5.8499999999999988 | 6.3499999999999988 | 6.8499999999999988 | 7.3499999999999988 | 7.8499999999999988 | 8.3500000000000014 | 8.8500000000000014
22Na - Experiment (1st) | 2.2449e-12 | 2.7604e-12 | 2.795e-12 | 3.5625e-12 | 3.7754e-12 | 3.5235e-12 | 4.5097e-12 | 4.2328e-12 | 5.6839e-12 | 9.9413e-12 | 6.8752e-12 | 4.097e-12 | 4.4916e-12 | 3.152e-12 | 2.978e-12 | 3.3467e-12 | 3.6055e-12 | 2.7635e-12 | 3.1974e-12 | 4.4444e-12 | 3.6871e-12 | 3.548e-12 | 4.0469e-12 | 4.0376e-12 | 3.5246e-12 | 3.6596e-12 | 3.4213e-12 | 3.4567e-12 | 2.9136e-12 | 2.8799e-12 | 2.919e-12
22Na - Experiment (2nd) | 2.3672e-12 | 2.7802e-12 | 3.3157e-12 | 3.5406e-12 | 3.643e-12 | 3.8934e-12 | 4.2848e-12 | 3.6433e-12 | 4.1041e-12 | 3.6572e-12 | 2.7636e-12 | 3.2296e-12 | 3.2178e-12 | 3.0622e-12 | 3.4311e-12 | 3.4673e-12 | 3.2846e-12 | 3.1578e-12 | 3.4629e-12 | 3.51e-12 | 2.789e-12 | 3.038e-12 | 3.5633e-12 | 4.0286e-12 | 3.5176e-12 | 3.6511e-12 | 3.4126e-12 | 3.6229e-12 | 3.3348e-12 | 3.0195e-12 | 2.9961e-12
22Na - Experiment (3rd) | 2.3535e-12 | 2.753e-12 | 3.121e-12 | 3.4942e-12 | 3.8881e-12 | 3.7561e-12 | 4.4246e-12 | 4.2531e-12 | 4.0837e-12 | 3.4243e-12 | 2.9403e-12 | 3.4664e-12 | 3.0854e-12 | 3.5054e-12 | 3.3527e-12 | 3.5678e-12 | 3.1422e-12 | 3.8185e-12 | 3.2006e-12 | 3.2874e-12 | 2.8878e-12 | 3.6417e-12 | 3.7235e-12 | 4.0121e-12 | 3.8198e-12 | 3.5567e-12 | 3.5935e-12 | 3.6181e-12 | 3.2475e-12 | 3.1337e-12 | 3.0091e-12
22Na - Simulation (1d) | 2.1736e-12 | 2.7222e-12 | 3.3676e-12 | 4.3699e-12 | 5.3975e-12 | 6.2254e-12 | 6.5525e-12 | 7.1716e-12 | 6.8553e-12 | 5.9334e-12 | 3.3861e-12 | 2.9157e-12 | 2.7362e-12 | 2.7873e-12 | 2.5139e-12 | 2.32e-12 | 2.4967e-12 | 2.3341e-12 | 2.471e-12 | 2.2572e-12 | 2.4882e-12 | 2.2572e-12 | 2.2342e-12 | 2.1646e-12 | 2.0742e-12 | 2.151e-12 | 2.0381e-12 | 1.9956e-12 | 2.0164e-12 | 2.0317e-12 | 1.9875e-12
Chart: Depth [mm]
| 0.25 | 0.75000000000000011 | 1.25 | 1.75 | 2.25 | 2.75 | 3.05 | 3.15 | 3.25 | 3.3499999999999996 | 3.4499999999999997 | 3.5500000000000003 | 3.6500000000000004 | 3.7500000000000004 | 3.85 | 3.95 | 4.0500000000000007 | 4.1499999999999995 | 4.25 | 4.3499999999999996 | 4.4499999999999993 | 4.5499999999999989 | 4.8499999999999988 | 5.3499999999999988 | 5.8499999999999988 | 6.3499999999999988 | 6.8499999999999988 | 7.3499999999999988 | 7.8499999999999988 | 8.3500000000000014 | 8.8500000000000014
88Y - Experiment (1st) | 0 | 0 | 0 | 0 | 0 | 5.3001e-14 | 1.3982e-13 | 4.3612e-13 | 1.6622e-12 | 4.6011e-12 | 4.235e-12 | 4.2303e-12 | 3.7265e-12 | 3.2833e-12 | 3.1408e-12 | 3.0337e-12 | 3.0717e-12 | 2.4955e-12 | 2.4989e-12 | 2.9521e-12 | 2.5283e-12 | 2.4254e-12 | 2.323e-12 | 1.7244e-12 | 1.3107e-12 | 1.7999e-12 | 1.5317e-12 | 9.2609e-13 | 1.6664e-12 | 1.4986e-12 | 1.0833e-12
88Y - Experiment (2nd) | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 1.2423e-12 | 7.3497e-12 | 1.6692e-11 | 1.6733e-11 | 1.5131e-11 | 1.461e-11 | 1.3569e-11 | 1.2537e-11 | 1.2175e-11 | 1.2371e-11 | 1.1152e-11 | 1.111e-11 | 1.0992e-11 | 1.1464e-11 | 1.095e-11 | 9.4423e-12 | 7.0527e-12 | 5.1319e-12 | 7.2396e-12 | 5.252e-12 | 3.5112e-12 | 5.706e-12 | 5.706e-12 | 3.9248e-12
88Y - Experiment (3rd) | 0 | 0 | 0 | 0 | 0 | 1.9419e-13 | 1.4682e-12 | 1.8578e-12 | 7.5287e-12 | 1.9392e-11 | 1.8061e-11 | 1.7695e-11 | 1.6117e-11 | 1.4703e-11 | 1.3342e-11 | 1.2694e-11 | 1.3103e-11 | 1.3221e-11 | 1.2548e-11 | 1.1439e-11 | 1.2762e-11 | 1.232e-11 | 1.0808e-11 | 8.1362e-12 | 5.7133e-12 | 8.5904e-12 | 6.588e-12 | 5.0778e-12 | 7.7597e-12 | 7.0181e-12 | 5.3548e-12
88Y - Simulation | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 8.4949e-13 | 1.4681e-11 | 1.844e-11 | 1.4158e-11 | 1.0031e-11 | 8.7403e-12 | 8.513e-12 | 7.1313e-12 | 6.8541e-12 | 7.6086e-12 | 6.7859e-12 | 9.5993e-12 | 7.7722e-12 | 7.6176e-12 | 5.6805e-12 | 3.1361e-12 | 2.2907e-12 | 1.1599e-12 | 4.7315e-13 | 3.8143e-13 | 2.2844e-13 | 1.5226e-14 | 0
Chart: Depth [mm]
| 0.25 | 0.75000000000000011 | 1.25 | 1.75 | 2.25 | 2.75 | 3.05 | 3.15 | 3.25 | 3.3499999999999996 | 3.4499999999999997 | 3.5500000000000003 | 3.6500000000000004 | 3.7500000000000004 | 3.85 | 3.95 | 4.0500000000000007 | 4.1499999999999995 | 4.25 | 4.3499999999999996 | 4.4499999999999993 | 4.5499999999999989 | 4.8499999999999988 | 5.3499999999999988 | 5.8499999999999988 | 6.3499999999999988 | 6.8499999999999988 | 7.3499999999999988 | 7.8499999999999988 | 8.3500000000000014 | 8.8500000000000014
237U - Experiment (1st) | 1.5183e-13 | 1.7106e-12 | 0 | 0 | 1.0011e-12 | 1.4049e-10 | 1.8369e-09 | 1.6506e-09 | 2.0037e-09 | 2.1535e-08 | 2.6995e-08 | 6.8001e-10 | 3.4453e-10 | 1.5284e-10 | 7.4868e-11 | 2.309e-11 | 2.6335e-11 | 0 | 2.6029e-11 | 1.7227e-11 | 2.2376e-11 | 2.87e-12 | 4.5903e-10 | 8.1308e-12 | 1.22e-10 | 3.1564e-09 | 7.2719e-11 | 2.4423e-11 | 3.1022e-09 | 4.6175e-11 | 8.1367e-12
237U - Experiment (2nd) | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 4.9318e-10 | 3.0896e-08 | 1.4601e-09 | 7.8718e-10 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 1.0504e-10 | 3.646e-09 | 6.1497e-11 | 0 | 0 | 0 | 0
237U - Experiment (3rd) | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 3.8559e-08 | 3.3855e-08 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
237U - Simulation | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 1.3511e-08 | 2.8053e-08 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0 | 0
Examples of the produced nuclides in Aluminium target
after irradiation by Uranium beam with energy 200MeV/u

## Slide 17
Beam-loss criteria
N. V. Mokhov and W. Chou (Eds.), Beam Halo and Scraping, The 7th ICFA Miniworkshop on High Intensity High Brightness Hadron Beams, Wisconsin, USA, 13-15 September 1999
. the tolerable beam-loss level of 1 W/m
. proton beam
. energy above100 MeV
. uniformly distributed along the beam line
. 100 days of operation
. at 30 cm (1 foot) from the component surface
. 4 hours after shutdown
. Dose rate bellow 1 mSv/h
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 18
Beam-loss criteria
. beam-loss criteria for heavy-ion accelerators
Ion 1GeV/u | Number of particles/s equivalent to 1W
1 H | 6.24E+09
4 He | 1.56E+09
12 C | 5.20E+08
20 Ne | 3.12E+08
40Ar | 1.56E+08
84 Kr | 7.43E+07
132 Xe | 4.73E+07
197 Au | 3.17E+07
238 U | 2.62E+07
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 19
Previous simulations
FLUKA 2008.3.6
. target materials: stainless steel, cooper
. primary beams: 1H, 4He, 12C, 20Ne, 40Ar, 84Kr, 132Xe, 197Au, 238U
. beam energies: 200MeV/u ÷ 1GeV/u
. target geometry: beam-pipe, bulky target
. normalized induced activities | beam power of 1 W | 3 months of irradiation
. several time points after irradiation
I.STRASIK, E.MUSTAFIN, M.Pavlovic: Residual activity induced by heavy ions and beam-loss criteria for heavy-ion accelerators, Phys. Rev. ST accel. Beams 13, 071004 (2010)
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 20
Previous simulations
FLUKA 2008.3.6
BULKY TARGET.
. target materials: cooper
. diameter 20 cm
. length 60 cm
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 21
Generic curve
FLUKA 2008.3.6
. time evolution of the activity
. independent from the projectile mass
. activity normalized to the activity at the end of irradiation
. obtained by averaging the data points of the individual curves corresponding to different primary ions
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]
. Time evolution of the relative activity in the Beam pipe by different projectiles at 500 MeV/u
. Inventory of nuclides produced in the Beam pipe by different projectiles at 500 MeV/u

## Slide 22
Scaling law
FLUKA 2008.3.6
SCALING LAW FOR BEAM-LOSS TOLERANCE.
. relative activities
. are not strongly depend on the projectile species
. dependent on the target material
( isotopes produced mostly by secondary particles)
. the activity induced by 1 W/m of beam losses is decreasing
. with increasing ion mass
. with decreasing energy
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]
. The Scaling factor is represented by the ratio of the normalized activity induced by 1 GeV proton beam, Ap (1GeV), to the normalized activity induced by the beam of interest at given energy, Ai(E).
. The activities were calculated by FLUKA at the end of Irradiation.
. The relative standard uncertainty of the presented data is less than 0.76%.

## Slide 23
FLUKA versions
FLUKA 2008.3.6
. beam energies: 200MeV/u ÷ 1GeV/u
. threshold for inelastic nucleus-nucleus interaction = 100MeV/u
FLUKA 2011.2b.5
. new version allows a treatment below 100MeV/u for heavy ion
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 24
New simulations
FLUKA 2011.2b.5
. target materials: cooper
. primary beams: 1H, 4He, 12C, 20Ne, 40Ar, 84Kr, 132Xe, 197Au, 238U
. beam energies: 25 MeV/u ÷ 1GeV/u
. target geometry: bulky target
. normalized induced activities | beam power of 1 W | 3 months of irradiation
. several time points after irradiation
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 25
New simulations
DEFAULTS NEW-DEFA
BEAM -2.0 0.0 0.0 -0.58875 -0.58875 4-HELIUM
BEAMPOS 0.0 0.0 -31.0
PHYSICS 3. EVAPORAT
PHYSICS 1. COALESCE
PHYSICS 2. EM-DISSO
IONTRANS 4-HELIUM (HEAVYION, 0.0)
GEOBEGIN COMBNAME
FLUKA 2011.2b.5
. evaporation model with heavy-fragment evaporation
. emission of high-energy light fragments through the coalescence mechanism
. ion electromagnetic dissociation
. the heavy-ion transport with nuclear interactions
. low-energy neutron transport was simulated down to thermal energies
. residual nuclei from low-energy neutron interactions were scored
INPUT FILES.
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 26
Generic Curves | 1 GeV/u
Chart: Time [days]
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 27
Generic Curves | 900 MeV/u
Chart: Time [days]
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 28
Generic Curves | 800 MeV/u
Chart: Time [days]
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 29
Generic Curves | 700 MeV/u
Chart: Time [days]
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 30
Generic Curves | 600 MeV/u
Chart: Time [days]
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 31
Generic Curves | 500 MeV/u
Chart: Time [days]
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 32
Generic Curves | 400 MeV/u
Chart: Time [days]
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 33
Generic Curves | 300 MeV/u
Chart: Time [days]
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 34
Generic Curves | 200 MeV/u
Chart: Time [days]
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 35
Generic Curves | 150 MeV/u
Chart: Time [days]
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 36
Generic Curves | 100 MeV/u
Chart: Time [days]
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 37
Generic Curves | 50 MeV/u
Chart: Time [days]
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 38
Generic Curves | 25 MeV/u
Chart: Time [days]
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 39
INDUCED ISOTOPES | 1 GeV/u
Chart: Induced isotopes
| Cu-64 | Co-58 | Cr-51 | Co-57 | Co-56 | V-48 | Mn-54 | Mn-52
1H | 29.4804 | 21.4535 | 10.0165 | 7.1481 | 5.9279 | 5.0356 | 2.7386 | 2.7814
4He | 34.527 | 23.5561 | 7.7868 | 6.9819 | 5.1542 | 3.5416 | 2.5068 | 2.0897
12C | 34.1041 | 24.189 | 7.8435 | 7.2208 | 5.3641 | 3.4308 | 2.5512 | 2.1387
20Ne | 33.6571 | 24.3701 | 7.9256 | 7.3293 | 5.4612 | 3.4433 | 2.5983 | 2.1525
40Ar | 32.9535 | 24.4042 | 8.1302 | 7.4055 | 5.5517 | 3.5274 | 2.652 | 2.2015
84Kr | 32.2515 | 24.3148 | 8.3744 | 7.4472 | 5.627 | 3.6598 | 2.703 | 2.2668
132Xe | 31.8474 | 24.1562 | 8.5144 | 7.4317 | 5.647 | 3.7448 | 2.7236 | 2.3017
197Au | 31.4766 | 23.9033 | 8.5602 | 7.3793 | 5.6256 | 3.7796 | 2.7217 | 2.3134
238U | 31.478 | 23.8731 | 8.6115 | 7.3711 | 5.6286 | 3.8025 | 2.7319 | 2.3231
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 40
INDUCED ISOTOPES | 1 GeV/u
Chart: Induced isotopes
| Cu-64 | Co-58 | Cr-51 | Co-57 | Co-56 | V-48 | Mn-54 | Mn-52 | Fe-55 | V-49 | Fe-59
1H | 29.4804 | 21.4535 | 10.0165 | 7.1481 | 5.9279 | 5.0356 | 2.7386 | 2.7814 | 1.6108 | 1.599 | 0.87326
4He | 34.527 | 23.5561 | 7.7868 | 6.9819 | 5.1542 | 3.5416 | 2.5068 | 2.0897 | 1.4373 | 1.1731 | 1.0811
12C | 34.1041 | 24.189 | 7.8435 | 7.2208 | 5.3641 | 3.4308 | 2.5512 | 2.1387 | 1.4891 | 1.1556 | 1.0891
20Ne | 33.6571 | 24.3701 | 7.9256 | 7.3293 | 5.4612 | 3.4433 | 2.5983 | 2.1525 | 1.5136 | 1.1607 | 1.09
40Ar | 32.9535 | 24.4042 | 8.1302 | 7.4055 | 5.5517 | 3.5274 | 2.652 | 2.2015 | 1.5434 | 1.1908 | 1.0949
84Kr | 32.2515 | 24.3148 | 8.3744 | 7.4472 | 5.627 | 3.6598 | 2.703 | 2.2668 | 1.5696 | 1.2324 | 1.0968
132Xe | 31.8474 | 24.1562 | 8.5144 | 7.4317 | 5.647 | 3.7448 | 2.7236 | 2.3017 | 1.5795 | 1.2586 | 1.0913
197Au | 31.4766 | 23.9033 | 8.5602 | 7.3793 | 5.6256 | 3.7796 | 2.7217 | 2.3134 | 1.575 | 1.269 | 1.0783
238U | 31.478 | 23.8731 | 8.6115 | 7.3711 | 5.6286 | 3.8025 | 2.7319 | 2.3231 | 1.5781 | 1.2756 | 1.0856
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 41
INDUCED ISOTOPES | 900 MeV/u
Chart: Induced isotopes
| Cu-64 | Co-58 | Cr-51 | Co-57 | Co-56 | V-48 | Mn-54 | Mn-52 | Fe-55 | V-49 | Fe-59
1H | 29.2965 | 21.8144 | 10.0647 | 7.3585 | 6.1313 | 4.9179 | 2.768 | 2.8289 | 1.6452 | 1.5788 | 0.87001
4He | 34.8179 | 23.7725 | 7.6729 | 6.9859 | 5.1301 | 3.4515 | 2.4816 | 2.0592 | 1.4266 | 1.1483 | 1.0925
12C | 34.362 | 24.4527 | 7.6709 | 7.2685 | 5.3552 | 3.3035 | 2.5415 | 2.0806 | 1.4833 | 1.1192 | 1.0978
20Ne | 33.8571 | 24.7057 | 7.7491 | 7.3944 | 5.4711 | 3.3166 | 2.5784 | 2.1052 | 1.5102 | 1.1234 | 1.0962
40Ar | 33.1002 | 24.7763 | 7.9755 | 7.4698 | 5.563 | 3.3914 | 2.6437 | 2.1597 | 1.5443 | 1.1536 | 1.1059
84Kr | 32.3508 | 24.6888 | 8.2363 | 7.5218 | 5.6505 | 3.5305 | 2.7026 | 2.2335 | 1.5745 | 1.1991 | 1.1106
132Xe | 31.9297 | 24.5062 | 8.3979 | 7.5121 | 5.6794 | 3.6063 | 2.729 | 2.2692 | 1.5862 | 1.224 | 1.1074
197Au | 31.5069 | 24.2359 | 8.4314 | 7.4537 | 5.6594 | 3.6449 | 2.7263 | 2.282 | 1.5823 | 1.234 | 1.0975
238U | 31.5062 | 24.1993 | 8.488 | 7.4545 | 5.6661 | 3.6688 | 2.7361 | 2.291 | 1.587 | 1.243 | 1.1012
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 42
INDUCED ISOTOPES | 800 MeV/u
Chart: Induced isotopes
| Cu-64 | Co-58 | Cr-51 | Co-57 | Co-56 | V-48 | Mn-54 | Mn-52 | Fe-55 | V-49 | Fe-59
1H | 29.1377 | 22.3589 | 9.9915 | 7.5785 | 6.3976 | 4.7842 | 2.8008 | 2.8524 | 1.6812 | 1.5352 | 0.8434
4He | 35.1501 | 23.9815 | 7.5251 | 6.986 | 5.1036 | 3.3784 | 2.4534 | 2.0199 | 1.4129 | 1.1196 | 1.0984
12C | 34.6539 | 24.8088 | 7.4548 | 7.2995 | 5.3392 | 3.1507 | 2.516 | 2.0217 | 1.4721 | 1.0784 | 1.1115
20Ne | 34.1273 | 25.1046 | 7.5442 | 7.4355 | 5.4501 | 3.1643 | 2.5543 | 2.052 | 1.5004 | 1.0803 | 1.1141
40Ar | 33.3003 | 25.1866 | 7.7619 | 7.5462 | 5.568 | 3.2295 | 2.6302 | 2.1056 | 1.5418 | 1.1104 | 1.1267
84Kr | 32.4948 | 25.107 | 8.0631 | 7.6129 | 5.6775 | 3.363 | 2.6992 | 2.1836 | 1.5791 | 1.1563 | 1.132
132Xe | 32.0455 | 24.9378 | 8.2117 | 7.6108 | 5.7105 | 3.4366 | 2.7283 | 2.2254 | 1.5923 | 1.18 | 1.1282
197Au | 31.5788 | 24.6066 | 8.2603 | 7.5447 | 5.6873 | 3.4721 | 2.7267 | 2.2354 | 1.587 | 1.1897 | 1.1179
238U | 31.5761 | 24.5906 | 8.3234 | 7.5451 | 5.6926 | 3.4959 | 2.7373 | 2.2481 | 1.5939 | 1.1999 | 1.1215
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 43
INDUCED ISOTOPES | 700 MeV/u
Chart: Induced isotopes
| Cu-64 | Co-58 | Cr-51 | Co-57 | Co-56 | V-48 | Mn-54 | Mn-52 | Fe-55 | Fe-59 | V-49
1H | 28.9048 | 23.0063 | 9.9138 | 7.9014 | 6.7207 | 4.5539 | 2.8178 | 2.8728 | 1.739 | 0.82073 | 1.4852
4He | 35.4875 | 24.2338 | 7.3831 | 6.979 | 5.0414 | 3.2815 | 2.4275 | 1.9725 | 1.3944 | 1.1148 | 1.1006
12C | 35.0164 | 25.1797 | 7.1923 | 7.3344 | 5.2904 | 2.9845 | 2.4793 | 1.9525 | 1.4547 | 1.1273 | 1.0253
20Ne | 34.4199 | 25.5461 | 7.2849 | 7.4874 | 5.4287 | 2.9732 | 2.5202 | 1.9752 | 1.4898 | 1.1358 | 1.0286
40Ar | 33.5676 | 25.6651 | 7.4895 | 7.6181 | 5.556 | 3.0224 | 2.6051 | 2.0321 | 1.5362 | 1.1502 | 1.0549
84Kr | 32.7278 | 25.5951 | 7.8093 | 7.7083 | 5.6832 | 3.1466 | 2.6902 | 2.1143 | 1.5793 | 1.1612 | 1.1022
132Xe | 32.2316 | 25.4398 | 7.9708 | 7.7124 | 5.732 | 3.2145 | 2.722 | 2.1589 | 1.5962 | 1.1577 | 1.1211
197Au | 31.7082 | 25.0792 | 8.0067 | 7.6326 | 5.6995 | 3.2479 | 2.7198 | 2.1694 | 1.5917 | 1.1429 | 1.1306
238U | 31.704 | 25.0611 | 8.0726 | 7.6433 | 5.7114 | 3.2674 | 2.7373 | 2.1822 | 1.5996 | 1.1442 | 1.1381
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 44
INDUCED ISOTOPES | 600 MeV/u
Chart: Induced isotopes
| Cu-64 | Co-58 | Co-57 | Cr-51 | Co-56 | V-48 | Mn-54 | Mn-52 | Fe-55 | Fe-59 | V-49
1H | 28.6781 | 23.8324 | 8.3571 | 9.6513 | 7.1081 | 4.2358 | 2.8377 | 2.8698 | 1.7983 | 0.81013 | 1.3915
4He | 35.8044 | 24.4912 | 6.9701 | 7.2433 | 4.9519 | 3.2132 | 2.3834 | 1.9252 | 1.3734 | 1.1404 | 1.0815
12C | 35.3894 | 25.6233 | 7.3425 | 6.8661 | 5.2216 | 2.7844 | 2.4262 | 1.8596 | 1.4317 | 1.1544 | 0.96981
20Ne | 34.8331 | 26.0222 | 7.5154 | 6.9293 | 5.35 | 2.7603 | 2.4715 | 1.8854 | 1.466 | 1.1641 | 0.96833
40Ar | 33.9163 | 26.2057 | 7.6724 | 7.148 | 5.5121 | 2.7751 | 2.565 | 1.9329 | 1.5192 | 1.1766 | 0.9838
84Kr | 33.0643 | 26.2001 | 7.7931 | 7.4543 | 5.6726 | 2.8857 | 2.6649 | 2.0144 | 1.5719 | 1.1927 | 1.0261
132Xe | 32.5359 | 26.0424 | 7.8196 | 7.6214 | 5.7259 | 2.93 | 2.6986 | 2.0576 | 1.5956 | 1.1902 | 1.0432
197Au | 31.9056 | 25.6281 | 7.7311 | 7.6531 | 5.6951 | 2.9448 | 2.6999 | 2.0745 | 1.5879 | 1.172 | 1.0492
238U | 31.9056 | 25.6183 | 7.7381 | 7.7192 | 5.7088 | 2.9786 | 2.7197 | 2.0886 | 1.5984 | 1.1787 | 1.0611
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 45
INDUCED ISOTOPES | 500 MeV/u
Chart: Induced isotopes
| Cu-64 | Co-58 | Co-57 | Cr-51 | Co-56 | Mn-54 | V-48 | Mn-52 | Fe-55 | Fe-59 | V-49
1H | 28.4607 | 25.0409 | 8.898 | 9.233 | 7.5582 | 2.8466 | 3.6791 | 2.8169 | 1.8731 | 0.79093 | 1.2637
4He | 36.0946 | 24.7643 | 6.9057 | 7.1124 | 4.8526 | 2.3436 | 3.1732 | 1.8753 | 1.3465 | 1.1687 | 1.0684
12C | 35.8205 | 26.028 | 7.2952 | 6.4819 | 5.0704 | 2.357 | 2.571 | 1.7475 | 1.391 | 1.1718 | 0.90038
20Ne | 35.3404 | 26.5248 | 7.5089 | 6.4866 | 5.2346 | 2.3899 | 2.5102 | 1.7569 | 1.428 | 1.1754 | 0.88937
40Ar | 34.4534 | 26.7921 | 7.6991 | 6.6435 | 5.4096 | 2.4988 | 2.4587 | 1.7986 | 1.4899 | 1.206 | 0.89285
84Kr | 33.547 | 26.9249 | 7.8725 | 6.9668 | 5.5991 | 2.6063 | 2.5425 | 1.873 | 1.5503 | 1.2284 | 0.92842
132Xe | 33.0041 | 26.7678 | 7.909 | 7.0937 | 5.6694 | 2.6562 | 2.5657 | 1.9159 | 1.5799 | 1.222 | 0.94036
197Au | 32.2356 | 26.2848 | 7.8134 | 7.1231 | 5.6396 | 2.6547 | 2.569 | 1.9251 | 1.5746 | 1.2074 | 0.94142
238U | 32.2529 | 26.2858 | 7.8398 | 7.185 | 5.669 | 2.6763 | 2.5943 | 1.9395 | 1.5857 | 1.2118 | 0.95229
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 46
INDUCED ISOTOPES | 400 MeV/u
Chart: Induced isotopes
| Cu-64 | Co-58 | Co-57 | Cr-51 | Co-56 | Mn-54 | V-48 | Mn-52 | Fe-55 | Fe-59 | V-49
1H | 28.0735 | 26.5 | 9.5632 | 8.5142 | 8.1177 | 2.8116 | 3.0611 | 2.7244 | 1.9157 | 0.74712 | 1.0771
4He | 36.1591 | 24.967 | 6.8113 | 7.0339 | 4.7058 | 2.3017 | 3.2136 | 1.8343 | 1.3031 | 1.2129 | 1.0759
12C | 36.2492 | 26.3378 | 7.193 | 5.9852 | 4.8434 | 2.2373 | 2.3695 | 1.6043 | 1.3255 | 1.205 | 0.82952
20Ne | 35.9882 | 26.9487 | 7.4098 | 5.9181 | 4.9887 | 2.2599 | 2.245 | 1.5847 | 1.3563 | 1.2108 | 0.80019
40Ar | 35.2304 | 27.3946 | 7.6538 | 5.9262 | 5.1889 | 2.376 | 2.0984 | 1.6008 | 1.4287 | 1.2312 | 0.77402
84Kr | 34.3613 | 27.6302 | 7.8693 | 6.2316 | 5.4024 | 2.5086 | 2.1311 | 1.6753 | 1.5049 | 1.2705 | 0.80135
132Xe | 33.755 | 27.5665 | 7.9481 | 6.3258 | 5.5185 | 2.5617 | 2.1031 | 1.7015 | 1.5347 | 1.2697 | 0.79939
197Au | 32.8136 | 26.9558 | 7.8385 | 6.3575 | 5.4648 | 2.5467 | 2.0883 | 1.7011 | 1.5331 | 1.2427 | 0.80032
238U | 32.8361 | 27.0475 | 7.879 | 6.3937 | 5.5102 | 2.5786 | 2.0912 | 1.7239 | 1.5487 | 1.2517 | 0.80237
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 47
INDUCED ISOTOPES | 300 MeV/u
Chart: Induced isotopes
| Cu-64 | Co-58 | Co-57 | Cr-51 | Co-56 | Mn-54 | V-48 | Fe-55 | Mn-52 | Fe-59 | H-3
1H | 27.6312 | 28.2829 | 10.3311 | 7.4947 | 8.6278 | 2.6765 | 2.3839 | 1.9388 | 2.4358 | 0.69511 | 0.48523
4He | 35.6785 | 24.8523 | 6.6031 | 7.0893 | 4.4596 | 2.2501 | 3.3465 | 1.2495 | 1.8169 | 1.2691 | 0.80979
12C | 36.5278 | 26.2261 | 6.8492 | 5.4551 | 4.4384 | 2.0603 | 2.2568 | 1.2141 | 1.4501 | 1.1965 | 0.98049
20Ne | 36.8028 | 26.9182 | 7.0902 | 5.1459 | 4.5075 | 2.0492 | 2.0509 | 1.2344 | 1.3689 | 1.1992 | 1.1184
40Ar | 36.3663 | 27.6941 | 7.3947 | 4.9555 | 4.7362 | 2.1341 | 1.6804 | 1.302 | 1.3218 | 1.2398 | 1.1454
84Kr | 35.7071 | 28.2124 | 7.694 | 5.1661 | 4.9967 | 2.293 | 1.6294 | 1.3936 | 1.3677 | 1.285 | 1.0817
132Xe | 35.0333 | 28.2732 | 7.7959 | 5.1747 | 5.114 | 2.3494 | 1.546 | 1.4298 | 1.3712 | 1.2884 | 0.99431
197Au | 33.7729 | 27.5462 | 7.693 | 5.1569 | 5.0546 | 2.3201 | 1.4992 | 1.4259 | 1.3742 | 1.2497 | 0.90848
238U | 33.8579 | 27.6807 | 7.7602 | 5.2402 | 5.1342 | 2.3662 | 1.5003 | 1.4461 | 1.3866 | 1.2786 | 0.8803
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 48
INDUCED ISOTOPES | 200 MeV/u
Chart: Induced isotopes
| Cu-64 | Co-58 | Co-57 | Co-56 | Cr-51 | Mn-54 | Fe-59 | Fe-55 | H-3 | U-237 | Be-7
1H | 27.2554 | 31.1638 | 11.4047 | 9.1982 | 5.2939 | 2.3161 | 0.57044 | 1.8808 | 0.42537 | 0 | 0.29044
4He | 33.1016 | 22.5942 | 5.8661 | 4.0203 | 7.3025 | 2.1026 | 1.2205 | 1.1249 | 1.4236 | 0 | 4.1815
12C | 35.2049 | 24.2523 | 5.9513 | 3.6951 | 5.3541 | 1.7983 | 1.0799 | 1.0167 | 1.419 | 0 | 6.4892
20Ne | 36.8685 | 24.8361 | 6.0921 | 3.6129 | 4.4734 | 1.6364 | 1.085 | 0.97878 | 1.7135 | 0 | 6.4936
40Ar | 37.9508 | 26.4001 | 6.5014 | 3.7708 | 3.7203 | 1.6849 | 1.1467 | 1.0354 | 1.755 | 0 | 3.9801
84Kr | 37.9183 | 27.7231 | 6.9882 | 4.1118 | 3.6908 | 1.837 | 1.2348 | 1.1375 | 1.6165 | 0 | 2.4003
132Xe | 37.3019 | 28.0136 | 7.1353 | 4.2262 | 3.4943 | 1.8855 | 1.2439 | 1.1748 | 1.4139 | 0 | 1.5233
197Au | 35.5153 | 27.3177 | 7.0327 | 4.1737 | 3.4085 | 1.8523 | 1.2355 | 1.1699 | 1.2312 | 0 | 1.1536
238U | 35.971 | 27.804 | 7.1716 | 4.2735 | 3.4455 | 1.8954 | 1.2508 | 1.1975 | 1.1615 | 0.9642 | 0.89973
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 49
INDUCED ISOTOPES | 150 MeV/u
Chart: Induced isotopes
| Cu-64 | Co-58 | Co-57 | Co-56 | Cr-51 | Mn-54 | H-3 | Fe-59 | Be-7 | Fe-55 | U-237
1H | 27.6068 | 33.1901 | 12.0356 | 9.0233 | 3.4912 | 1.9696 | 0.358 | 0.50088 | 0.23544 | 1.71 | 0
4He | 28.5407 | 16.6388 | 4.4181 | 3.3412 | 7.4182 | 1.7875 | 2.3819 | 0.89376 | 8.9257 | 0.931 | 0
12C | 31.6869 | 20.0963 | 4.9084 | 3.1262 | 6.1525 | 1.6507 | 2.2047 | 0.82449 | 11.307 | 0.89027 | 0
20Ne | 34.8991 | 20.4447 | 4.7732 | 2.8098 | 4.6479 | 1.3286 | 2.7151 | 0.83663 | 11.2014 | 0.7562 | 0
40Ar | 38.4567 | 23.7894 | 5.4537 | 2.938 | 2.9846 | 1.2717 | 2.6479 | 0.98298 | 6.5507 | 0.79153 | 0
84Kr | 39.4418 | 26.1172 | 6.1117 | 3.2618 | 2.9055 | 1.4726 | 2.2851 | 1.1282 | 3.699 | 0.9045 | 0
132Xe | 38.9305 | 26.9149 | 6.411 | 3.4471 | 2.5668 | 1.4811 | 1.9051 | 1.1807 | 2.1537 | 0.94389 | 0
197Au | 37.0569 | 26.3827 | 6.3471 | 3.4349 | 2.457 | 1.4705 | 1.603 | 1.1703 | 1.5734 | 0.94506 | 0
238U | 37.999 | 27.2933 | 6.5666 | 3.5612 | 2.4348 | 1.53 | 1.4967 | 1.2222 | 1.2163 | 0.98703 | 0.75056
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 50
INDUCED ISOTOPES | 100 MeV/u
Chart: Induced isotopes
| Cu-64 | Co-58 | Co-57 | Co-56 | H-3 | Be-7 | Cr-51 | Fe-59 | Mn-54 | Co-60 | Fe-55
1H | 29.3469 | 35.8152 | 11.9843 | 7.9436 | 0.23058 | 0.10735 | 1.0637 | 0.36973 | 1.1445 | 0.41804 | 1.2186
4He | 19.6516 | 9.0325 | 3.006 | 3.07 | 2.7131 | 12.2366 | 10.9306 | 0.40459 | 1.784 | 0.29359 | 0.85683
12C | 25.9185 | 13.3606 | 3.4407 | 2.71 | 2.6426 | 16.5439 | 8.2591 | 0.40783 | 1.7162 | 0.38587 | 0.80801
20Ne | 30.8999 | 13.3524 | 2.9255 | 1.7834 | 3.5138 | 17.3883 | 5.8134 | 0.46296 | 1.0109 | 0.44597 | 0.49783
40Ar | 39.3148 | 18.808 | 3.7361 | 1.7188 | 3.7309 | 10.2859 | 2.6106 | 0.69902 | 0.79515 | 0.60627 | 0.44968
84Kr | 41.9055 | 23.0573 | 4.6391 | 2.1241 | 3.1438 | 5.3494 | 2.3999 | 0.88745 | 0.98353 | 0.69269 | 0.56709
132Xe | 41.5579 | 24.3375 | 5.0682 | 2.3006 | 2.4495 | 2.8547 | 1.6918 | 1.0298 | 0.94936 | 0.70673 | 0.5906
197Au | 40.0389 | 24.3278 | 5.1227 | 2.3057 | 1.9413 | 2.0215 | 1.5204 | 0.99409 | 0.93948 | 0.69108 | 0.60602
238U | 41.6753 | 25.6672 | 5.4204 | 2.4551 | 1.7438 | 1.5 | 1.454 | 1.0869 | 0.97952 | 0.7221 | 0.63254
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 51
INDUCED ISOTOPES | 50 MeV/u
Chart: Induced isotopes
| Cu-64 | Co-58 | Co-57 | Be-7 | H-3 | Co-56 | Cr-51 | Fe-59 | Co-60 | P-33 | V-48
1H | 35.2395 | 37.7954 | 5.5614 | 0.01537 | 0.040891 | 0.062807 | 0.12454 | 0.024947 | 0.26788 | 0 | 0
4He | 13.5127 | 13.502 | 5.378 | 8.0848 | 1.8681 | 5.9835 | 16.223 | 0.76503 | 0.27043 | 0.080848 | 8.498
12C | 19.0602 | 8.0736 | 2.4745 | 16.6013 | 1.7541 | 2.8661 | 11.9984 | 0.24808 | 0.25685 | 0.9895 | 6.7141
20Ne | 24.8321 | 7.4861 | 1.4966 | 17.7855 | 2.5289 | 1.2676 | 7.2258 | 0.28521 | 0.32044 | 2.0504 | 6.9519
40Ar | 39.7311 | 11.5726 | 1.6833 | 11.0251 | 3.0569 | 0.73322 | 2.5545 | 0.29924 | 0.49012 | 3.8201 | 2.3553
84Kr | 45.8644 | 15.6886 | 2.3269 | 5.9507 | 2.5509 | 0.78986 | 2.544 | 0.53654 | 0.57437 | 1.7681 | 1.6355
132Xe | 46.6178 | 17.3709 | 2.4271 | 3.0376 | 1.8508 | 0.71558 | 0.99609 | 0.57039 | 0.58753 | 0.77253 | 0.70638
197Au | 45.7599 | 17.6812 | 2.5206 | 1.947 | 1.3761 | 0.63015 | 0.72467 | 0.62987 | 0.58066 | 0.49559 | 0.55462
238U | 48.5271 | 19.6236 | 2.7347 | 1.3154 | 1.2246 | 0.74153 | 0.71913 | 0.67459 | 0.61855 | 0.46763 | 0.41089

## Slide 52
INDUCED ISOTOPES | 25 MeV/u
Chart: Induced isotopes
| Cu-64 | Co-58 | Co-57 | Be-7 | H-3 | Cr-51 | Co-60 | Cs-131 | Eu-147 | Ag-111 | V-48
1H | 48.7677 | 0.16057 | 0 | 0 | 0.0039605 | 0 | 0.051347 | 0 | 0 | 0 | 0
4He | 18.3054 | 24.831 | 7.645 | 2.0828 | 1.9487 | 1.7858 | 0.41776 | 0 | 0 | 0 | 0.21067
12C | 12.0122 | 9.162 | 3.8569 | 12.9786 | 0.89284 | 7.7456 | 0.18001 | 0 | 0 | 0 | 2.8822
20Ne | 14.4168 | 5.3208 | 2.2449 | 11.4628 | 1.2596 | 11.0479 | 0.196 | 0 | 0 | 0 | 7.3942
40Ar | 28.5984 | 4.923 | 1.1442 | 6.8327 | 1.616 | 5.2586 | 0.36244 | 0 | 0 | 0 | 4.3289
84Kr | 39.3369 | 7.1184 | 1.0762 | 4.2129 | 1.4765 | 3.4753 | 0.47408 | 0.25536 | 0 | 0 | 2.3567
132Xe | 45.9609 | 8.0667 | 0.76564 | 2.1992 | 1.1526 | 1.2199 | 0.50655 | 0.40916 | 0.15967 | 0.0062076 | 1.0109
197Au | 46.1754 | 8.2821 | 0.68123 | 1.3762 | 0.81701 | 0.94925 | 0.49398 | 0.62386 | 1.0689 | 0.0090464 | 0.71287
238U | 52.4188 | 9.6749 | 0.79437 | 0.79283 | 0.74257 | 0.70944 | 0.55673 | 0.52573 | 0.50127 | 0.48856 | 0.48047
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 53
Energy Mass | 1 GeV/u | 900 MeV/u | 800 MeV/u | 700 MeV/u | 600 MeV/u | 500 MeV/u | 400 MeV/u | 300 MeV/u | 200 MeV/u | 150 MeV/u | 100 MeV/u | 50 MeV/u | 25 MeV/u
1 H | 1.00 | 1.01 | 1.02 | 1.05 | 1.09 | 1.16 | 1.28 | 1.49 | 1.90 | 2.25 | 2.81 | 4.17 | 8.51
4 He | 0.87 | 0.87 | 0.87 | 0.88 | 0.91 | 0.97 | 1.09 | 1.33 | 1.98 | 2.85 | 4.61 | 9.31 | 19.86
12 C | 1.18 | 1.23 | 1.30 | 1.42 | 1.59 | 1.88 | 2.37 | 3.35 | 5.96 | 9.76 | 17.12 | 35.28 | 74.36
20 Ne | 1.51 | 1.61 | 1.77 | 2.00 | 2.34 | 2.86 | 3.77 | 5.54 | 10.15 | 16.39 | 28.33 | 60.41 | 138.25
40Ar | 1.97 | 2.17 | 2.42 | 2.79 | 3.34 | 4.19 | 5.63 | 8.42 | 15.17 | 23.08 | 37.29 | 76.62 | 194.25
84 Kr | 3.03 | 3.39 | 3.88 | 4.58 | 5.57 | 7.10 | 9.69 | 14.60 | 25.67 | 36.69 | 54.69 | 107.10 | 254.56
132 Xe | 3.85 | 4.34 | 4.99 | 5.89 | 7.23 | 9.24 | 12.59 | 18.71 | 32.10 | 43.74 | 62.94 | 116.75 | 261.93
197 Au | 4.92 | 5.56 | 6.41 | 7.58 | 9.29 | 11.88 | 16.15 | 23.75 | 39.92 | 52.88 | 73.26 | 124.72 | 262.71
238 U | 5.12 | 5.77 | 6.63 | 7.84 | 9.61 | 12.21 | 16.50 | 24.25 | 39.49 | 51.59 | 70.07 | 113.18 | 245.72
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]
Chart: Primary ion mass number
| 1 | 4 | 12 | 20 | 40 | 84 | 132 | 197 | 238
1 GeV/u | 1 | 0.8726 | 1.1805 | 1.506 | 1.9698 | 3.0298 | 3.8535 | 4.9166 | 5.116
900 MeV/u | 1.0072 | 0.86912 | 1.2282 | 1.6148 | 2.1663 | 3.3908 | 4.3363 | 5.5589 | 5.7692
800 MeV/u | 1.0211 | 0.86796 | 1.3041 | 1.7709 | 2.4239 | 3.8801 | 4.9922 | 6.4089 | 6.6275
700 MeV/u | 1.0465 | 0.87894 | 1.4176 | 1.996 | 2.7921 | 4.5799 | 5.8885 | 7.5763 | 7.8436
600 MeV/u | 1.089 | 0.90876 | 1.5947 | 2.3359 | 3.3412 | 5.5664 | 7.226 | 9.2911 | 9.6088
500 MeV/u | 1.1559 | 0.96949 | 1.8808 | 2.8646 | 4.1923 | 7.0987 | 9.2426 | 11.8805 | 12.215
400 MeV/u | 1.2755 | 1.0864 | 2.3691 | 3.7677 | 5.6326 | 9.6923 | 12.5912 | 16.148 | 16.4999
300 MeV/u | 1.4886 | 1.3339 | 3.3513 | 5.5386 | 8.4157 | 14.5963 | 18.7126 | 23.7545 | 24.2542
200 MeV/u | 1.9014 | 1.9847 | 5.9555 | 10.1531 | 15.1701 | 25.6723 | 32.1014 | 39.9183 | 39.4904
150MeV/u | 2.2525 | 2.8504 | 9.7608 | 16.3894 | 23.078 | 36.6939 | 43.7383 | 52.8763 | 51.5942
100 MeV/u | 2.8092 | 4.6061 | 17.1182 | 28.3267 | 37.2884 | 54.6906 | 62.9359 | 73.256 | 70.0718
SCALING LAW

## Slide 54
CONCLUSION
Activity induced by Uranium beam vs. 1GeV protons
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]
Tolerable beam loss for U beam | FLUKA 2008.3.6 | FLUKA 2011.2b.5
1GeV/u | 5 W/m | 5 W/m
500 MeV/u | 12 W/m | 12 W/m
200 MeV/u | 60 W/m | 40 W/m
150 MeV/u |  | 52 W/m
Chart: Primary ion mass number
| 1 | 4 | 12 | 20 | 40 | 84 | 132 | 197 | 238
1 GeV/u | 1 | 0.8726 | 1.1805 | 1.506 | 1.9698 | 3.0298 | 3.8535 | 4.9166 | 5.116
900 MeV/u | 1.0072 | 0.86912 | 1.2282 | 1.6148 | 2.1663 | 3.3908 | 4.3363 | 5.5589 | 5.7692
800 MeV/u | 1.0211 | 0.86796 | 1.3041 | 1.7709 | 2.4239 | 3.8801 | 4.9922 | 6.4089 | 6.6275
700 MeV/u | 1.0465 | 0.87894 | 1.4176 | 1.996 | 2.7921 | 4.5799 | 5.8885 | 7.5763 | 7.8436
600 MeV/u | 1.089 | 0.90876 | 1.5947 | 2.3359 | 3.3412 | 5.5664 | 7.226 | 9.2911 | 9.6088
500 MeV/u | 1.1559 | 0.96949 | 1.8808 | 2.8646 | 4.1923 | 7.0987 | 9.2426 | 11.8805 | 12.215
400 MeV/u | 1.2755 | 1.0864 | 2.3691 | 3.7677 | 5.6326 | 9.6923 | 12.5912 | 16.148 | 16.4999
300 MeV/u | 1.4886 | 1.3339 | 3.3513 | 5.5386 | 8.4157 | 14.5963 | 18.7126 | 23.7545 | 24.2542
200 MeV/u | 1.9014 | 1.9847 | 5.9555 | 10.1531 | 15.1701 | 25.6723 | 32.1014 | 39.9183 | 39.4904
FLUKA 2008.3.6
FLUKA 2011.2b.5

## Slide 55
COLABORATION
. control systems
. sc magnets & testing
. material research
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]
. voltage breakers
. optical microphones

## Slide 56
Dose rate
RANGE AREA.
. range = 3.5mm
.elliptical beam shape
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]

## Slide 57
THANK
YOU
f o r y o u r
ATTENTION
[ p.katrik@gsi.de ]
[ 10th December 2014 | Storage Rings Meeting | Peter KATRIK | TU Darmstadt | p.katrik@gsi.de ]