## Slide 1: Cryogenic Current Comparators – basics and the next generation
13th SPARC Topical Workshop 16.–20. Sep. Jagiellonian University in Kraków, Poland
Volker Tympel1, R. Neubert1, P. Seidel1, R. Geithner2,3,
J. Golm1,3,T. Stöhlker2,3,4, F. Kurian2,3,4,
T. Sieber4, M. Schwickert4, M. Fernandes5,6
1Institute of Solid State Physics, University of Jena, Germany;
2Institute for Optics and Quantum Electronics, University of Jena, Germany;
3Helmholtz Institute Jena, Germany;
4GSI Helmholtz Center for Heavy Ion Research, Darmstadt, Germany;
5The Cockcroft Institute, University of Liverpool, Daresbury, U.K.;
6CERN European Organization for Nuclear Research, Geneva, Switzerland

## Slide 2: OUTLINE
● Why superconducting?
● Cryogenic Current Comparator (CCC)
● Does it work?
● Next generation CCC-XD: Flux concentrator
● Challenges
● Short summary
V. Tympel (Institute of Solid State Physics) Friedrich-Schiller University Jena, Germany
Notes: Planned Future installations of the SQUID-based Beam Current Monitor

## Slide 3: Why superconducting?
Aluminum 1.5 mm
Tin plate 0.8 mm
Cu 0.8 mm
V2A steel 1.7 mm
Aluminum foil, single layer
Decreasing of the magnetic field
Frequency f / Hz
Shielding
better
V. Tympel (Institute of Solid State Physics) Friedrich-Schiller University Jena, Germany

## Slide 4
mu-metal
Frequency f / Hz
Decreasing of the magnetic field
Nickel–iron soft magnetic alloy
Aluminum 1.5 mm
Tin plate 0.8 mm
Cu 0.8 mm
V2A steel 1.7 mm
Aluminum foil, single layer
Why superconducting?
Shielding
V. Tympel (Institute of Solid State Physics) Friedrich-Schiller University Jena, Germany

## Slide 5
Door of the magnetically shielded room
at the university of Jena:
2 layers mu-metal
1 layer Cu
43 cm
Thickness
Why superconducting?
Shielding
V. Tympel (Institute of Solid State Physics) Friedrich-Schiller University Jena, Germany

## Slide 6
Boutside= Binside
Normal conductor
Binside=0
Boutside>> 0
Superconductor
Meissner effect: the expulsion of a magnetic field
=> ideal magnetic shielding
Why superconducting?
Shielding
V. Tympel (Institute of Solid State Physics) Friedrich-Schiller University Jena, Germany

## Slide 7
AC
Normal conductor
Superconductor
AC/DC
AC
AC/DC
Boutside= Binside
Normal conductor
Binside=0
Boutside>> 0
Superconductor
Meissner effect: the expulsion of a magnetic field
=> ideal magnetic shielding
A constant magnetic field leads to
screening current => DC- Sensor
Why superconducting?
DC-Transformer
V. Tympel (Institute of Solid State Physics) Friedrich-Schiller University Jena, Germany

## Slide 8
DC-SQUID
JJ
JJ
Ibias
VSQUID
A
Φ = ∫ B dA
B
Ibias
I
∆V
n∙Φ0
(n+½)∙Φ0
VSQUID
VSQUID
∆V
Φ0
Φ
operating
point
Φn
Φn+1
Two Josephson junctions act as a
DC-SQUID, Interference leads to
=> high sensitivity.
The magnetic-field dependency => resolution: << Φ0
A closed loop control => range: >> Φ0
Why superconducting?
SQUID – Sensor
V. Tympel (Institute of Solid State Physics) Friedrich-Schiller University Jena, Germany

## Slide 9: Φ0 flux quantum?
B ≈ 60 µT
R ≈ 400 000 km
Earth
Moon
B ≈ 20∙10-5 µT
3 mm
3 mm
@ moon
Φ0
S
N
≈ 2∙10-9 µT m2 = 2∙10-5 µT cm2

## Slide 10
charged
particle
beam
5 A
B
Principle of the
Cryogenic
Current
Comparator
CCC
strong beam
V. Tympel (Institute of Solid State Physics) Friedrich-Schiller University Jena, Germany

## Slide 11
B=0
B
-i
i
charged
particle
beam
Principle of the
Cryogenic
Current
Comparator
contactless & non-destructive
5 nA
CCC
weak beam
V. Tympel (Institute of Solid State Physics) Friedrich-Schiller University Jena, Germany

## Slide 12
SQUID
Pick-up coil
Transformer
Superconducting shielding
Compensation
Current
Cryogenic liquid
LHe
Magnetic flux
Concentrator ring
Flux gap
Charged particle beam
Metrology
Calibration
Current
Magnetic field B
Four-wire
Measurement
Flux
Compensator

## Slide 13
[A. Peters et al., A Cryogenic Current Comparator for the Absolute Measurement of nA Beams, AIP Conf. Proc. 451 pp. 163-180 (1998)]
Pb-shielded CCC assembled
in a beam line
Nb-shielded CCC before assembling
in a beam line.
@ GSI
@ CERN
Realisations
V. Tympel (Institute of Solid State Physics) Friedrich-Schiller University Jena, Germany

## Slide 14
@ CERN
Linear correlation between SEM and
CCC signal with a slope of ~ 0.8.
Current sensitivity of the CCC tested via
beam simulating wire or to calibration coil.
@ GSI
It works!
V. Tympel (Institute of Solid State Physics) Friedrich-Schiller University Jena, Germany

## Slide 15
[R. Geithner et al., Cryogenic current comparator for storage rings and accelerators, MOPB013, Proc. of IBIC2015, Proc. of IBIC2015]
SEM/CCC measurement of a 600 MeV/u beam of slowly extracted Ni26+ ions.
Longitudinal-Schottky and CCC measurement during one AD cycle (10% nominal intensity). IBIC2016: 3-nA beam without problems
[M. Fernandes et al., A Cryogenic Current Comparator for the Low
Energy Antiproton Facilities at CERN, MOPB043, Proc. of IBIC2015]
spill monitoring
@ GSI
It works!
@ CERN

## Slide 16
● @ FAIR larger beamline diameter => CCC with eXtended Dimensions CCC-XD
● larger bandwidth => new core materials
specific thermo-magnetic, gas and heat treatment process of amorphous Fe-alloy NANOPERM® ribbons
GSI328plus
Next generation: CCC-XD
V. Tympel (Institute of Solid State Physics) Friedrich-Schiller University Jena, Germany
330 mm
≈ 1500 turns of
15 µm layers

## Slide 17
E4980A Precision LCR Meter, 20 Hz to 2 MHz
Mode: Ls-Rs
Complex relative
permeability
Loss angle
Without core
With core
CCC-XD: Flux concentrator
V. Tympel (Institute of Solid State Physics) Friedrich-Schiller University Jena, Germany

## Slide 18
Ls-Messungen bei 4,2 K
100 kHz
Thesis, René Geithner, 2013
„Untersuchung der Tieftemperatureigenschaften magnetischer Materialien für den Einsatz im Kryostromkomparator“
First measurements @ 4.2 K:
● noisy
● core materials with
small bandwidth
CCC-XD: Flux concentrator
V. Tympel (Institute of Solid State Physics) Friedrich-Schiller University Jena, Germany

## Slide 19
Tympel, et al., IBIC 2016
„The next generation of Cryonic Current Comparators for beam monitoring“
Now @ 4.2 K:
● SNR better 200 : 1
● core materials with
larger bandwidth
100 kHz
CCC-XD: Flux concentrator
V. Tympel (Institute of Solid State Physics) Friedrich-Schiller University Jena, Germany

## Slide 20
Now: Temperature below 2 K
● below Lambda-point
(50 hPa & 2,17 K)
=> superfluid He II
4.2 K
CCC-XD: Flux concentrator
Tympel, et al., IBIC 2016
„The next generation of Cryonic Current Comparators for beam monitoring“
V. Tympel (Institute of Solid State Physics) Friedrich-Schiller University Jena, Germany
He I
He II
Thermal
Conductivity => ∞

## Slide 21
green: Faraday Cup
black: DESY-CCC
Geithner et al., Rev. Sci. Instrum., 82(1):013302, 2011
Next challenges
● Drifts
● Microphonic effects
V. Tympel (Institute of Solid State Physics) Friedrich-Schiller University Jena, Germany

## Slide 22: Thank you for your attention.
Squid it !
Charged beam:
Short summary
V. Tympel (Institute of Solid State Physics) Friedrich-Schiller University Jena, Germany

## Slide 23: Number?

## Slide 24: Magnetic disturbance
Magnetic Cycle of AD Dipoles in arbitrary units
SQUID/FLL raw signal of beam current ( green), and same signal filtered with a moving average (red)
Calibrated beam current measurement after filtering and baseline recovery (before beam injection and after beam extraction)
[M. Fernandes et al., A Cryogenic Current Comparator for the Low
Energy Antiproton Facilities at CERN, MOPB043, Proc. of IBIC2015]

## Slide 25: Attenuation Factor FAIR-CCC
Increased number of meander from 7 auf 12
Transvers fields (perpendicular to beam)
  187 dB, (DESY-CCC:167 dB)
Longitudinal fields (parallel to beam)
  199 dB, (DESY-CCC: 187 dB)

## Slide 26: OPERATION
Working principle of SQUID electronics in flux-locked loop (FLL) mode
Environment & Calibration Handling
Notes: Due to the periodically dependence of the voltage the SQUID is not useful for flux changes above 0.5 phi0 in this way because it is not clear on which point of the U-phi characteristics you are.
Therefore an electronics in flux-locked loop (FLL) mode is used which runs the SQUID in the working point with maximum sensitivity.
I f the flux through the SQUID is changed the voltage drop is amplified and integrated and current is applied to the feedback coil which is in our case an additional winding on the pickup coil to compensate the flux and stabilize the working point.
The signal you measure is the feedback signal. With the knowledge of the overall flux sensitivity in flux/voltage you can calculate the flux trough the pickup coil and if you know the overall current sensitivity in current/flux you can calculate the beam current.

## Slide 27
4 Kernmessungen - Induktivitätsmessungen
27
uH(t)
uL(t)
Automatisch
Abgleichende
Messbrücken-
Methode:
1. Erzeugung virtueller Masse „Low“
2. L-Berechnung durch uH(t), uR(t)
und R1
uR(t)
Low

## Slide 28
E4980A Precision LCR Meter, 20 Hz to 2 MHz
4 Kernmessungen - Induktivitätsmessungen
28

## Slide 29
4 Kernmessungen - Komplexe Permeabilität
29
E4980A Precision LCR Meter, 20 Hz to 2 MHz
Mode: Ls-Rs
Komplexe relative
Permeabilität
Verlustwinkel
ohne Kern
mit Kern

## Slide 30
4 Kernmessungen - Komplexe Permeabilität
30
Toroidspule mit N Windungen:
Außendurchmesser
Innendurchmesser
Höhe
Korrekturfaktor geom. Induktivität
Korrekturen:
Re:
Im:
Verlustwinkel:
Fluktuations-Dissipations-Theorem
Dissertation René Geithner, 2013

## Slide 31
4 Kernmessungen – AL-Wert
31

## Slide 32
4 Kernmessungen – Erfahrungen
32
Induktivität der DESY-CCC-Pickup-Spule mit Vitrovac 6025F
„Optimierung eines kryogenen Stromkomparators
für den Einsatz als Strahlmonitor“
Dissertation
René Geithner, 2013
Strom möglichst hoch!
E4980A LCR-Meter: 20 mA
100 kHz

## Slide 33
4 Kernmessungen – letzte Pickup-Spule
33
Ls/Rs-Messungen bei 4,2 K; blau: DESY-CCC
grün: FAIR-CCC: Nanoperm M764
„Optimierung eines kryogenen Stromkomparators
für den Einsatz als Strahlmonitor“
Dissertation
René Geithner, 2013

## Slide 34
4 Kernmessungen – neue Testkerne
34
Vacuumschmelze Hanau:
amorphe Kerne: Vitrovac
nano-kristalline K.: Vitroperm
Rascherstarrungstechnologie für amorphe Bänder
Bänder => gewickelte Kerne
Magnetec GmbH:
nano-kristalline K.: Nanoperm

## Slide 35
4 Kernmessungen – neue Testkerne
35
Wärme-
behandlung:
[Vacuumschmelze Hanau]

## Slide 36
Coercivity Hc vs. grain size D for various soft magnetic metallic alloys:
Fe–Nb–Si–B (solid triangles) [12],
Fe–Cu–Nb–Si–B (solid circles) [2] and [12], Fe–Cu–V–Si–B (solid nablas [2] and open down triangles [13]),
Fe–Zr–B (open squares) [14],
Fe–Co–Zr (open diamonds) [16],
NiFe alloys (+ center squares and open triangles) [17] and
Fe–6.5 wt.% Si (open circles) [18]. (Reprinted from Herzer [2].)

## Slide 37
4 Kernmessungen – neue Messungen
37
Korrektur:
M-116 @ RT

## Slide 38
4 Kernmessungen – Kurzschluss-Korrektur
38
Korrektur:

## Slide 39
4 Kernmessungen – Anzahl der Windungen
39
Viele Windungen:
stabile Daten
aber
schnell Resonanzen
34
1
M-116 @ RT

## Slide 40
4 Kernmessungen – Messkabel
40
Je kurzer,
desto besser!
„3er-Kabel“ für den Kryostaten
M-116+ @ RT

## Slide 41
4 Kernmessungen – Messstrom
41
Ls / Rs hängen
vom Messstrom ab!
E4980A max.: 20 mA
Magnetec: 100 mA
M-116 17 Wdg @ RT

## Slide 42
4 Kernmessungen – Messungen im Weithalskryostaten
42
4,2 K
Lange Kabel
1 Windung
Störungen
50 Hz / 150 Hz
Auf stabile Verkabelung achten!
M-116 / 116+ @ 4,2 K

## Slide 43
4 Kernmessungen – Messungen Auswerteprogramm
43
C++ Programm: Mess-Files einlesen und verrechnen
Erstellen von Ls(T) / Rs(T) und 3D-Vorlagen
Erstellen Mittelwerte / Vertrauensbereich
Alle 11 Min.
ein File mit
201 Frequenzen
je Frequenz:
Temperatur
Ls
Rs

## Slide 44
4 Kernmessungen – Messungen Auswerteprogramm
44
Ls
Vertrauensbereich
3-Sigma Bereich:
20 Hz: 1 / 200
100 kHz: 1/ 100 000
Störungen
35 Hz - ?
50 Hz - Netz
150 Hz - Netz
M-116+ @ 4,2 K

## Slide 45
4 Kernmessungen – Messungen Auswerteprogramm
45
Rs
3-Sigma Bereich:
20 Hz: 1 / 10
100 kHz: 1/ 50 000
Störungen
35 Hz - ?
50 Hz - Netz
150 Hz - Netz
M-116+ @ 4,2 K

## Slide 46
4 Kernmessungen – Messungen Auswerteprogramm
46
µ‘
M-116+ @ 4,2 K

## Slide 47
4 Kernmessungen – Messungen Auswerteprogramm
47
µ‘‘
>100 kHz
M-116+ @ 4,2 K

## Slide 48
4 Kernmessungen – Messungen Auswerteprogramm
48
tan(δm)
M-116+ @ 4,2 K

## Slide 49
4 Kernmessungen – Messungen Auswerteprogramm
49
Ls linear
z.B. 20 Hz:
(28,3 ±0,2) µH P=99,8 %
+ systematische
Fehler !
M-116+ @ 4,2 K

## Slide 50
4 Kernmessungen – Messungen Auswerteprogramm
50
tan(δm) linear
M-116+ @ 4,2 K

## Slide 51
4 Kernmessungen – 3D Diagramme
51
M-116plus Rs log10
M-116plus Ls

## Slide 52
4 Kernmessungen – Ls(T)
52
„100 000er“-µ‘-Kern
„30 000er“-µ‘-Plus-Kern

## Slide 53
4He I
flüssig
gasförmig
4He II
supra-fluid
fest
Temperatur T / K
Druck p / bar
Druck p / Pa
4,2 K
λ-Punkt
50,36 hPa
2,1768 K
53
5 < 4,2 K suprafluides LHe II
Druckverminderung
Abpumpen von He

## Slide 54
5 < 4,2 K suprafluides LHe II
Quantenflüssigkeit mit
makroskop. Quanteneffekt
Innere Reibung / Viskosität η
Dynamische Viskosität in mPa∙s :
Glas @RT 1022…1024
Steinsalz 1018…1021
Glas @Verarbeitungstemp. 106…1012
Wasser @20°C 1
Diethylether 0,24
LN2 0,14
LHe II => 0
https://www.youtube.com/watch?v=2Z6UJbwxBZI
54

## Slide 55
Quantenflüssigkeit mit
makroskop. Quanteneffekt
Wärmeleitfähigkeit λ
Wärmeleitfähigkeit in W/(K∙m) :
Polystyrol ≈ 0,04
LN2 0,15
Glas ≈ 0,8
Messing 120
Kupfer rein 400
Diamant 2400
LHe II => ∞
https://www.youtube.com/watch?v=2Z6UJbwxBZI
LHe I
LHe II
keine Siedeblasen
weniger Rauschen
55
5 < 4,2 K suprafluides LHe II

## Slide 56
Quantenflüssigkeit mit
makroskop. Quanteneffekt
spez. Wärmekapazität c
Tλ = 2,1768 K @ 50,36 hPa
* Kalibrierung
* Temperaturstabilisierung
M. J. Buckingham , W. M. Fairbank, ‘‘The nature of the λ-transition in liquid helium’’, Progress in Low Temperature Physics, 1961, Vol. 3, pp. 80–112.
56
5 < 4,2 K suprafluides LHe II

## Slide 57
57
5 < 4,2 K Abpumpen
Start
Theorie: Ende
Praxis: Ende

## Slide 58
Scroll-
pumpe
15 m3/h
He-
„Uhr“
10 dm3/U
Nadelventil
Bypass
Druckmesser
He-Druckausgleich
He-
Rückleitung
≈1000 mbar
Weithals-Kryostat
58
5 < 4,2 K Abpumpen
Gefüllt: LHe-Bedarf: ca. 0,63 l/h => 450 mW

## Slide 59
He-“Verbrauch“
s/U
Vor: 75
Anfang: 25
Begrenzung: 13
Ende: 80
+ 12h 80
59
07:50
25 s/U
08:07
15 s/U
08:30
14 s/U
09:10
13 s/U
10:10
13 s/U
11:45
13 s/U
12:40
24 s/U
14:15
48 s/U
19:15
80 s/U
Bypass auf
Gasstrom-Regelung
über Nadelventil
Druck p / mbar
Temperatur T / K
[Thermodynamic Properties of Helium ... Robert D. McCarty,1973]
5 < 4,2 K Abpumpen
λ-Punkt 2,1768 K

## Slide 60
60
5 < 4,2 K Abpumpen
Temperatur-Sensor
OK ?
Maximum der
spez. Wärmekapazität
beim Lamda-Punkt Tλ
sollte nachweisbar sein!
λ-Punkt 2,1768 K

## Slide 61
61
19:30
19:20
in 10 Minuten auf Normaldruck
Druck p / mbar
Temperatur T / K
[Thermodynamic Properties of Helium ... Robert D. McCarty,1973]
5 < 4,2 K He-Druckausgleich
Temperatur
OK ?
Lamda-Punkt
Tλ
λ-Punkt 2,1768 K

## Slide 62
62
5 < 4,2 K Abpumpen
Spezialanfertigung
GSI-328plus No.4
1. Messung
328 mm
2 K - RT

## Slide 63
63
5 < 4,2 K Abpumpen
Spezialanfertigung
GSI-328plus No.4
1. Messung
328 mm
2 K - RT