## Slide 1: Status of works on the Collaboration Contract between IHEP and FAIR
  Andrey Ryazantsev
  on behalf of the IHEP-Protvino group

## Slide 2: Major milestones for the EMC Barrel Mechanics
“Batch 1 of the Pre-Series Slice (PSS-B1) comprises 70 to 80% of the components for the full Pre-Series Slice while batch 2 (PSS-B2) comprises all remaining components to be delivered for the Pre-series Slice.”

## Slide 3: Crystals support structure
Super Module types
#1 #2 #3 #4 #5 #6 #7
(1 module) (3 different modules in each) ( 2 different modules)
7(-) 6(-) 5(-) 4(-) 3(-) 2(-) 1(-) 1(+) 2(+) 3(+) 4(+) 5(+) 6(+) 7(+) 8(+) 9(+) 10(+) 11(+)
18 different types of the single carbon fiber alveoli units of 2×4 cells [2×3 cells for 11(+)]
(5 units / module)
Proto 120
Beam

## Slide 4
Single alveoli units production
10 of 18 different type molds are available: from 1(-) through 9(+)
9 of them - from 1(+) through 9(+) - have successfully passed the input acceptance tests at IHEP with the use of the CMM DEA Mistral; type 1(-) is being measured nowadays.
Types 2(-) and 3(-) will be ready soon
Several single alveoli units of each type from 1(+) through 9(+) were produced (only preliminary cut) and measured with the CMM. The results of the measurements showed a good compliance to the 3D tolerance model.
Tools for the precise cutting of the single carbon alveoli units of type from 1(+) through 9(+) were produced, delivered and accepted; production of remaining types is in progress.

## Slide 5
Alveoli packs production
The assembly devices to glue alveoli packs and to assemble modules of type from 1(-) through 9(+) were produced and delivered to IHEP, 2(-) and 3(-) will be ready soon.
Parts of the assembly device of type 8(+) that define geometry correctness of the alveoli packs were carefully measured with CMM. All dimensions are within tolerances.
First alveoli pack of type 8(+) was produced.
Rear inserts and intermediate plates of type from 1(-) through 3(-) and from 1(+) through 3(+) were delivered and passed the acceptance tests → ready to produce alveoli packs of type 1(+), 2(+) and 3(+).
Rear inserts and intermediate plates of type from 4(+) through 9(+) and from 4(-) through 7(-) are expected to be ready at the end of October.

## Slide 6: First alveoli pack of type 8(+)
5 single alveoli units were cut precisely with the use of the new cutting tool

## Slide 7: First alveoli pack of type 8(+)
5 single alveoli units filled up with the “dummy crystals” and jointed with a glue
are in the assembly device with rear inserts and intermediate plates

## Slide 8: First alveoli pack of type 8(+)
Assembly device is being placed in the oven

## Slide 9: First alveoli pack of type 8(+)

## Slide 10
Aluminum Support Beam
Foam
Super-Modules
Side Covers
Cooling System
Back Cover
Design of EMC Barrel slice (by Valery Ferapontov)

## Slide 11: Pre-series support beam production
Three experts from IHEP visited the manufacturing companies in Germany:
-Hamburg, GLEICH Aluminiumwerk GmbH & Co/KG Kaltenkirchen
-Jena, M&B GmbH Siegmar

## Slide 12: Pre-series support beam production
Five-axis machine in Jena with a base of 2.5×4.0 m

## Slide 13: Pre-series support beam production
Tender is required!
In case of success, M&B GmbH Siegmar will produce the support beam from an aluminum blank provided by GLEICH Aluminiumwerk GmbH & Co/KG Kaltenkirchen .
Expected time:
2 months for the tender procedure,
35 working days - production cycle,
~ 2 weeks for shipping and custom formalities.

## Slide 14: Design of front inserts and optical fibers tracing (Suggested by V. Ferapontov and A. Levin)

## Slide 15: Design of front inserts and optical fibers tracing (Suggested by V. Ferapontov and A. Levin)
Currently !!!
Under discussion with Philippe Rosier

## Slide 16
EMC Barrel assembly (by Valery Ferapontov)
Technological beam
V. Ferapontov needs the technical drawing of the support structure for the pre-series slice assembly and tests to finalize design of the technological beam

## Slide 17: Summary and open questions
  Design of the pre-series slice (uploaded in EDMS) is ready. Waiting for the official approval (Milestone M7 – Final design review for pre-series slice).
  Almost all technological tools for the alveoli production and modules assembly of all the types were designed, their production is in progress. More than 50% of them were delivered to IHEP, passed the acceptance tests and are currently in use.
  About 60 % from the volume of crystal support structure to be delivered in the batch 1 is ready.
Design of front inserts and fibers tracing - need to solve the lack of space problem.
Scenario of the slice assembly – need the revision of existing assembly tools .