## Slide 1
Secondary electron yield of surfaces: laboratory measurements, influence of temperature and magnetic field
M.Taborelli, for TE-VSC, CERN

## Slide 2
The secondary electron yield: SEY
number of emitted electrons (secondary)
number of impinging electrons (primary)
SEY=
δmax or SEYmax = maximum value as a function of primary energy
Emax = primary energy of the maximum
secondaries
Primary e-
N
0 500 1000 1500 2000 2500 3000
Primary Energy [eV]
2.5
0.5
2.3
2.1
1.9
1.7
1.5
1.3
1.1
0.9
0.7
Cu as rec.
Emax
δmax
SEY
N.Hilleret
measurements
The electrons in that energy range escape from depth of less than 20 nm: SEY depends on surface properties

## Slide 3
electron gun
Ip = Is + Ic
d = Ic / (Is + Ic)
Sample
Ip
Ic
A
Is
A
Ic
Measurement of SEY of surfaces
electron gun
Sample
Ip
A
Is
Faraday cup
Ip with Faraday cup
d = 1-Is/Ip
Gun is closer to sample:
better adapted for low Ep
Currents are not all measured simultaneously
collector
+ -
+ -
+ -
sometimes Ip is measured just by polarising the sample positive: in this way the elastic electrons are lost
measurements

## Slide 4
Accuracy and precision
Precision (reproducibility) is high, better than 0.05 (see the two red curves)
Accuracy with respect to the absolute SEY is lower and systems of different geometry give values of +/- 0.1 on SEYmax
Systems give sligthly different results depending on configuration….
Coll
Fara
measurements

## Slide 5
Measurements done at low dose (below 10-6 C/mm2) to avoid conditioning of the surface: very important for as-received air exposed samples
Keep a low dose!
A low dose is mandatory to measure the SEY of insulators (charging)
OFE copper
V.Baglin et al. LHC project report 472
2.6
2.4
2.2
2.0
1.8
1.6
1.4
1.2
1.0
1e-8 1e-7 1e-6 1e-5 1e-4 1e-3 1e-2
Dose [C/mm2]
measurements

## Slide 6
Pulsed: example of alumina
Charging after the first curve perturbs the following measurements
measurements
Pulsed measurements
1e-13 C/mm2/point
5μs/pulse
Neutralization with 5eV beam for 60s

## Slide 7
In situ I: SEY measurements in the SPS accelerator
LHC-Project Report 632, 2003 J.M.Jimenez et al
Rotatable sample system in line of sight of SPS beam; operated remotely
Hours of LHC beam operation
Copper conditioning
measurements

## Slide 8
In situ II: Samples exposed and transferred in UHV
See also: M.Pivi et al SLAC-pub-14000, 2010
CESR-TA Cornell: W.Hartung at al IPAC2013, Shanghai, 3493
measurements

## Slide 9
SEY of samples measured in situ before and after conditioning
The SEY of several samples as a function of operation time in positions where only e-cloud impinges and other where e-cloud and synchrotron radiation impinge
In situ II: CESRTA system, conditioning monitoring
CESR-TA Cornell: W.Hartung at al IPAC2013, Shanghai, 3493
measurements

## Slide 10
collector
e-gun
Cold head facing an e-gun collector system in RT UHV chamber
From RT down to 6K
P in low 10-9 mbar (H2 > H2O > CO > CO2)
Suitable for measurements at primary energy above 80 eV, dose < 10-7 C/mm2 for full curve
Ic
Is
Example of a setup for cold SEY
temperature

## Slide 11
There is no or weak intrinsic T dependence of SEY for an as received metal surface:
The slight SEY decrease at low T is possibly due to the influence of adsorbates upon cooling (same for ion induced yield H.Rothard et al PRB30, 9224,1988 )
Copper OFE
Nb
Intrinsic temperature dependence of SEY?
temperature

## Slide 12
E
KT
25meV=KT<< E=1-10 eV
Production of secondary:
The excitations involved to generate secondary electrons are of the order of eV (to overcome the work function)
Vac. level
EF
Transport:
The excitations limitng the mean free path in metals at several eV above EF is dominated by electron-electron interaction (phonons are less important) and the DOS occupancy changes only marginally in the practical temperature range
…what about insulators?
Why is the temperature effect so weak?
temperature

## Slide 13
M. V. Gomoyunova, J. Tech. Phys. 28, 2473, (1958) , in J. Cazaux JAP 89, 8265 (2001)
J.B.Johnson et al, Phys Rev. 91, 582 (1953)
NaCl
MgO
The SEY decreases with T:
→ generally explained by the reduction of escape of secondaries which is limited by e-phonon scattering → at high T there are more phonons → more scattering →shorter mfp → lower SEY
SEY
SEY
740C
RT
Intrinsic T dependence of insulators
temperature

## Slide 14
SEYmax
V.Baglin et al. Proc Chamonix X, p130, 2000
Low temperatures provoke condensation:
The curve saturates at about 150ML….the mfp of escaping secondary electrons is very large (larger than for metals, and also larger than for CO, CO2 etc)
Condensed water on cold copper surface
SEY
2.4
2.2
2.0
1.8
1.6
1.4
1.2
1.0
0.8
0 500 1000 1500 2000 2500
as rec
45 ML
65 ML
200ML
temperature

## Slide 15
CO adsorption lowers the SEY of as-received copper at any coverage
Emax decreases at high coverage
Condensed layers: CO on OFE copper
6K
temperature

## Slide 16
Not monotonic: cannot be explained as a sum of CO and Cu SEY
Saturation at 25ML, much lower coverage than water  smaller escape depth
Cumulative CO physisorption on Cu OFE
6K
The SEY of CO is the lowest compared to H2O , CO2, CH4, N2
Condensed layers: CO on OFE copper
temperature

## Slide 17
Low primary energy: motivation for the measurements
The low energy part influences the e-cloud threshold :
Simulation for LHC beam in the arcs, 72 bpi and 288 bpi at nominal intensity
Courtesy G.Iadarola, PhD Thesis
Courtesy G.Iadarola, PhD Thesis
max
δmax
Courtesy G.Iadarola, PhD Thesis
SEY= elas + true
Primary energy [eV]
R0
Low Ep

## Slide 18
Can we measure the SEY at low primary energy?
Yes, by retarding (- bias on the sample), sacrifying some angular accuracy
Polycrystalline copper
Low Ep
Cimino et al, Phys. Rev. ST Accel. Beams 18, 051002, 2015

## Slide 19
To get a meaningful energy scale one must take into account the difference of WF between gun and sample and a possible error in gun voltage. Calibrate by a sample with known Φs
More in detail: what is the energy scale
EFs
Vgun=0
EFf
Vgun= 0.5 V
EFf
Vgun= 0.8 V
EFf
Vgun= 3 V
EFf
0.5V
0.8V
3.0V
Φs
WF difference
sample-filament+ gun error
Low Ep

## Slide 20
Energy scale and WF
Assume for Au:
Φ=5.2eV
Get:
ΦAl =4.0 eV
ΦCu= 4.4 eV
ΦHOPG=4.4eV
In collaboration with A.Bellissimo (UniRoma3)
Low Ep
The structures (dips) are possibly at threshold of inelastic processes
in competition with elastic scattering (H.E.Farnsworth 1928, p41-57)

## Slide 21
Effect of magnetic field
measurements?
B-field

## Slide 22
Charge measured by displacement current:
The charge is measured by integrating the displacement currents: this does not need a collector or Faraday cup!
A.Krasnov et al. Proc DIPAC2011, p236
B-field

## Slide 23
Incidence and transport: static uniform magnetic field perpendicular to a flat surface, like in a dipole
An electron arriving to the surface with an angle β will keep its angle of incidence with respect to the surface normal
B
VII
V
The B field modifies only the direction of V, but not its length: the V vector remains on a cone
β
No change of angle of incidence: on a flat surface no change of SEY is expected
The electron travels for the length of a mfp   collision time 
It reaches a depth V independent of B
B-field

## Slide 24
In the material: effect of static magnetic field on the secondary electrons transport and cascade
The B-field in the solid does not change V and V : no change of depth of the cascade
Is the angle change due to B relevant before a scattering event? How long is  ?
 slowest escaping electrons
 V  EFERMI+WF > 5eV inside
 8 nm
V : low V give the smallest Larmor radius:
When is rL  ?
EFERMI
outside
inside
WF
Vout
Vin
B
B-field
V

## Slide 25
5eV
Comparison of Larmor radius and electron mean free path
V corresponds to 5eV and an inelastic mean free path of 8nm
V giving an rL of about 8nm corresponding to an energy of 0.0005eV….
Those values of V/V are electrons travelling within 0.5 deg from the normal to the surface,  no major effect is expected from their change of trajectory
at 9T
B-field
V
V

## Slide 26
Secondary electrons emitted from a rough surface (grooves) with B field normal to surface will hit the surface again:
Condition for hitting:
The condition is independent of the field B!
It depends on the initial direction Vy, Vz ….
L.Wang et al. SLAC-PUB 12001, 2006
B-field
Rough surfaces and electron trapping
The steeper the surface the better it is

## Slide 27
The effect of B on a rough surface
Published simulations do not perfectly agree (both with a flat surface with SEY=1.75): not clear if the field reduces the performance
No B
0.2T
60º
40º
M.Pivi et al SLAC-PUB 13020, 2007
Normal incidence
L.Wang
SLAC-PUB-12641
July 2007
flat
0.2T
Normal incidence
«effective SEY»: ratio of all electrons impinging and leaving in e-cloud
1.4
1.2
1
0.8
0.6
0.4
0.2
0
New simulations in progress by N.Fil, ONERA Toulouse
β
β
B-field

## Slide 28
THANK YOU
THANK YOU AND…
SEE YOU IN GENEVA IN 2018

## Slide 29
In magnetoresistance the conduction electrons at Fermi level are involved, therefore we expect a stronger effect:
Electrons are slower and the respective Larmor radius is smaller than for secondaries
The mean free path is much longer than for secondaries
Effect of magnetoresistance:
Very pure copper,
mfp about 30 μm
(PRB 23, 483, 1981)
For copper the effect scales with H/ρ0
It nicely illustrates the mean free path influence (or RRR)
H x S (MGauss)
S=R(273K)/R(4.2K)
J.Phys.Chem Solids
11, 37, 1959
Beam screen copper has RRR~100, therefore we expect and effect of about Δρ/ρ0 ~2

## Slide 30
No reflected power (= no multipacting) in the coated dipoles with the available input power (tested up to 2 Tesla)
Easy to achieve multipacting in the non-coated dipole (even after prolonged conditioning).
Reflected power
SPS dipole
Multipacting test bench
Lab characterization
This enables to evaluate the performance in a situation more similar to the effect of the beam

## Slide 31
N(Es) , EDC
Secondary electron Energy
elastic
true
secondaries
Auger
backscattered
From F.Perez et al
Conceptually one can distinguish in principle different contributions to the electrons scattered by a surface.
NB: We measure in general the total yield and call it secondary electron yield
The secondary electrons
50eV
Primary electron Energy (eV)
SEY
__ total SEY
__ true secondaries
__ elastically backscattered
__ inelastically backscattered
1
0 E1 200 E2 1500

## Slide 32
Average escape depth of secondary electrons
p
primary energy
primary
beam
SEY
Why does the curve have a maximum?
All materials display a curve with a maximum (Emax) as a function of primary energy
secondaries
Remark on angle!
Important for multipacting RF crossing 1 and for SEY

## Slide 33
SEY and roughness
The secondary electrons cannot escape from high aspect ratio roughness
The effect is purely geometric and is scale invariant (for a size above the mfp of electrons)
Effect well known
H.Bruining 1938
Simulation J.Kawata et al J. Phys. Soc. Jpn. 63, pp. 795-806 (1994)

## Slide 34
e-gun
measured
spot
sample
Setup in BA5
Measurement done during the technical stop (the electronics must be brought in the tunnel)
MBB profile
(no magnetic field)

## Slide 35
SEY vs position, transverse to the beam
-25 0 +20 mm
before installation in SPS
bottom
(not facing the beam)
Primary energy [eV]
SEY

## Slide 36
Microscopic roughness: laser treated surface
R.Valizadeh et al. APL 105, 231605 (2014)
Cu as-rec.
Cu treated
sample: A.Abdolvand Uni Dundee
20 μm
Laser structured surfaces: the SEY reduction is due to the micro-roughness
Under study as candidate for LHC triplets and FCC
Mitigation

## Slide 37
Test with the SPS proton beam in e-cloud monitors
SPS
proton
beam
e-cloud current
48 strips spaced 1.25 mm
vacuum chamber
Coated liner
B-field 1.2KGauss
80 cm
The B-field of 1.2kGauss corresponds to the field of the SPS dipoles at injection energy (26 GeV)

## Slide 38
Inner
Time [s]
Time [s]
ECM with SPS dipole
beam pipe
cross section
coating
uncoated
uncoated
coated
uncoated
Installed all in all 6 a-C coated liners; LHC type beams (26GeV and 450GeV, up to 1.8 x1011 p/b x 72 b, 25 ns spacing) did not show e-cloud
one installed in 2008 without loss of performance up to 2015 (exposed to 1 year venting during LS1)
samples extracted after operation did not show significant SEY increase
Example:
StSt
StSt
StSt
a-C
Test with proton beam in e-cloud monitors