## Slide 2: Research on high temperature superconducting (HTS) coatings for the FCC
Sergio Calatroni – CERN
In collaboration with: CNR-SPIN and TU-Wien // ALBA, ICMAB and IFAE

## Slide 3: Outline
The FCC-hh
Basics of beam dynamics & impedances
Surface impedance – normal metals
Surface impedance – superconductors
Surface impedance – superconductors in B field
Case for Tl-1223 and Y-123

## Slide 4
Future Circular Collider Study

## Slide 5: FCC-hh: pushing the energy frontier
The name of the game of a hadron collider is energy reach
Compared to the LHC:
Factor ~6 in energy  Ecms 100 TeV pp
Factor ~3 in radius  bending 100 km
Factor ~2 in field  Bdipole 16 T
Factor ~144 in synchrotron radiation power  E4-2

## Slide 6: Synchrotron radiation/beam screen
High synchrotron radiation load (SR) of protons @ 50 TeV:
~30 W/m/beam (@16 T)
5 MW total in arcs (LHC <0.2W/m)
New type of ante-chamber
absorption of synchrotron radiation
avoids photo-electrons, helps vacuum
Courtesy: C. Garion
Taking into account vacuum requirements, overall cryogenic efficiency and power consumption of the accelerator, the synchrotron radiation has to be absorbed at 50 K
Copper coating as in the LHC
… it might not be good enough for the FCC-hh

## Slide 7: Impedance basics
Image charges flow on the surface of the beampipe and produce wakefields
The wakefields potential is proportional to surface impedance
Power dissipation from wakes is where is a summation of over the bunch frequency spectrum
Wakefields have an effect on beam stability, in particular the transverse plane
Risetime of resistive-wall instability depends on the surface impedance
with at the frequency of the unstable mode
Transverse mode-coupled impedance (TMCI) limits the maximum
bunch intensity, also linked to the surface impedance

## Slide 8: Normal metals in the local limit
Vdc
S=a2
d

## Slide 9: Two-fluids model
Frequency independent
Perfect metals:
Superconductors:
Density of “super-electrons”
Normal metals:

## Slide 10: Superconductors in the local limit
From BCS theory, for
When

## Slide 11: Expected performance
Surface resistance at zero Hrf and zero Bext
M. Hein, “High-Temperature Superconductor Thin Films at Microwave Frequencies”, Springer
HTS can have surface resistance lower than Cu
at T< 77 K and 0 T
f < 10 GHz
Sundaresan et al. , IEEE TRANS. APPL. SUPERCOND. 13 (2003) 2913
Tc ~100 K
Tc ~120 K

## Slide 12
From: Ruggero Vaglio

## Slide 13: Fluxon motion in RF
Gittleman and Rosenblum:
Phys Rev. Lett. 16, 734 (1966)
J. Appl. Phys. 39, 2617(1968)
At B0>>Bc1 repulsion forces between fluxon lines are higher with respect to the pinning forces. The fluxon array feels a periodic force of the form:
Chart: 
d
If (small amplitude oscillations)

## Slide 14: Fluxon motion in RF
The rigid fluxon lattice behaves as an harmonic damped oscillator
with
if m=0
Solving for v0:
with
“depinning frequency”
Marcon, Fastampa, Giura, Silva:
Phys Rev. B, 43, 2940 (1991)

## Slide 15: Surface impedance: effect of magnetic flux
For HTS the effect of a field B>>Bc1 is dominating over intrinsic properties
S. Calatroni, R. Vaglio submited to IEEE Trans. Appl. Supercond.
Depinning frequency 0 1÷100 GHz from literature on HTS.

## Slide 16: Surface resistance: effect of magnetic flux
Flux flow regime
No flux flow
Flux flow and dissipation depend on pinning strength and frequency
Properties can be calculated in principle on the basis of standard DC transport measurments

## Slide 17: Surface resistance: effect of magnetic flux
0 = 5.8 GHz at 1.06T, 0 = 2.9 GHz at 16T
Bc2 = 65 T
 = 50 µΩcm
Surface impedance Z of YBCO compared to Cu at 50 K
1.06 T magnetic field
16 T magnetic field
Transport measurements: J. Fleiter and A. Ballarino, “Parameterization of the critical surface of REBCO conductors”, priv. comm. And https://edms.cern.ch/document/1426239/2

## Slide 18: HTS films requirements for beam screen: FCC
Beam screen of ~30mm diameter.
Assuming a film thickness / skin depth of 1 µm the HTS material should have a critical current density
Jc of about 25 kA/cm2 (2.5x108 A/m2) at 50 K and 16T
In this conditions it must have a
surface impedance better than copper in the needed frequency range
Instantaneous current at a fixed point
8-cm bunch frequency spectrum

## Slide 19: Material choices
Data from:
Nature 414, 368-377 (15 November 2001)
High-Tc superconducting materials for electric power applications
David Larbalestier, Alex Gurevich, D. Matthew Feldmann & Anatoly Polyanskii
Superconductor Science and Technology, Volume 11, Number 8
Synthesis and properties of fluorine-doped Tl(1223): bulk materials and Ag-sheathed tapes
E Bellingeri, R E Gladyshevskii, F Marti, M Dhallé and R Flükiger
Courtesy: E. Bellingeri

## Slide 20: Comparison: Y-123, Bi-2223, Tl-1223
Susanne Tönies, Harald W. Weber, Gerhard Gritzner, Oliver Heiml, and Mario H. Eder,
IEEE TRANSACTIONS ON APPLIED SUPERCONDUCTIVITY, VOL. 13, NO. 2, JUNE 2003

## Slide 21: Comparison table
 | YBCO | Tl1223
PROs | Safe Very high Jc Very high steep Hirr Proven technology on tapes (IBAD, …) | High Tc High Jc High Hirr Very tolerant for out stoichiometry Substrate-tolerant (Ag coating)
CONs | Strong weak link problems Lower Tc Very sensitive to stoichimetry Substrate is critical | Toxic Weak link?
Courtesy: E. Bellingeri

## Slide 22: Challenges for HTS coatings
YBCO and Tl-based HTS are the only possible candidates
How to obtain good quality HTS inside tube geometry
  Considerable experience exists in coated tape production for YBCO, scalability to tubes is extremely challenging
  Tl-based HTS has characteristics similar to YBCO, and should allow full scalability to tubes thanks to electrodeposition on silver (coated) substrates

## Slide 23: Collaboration on Tl-based HTS
CERN has started a Collaboration with CNR-SPIN and TU Wien in the frame of the FCC to develop Tl-based coatings
Scope of the collaboration is focussed on identifying a coating process scalable to the full beam screen
FCC frame allows for fundamental R&D on materials with possible outcomes outside the primary goal (e.g. coated conductors for magnets)

## Slide 24: WP highlights (future work)
WP2 (CNR-SPIN): explore precursors preparation, produce policrystalline films and identify suitable production route for thick Tl-HTS films
Courtesy: E. Bellingeri

## Slide 25: c-axis texture on untextured Ag

## Slide 26: Collaboration on YBCO-based HTS
CERN has signed a Collaboration with ICMAB, IFAE and ALBA (Barcelona) in the frame of the FCC to develop a beam screen design based on Coated-Conductors (HTS tapes)
Scope of the collaboration is focussed on identifying ways of using existing high-performance HTS tapes for manufacturing the beam screen
Three-years time-frame to address all manufacturing questions and their impact on SC properties
Development of an RF test station for samples in high magnetic field

## Slide 27: Barcelona proposal
Courtesy: T. Puig, F. Perez

## Slide 28: Outlook
Strong motivation for HTS coatings for FCC beam screens, with potential of drastically reducing beam impedance.
Tl-1223:
  Promising performance, might open up >100 K temperature window
  Scalable coating -> R&D with CNR-SPIN and TU Wien
YBCO:
  Proven performance
  Challenging to coat inside beam screens, need forming technology -> R&D with ICMAB-ALBA-IFAE
Coating properties need extensive experimental validation, for any specific coating process.

## Slide 30: Transverse impedance
F. Sacherer in: Proceedings of the First Course of the International School of Particle Accelerators, CERN 77-13, p. 198

## Slide 31
TlxBa2CayCuy+1Oz
Site | Tlx | Ba2 | Cay | Cuy+1 | Oz
Stoichiometry | X=1 o 2 | 2 | Y=0,1,2 | Y+1=1,2,3 | Z=5…10
Substitution | Pb,Bi,Cu,Hg | Sr | Tl | NONE | F

## Slide 32: Y-123 vs Tl-2212

## Slide 33: Non-linearities