## Slide 1: Dynamic Vacuum Challenges for Heavy Ion Accelerators
Markus Bender

## Slide 2: Swift heavy ion-induced desorption
Dynamic vacuum

## Slide 3: Desorption yield measurements
sample holder
ion gauge
sector valve
RGA
conductance
collimator
from
accelerator
TMP
TSP
IP
10-7 mbar
10-10 mbar
10-8 mbar
TMP
current
transformer
ion gauge
Experiments by: M. Bender, A. Krämer,
H. Kollmus (GSI), E. Mahner (CERN) 2003
desorption yield out of
pressure increase:
(short single pulse, no pumping)
time dependent:
(continuous bombardment)

## Slide 4: What we measure...
scrubbing
Continuous bombardment
1Hz, 91010 ions/pulse
Single shot
91010 ions/pulse
1.4 MeV/u C2+  Al, perpendicular incidence
time [min]
total pressure increase [mbar]

## Slide 5: Review of heavy-ion induced desorption data
PRST-AB 11, 104801 (2008)
Courtesy Edgar Mahner
Notes: We wanted to investigate the material that was irradiated to find a relation between the amount and composition of desorbed gas and the material.

## Slide 6: Scaling: Electronic Energy Loss
C, Cr and Pb -> stainless steel, calculated using the CMEE library
neff [mol./ion]
measurement
1900
300
10
dE/dx
[MeV cm2/g]
46250
19520
3270
(dE/dx)2
normalized
1900
338
9.5
Pb
Cr
C
H. Kollmus, M. Bender, E. Mahner, et al., JVST A 27 (2009)

## Slide 7: Material Investigation with ERDA
element-specific depth profiling up to ~ 1mm resolution few nm
 How are the target properties correlated to the desorption?
(surface property, bulk purity, oxidation...)
Sample Characterization
Desorption Yield Measurement
RGA
Detector
Xe
Sputter
Source
Beam
à
Feed Through
Faraday Cup

## Slide 8: Contents of Stainless Steel
O
0 nm
180 nm

## Slide 9: Desorbed Gas ≠ sputtered Oxide Layer
fluence [particles/cm2]
desorption
oxide layer
6.5E14 mol/cm2 ~ 1ML
H. Kollmus, M. Bender, W. Assmann, et al., Vacuum 82 (2008)

## Slide 10: Material Dependence
Cu2O  insulator:
poor el. & th. conductivity
h~1530 (Proj: 1.4MeV/u Xe)
mainly CO, H2, CO2 for both samples
Cu  conductor:
free electrons moderate energy load
h~350 (Proj: 1.4MeV/u Xe) mainly H2
concentration [%]
oxidized copper
metallic copper
+ acid treatment
depth [nm]
depth [nm]
M. Bender, H. Kollmus, W. Assmann, Nucl. Inst. Meth. B 256 (2007)

## Slide 11: Oxidation Prevention
Rhodium coating
  no oxide layer (noble metal)
  less diffusion
  lower energy loss dE/dx
  measured yields: ≳ 1000 (1.4 MeV/u Xe)
Gold coating
  no oxide layer (noble metal)
  diffusion into copper
  high energy loss dE/dx
  measured yields: h ≲ 200 (1.4 MeV/u Xe)

## Slide 12: Summary of Experimental Results
Desorbed gas is not the sputtered impurities of the material
Desorbed gas is always CO, CO2 and H2
  Also the contents of the residual gas
Link to the substrate
  Insulators (Cu2O) desorb more than conductors
Higher temperature bakeout of loss regions reduces desorption
  At 350°C highest CO desorption
Thermal moderated surface process with link to the substrate
  Desorption = release of weakly bound surface adsorbats
  Transient overheated spot drives the release
  (dE/dx)2-scaling

## Slide 13: “Cure” for the dynamic vacuum
beam loss collimator
  Gold coated OFHC-copper
    Ni diffusion barrier
  in-situ bake out of the loss sections minimize the desorption
    while cooling down from the UHV bake out collimator is kept at higher temperature
beam
dipole
collimator
heater
pump

## Slide 14: ”Cure“ for the dynamic vacuum

## Slide 15: Idea of thermal moderated Desorption
inelastic
Thermal
Spike Modell
projectile ion loses energy
(mainly to the electronic system)
electrons carry energy away
from the ion track
the hot electrons transfer the energy
to the lattice by e-p coupling
thermal desorption due to
enhanced surface temperature
nuclear collisions
How can 1 ion trigger the desorption of some 100 gas molecules?

## Slide 16: The inelastic Thermal Spike Model
Solving the equations: radial time dependant temperature distribution
Electronic Subsystem:
Lattice System:

## Slide 17: Temperature of the Electrons
time [s]
radius [nm]
temperature [K]
(1.4MeV/u XeCu)

## Slide 18: Temperature of the Lattice
time [s]
radius [nm]
temperature [K]
(1.4MeV/u XeCu)

## Slide 19: Thermal Desorption
M. Bender, H. Kollmus, M. Toulemonde, et al., Nucl. Inst. Meth. B 267 (2009)

## Slide 20: Desorbed Molcules
time [s]
radius [nm]
desorbed molecules
radial function, integral over 2p
(1.4MeV/u XeCu)

## Slide 21: Some Numbers
Collision System | experimental value | model value 1 ML; 0,4 eV; 1,5 e -
1,4 MeV/u Xe  Cu | 290...360 | 185
1,4 MeV/u Xe  Au | 90 | 165
1,4 MeV/u Xe  Rh | 1285 | 3400
1,4 MeV/u Xe  Cu2O | 1530 | 10000
1,4 MeV/u C  Cu | 10 | 5
1,4 MeV/u Cr  Cu | 150 | 40
1,4 MeV/u Pb  Cu | 800 | 525
4,2 MeV/u Pb  Au | 800 | 675
M. Bender, H. Kollmus, M. Toulemonde, et al., Nucl. Inst. Meth. B 267 (2009)

## Slide 22: High Intensity on Targets
Spiral2: 5e14 ions per second (S3 @ FISIC)
even with lowest desorption yields (100) and high pumping speed (some 1000 l/s) the system will break down within seconds
AND THE DESORBED GAS WILL BE ACTIVATED!
How to minimize the desorption yield?

## Slide 23: Latest Experiments Ca on Au-Ni-Cu
h = 37500

## Slide 24: LINAC 3 cryogenic target experiment 2009
  Bakeable UHV system with 2 RGA's, 2 BAG's, gas injection system, MTV, linac beam control
  Cryogenic target assembly developed
  Static pressure: low 10-11 Torr
27.9.2009
Courtesy Edgar Mahner

## Slide 25: LINAC 3 cryogenic target assembly 2009
Cryogenic targets:  141 mm, mounted on a cold-head, 2 samples tested: bare Cu and Au/Cu
Temperature control: 3 sensors (PT100, RhFe, Si diode) + 2 heaters (25 W)
Cu radiation shield: electro-polished outside, coated inside. Lowest target temperature achieved: 6.3 K
Assembly with bare Cu target and instrumentation feedthroughs
Ions: Pb54+ @ 4.2 MeVu,
Impact angle:  = 0°
Intensity: 1.1-1.5109 ions/pulse
Targets: bare Cu, Au/Cu
Target temp.: 300, 77, 6.3 K
4.9.2009
3.9.2009
3.9.2009
E. M. et al. PRST-AB 14, 050102 (2011)
Courtesy Edgar Mahner

## Slide 26
LINAC 3 pressure rises and desorption yields
Au/Cu target at 300, 77, 6.3 K
Pb54+ (4.2 MeV/u),  = 0
E. M. et al. PRST-AB 14, 050102 (2011)
Courtesy Edgar Mahner

## Slide 27: LINAC 3 temperature and CO gas adsorption Desorption yields for Au/Cu and Cu
Both targets have a factor of 18 lower desorption yield at 6.3 K compared to the 300 K value.
Experiments have shown, for the first time, that the heavy-ion induced desorption yield is temperature-dependent.
10 ML
1 ML
E. M., L. Evans, D. Küchler, R. Scrivens, M. Bender, H. Kollmus, D. Severin, M. Wengenroth, PRST-AB 14, 050102 (2011)
Courtesy Edgar Mahner

## Slide 28: “Our Expectation": 1 Monolayer
T: Cryo

## Slide 29: “Our Expectation": few Monolayers
T: Cryo

## Slide 30: “Our Expectation": many Monolayers
T: Cryo
K (Ice), C (Ice), ...
?

## Slide 31: Conclusion and Outlook
Ion-induced desorption is still a topic in new accelerator facilities
Dedicated studies needed:
  Cryogenic surfaces (coverage, temperature,...)
  Room temperature (contribution of diffusion from unbaked targets)
Surface and bulk investigations needed
   ERDA for concentration of light elements
   XPS for oxides / carbides
Enhance existing model to cryogenic temperatures and diffusion

## Slide 32: Conclusion and Outlook
Vaccum diagnostic
Flange or window
Cooled apperture
Sample 
Cooling /Heating
Turbo pump
UHV-Pump
IZ, TSP
Bypass-
valve
Electron-gun
keV-sputter-gun

## Slide 33: Conclusion and Outlook

## Slide 34: Acknowledgement
GSI: H. Kollmus, A. Warth, L. Bozyk, D. Severin, C. Trautmann, A. Gumberidze
CERN: E. Mahner
IRFU: M. Authier, O. Cloue, A. Drouard
INSP: E. Lamour, S. Mace, C. Prigent, D. Vernhet, S. Steydli
CIMAP: P. Rousseau, M. Toulemonde
GANIL: C. Stodel, R. Levallois
LMU: W. Assmann
HSRM: F. Völklein