## Slide 1: Challenges of vacuum chambers with adjustable gap for SC undulators
C. Boffo, Th. Gerhard, M. Turenne, W. Walter; Babcock Noell GmbH
S. Casalbuoni, A. Cecilia, S. Gerstl, A. Grau, T Holubek, C. Meuter, D. Saez de Jauregui, R. Voutta; Karlsruhe Institute for Technology
Beam Dynamics meets Vacuum, Collimators and Surfaces 08-10 March 2017

## Slide 2: Outline
Undulators and SCUs
SCU15 and SCu20
Requirements for the vacuum chamber
Technological solutions
Summary
C. Boffo Beam Dynamics meets Vacuum etc. 8-10 Match 2017

## Slide 3: Babcock Noell GmbH Your best partner of cutting edge development
C. Boffo Beam Dynamics meets Vacuum etc. 8-10 Match 2017

## Slide 4: Undulators Evolution of the spieces
PM
PM
Vacuum chamber
Room temperature (stabilized)
Strongest possible PM
Gap adjustment to modify B
Classical PM
Vacuum chamber
PM
PM
Room temperature
Magnets get closer B increase
Gap adjustment to modify B
In vacuum PM
Vacuum chamber
PM
PM
Temperature ~100 K
Magnets get cooled B increase
Gap adjustment to modify B
Cryo PM
C. Boffo Beam Dynamics meets Vacuum etc. 8-10 Match 2017
Vacuum chamber
SC
SC
Vacuum chamber
Temperature ~4 K
Higher fields with SC
Superconducting

## Slide 5: Undulators Motivation
Slide courtesy of KIT
C. Boffo Beam Dynamics meets Vacuum etc. 8-10 Match 2017

## Slide 6: SCUs Main parameters
 | SCU15 | SCU20 | Units
Period length | 15 | 20 | mm
Full periods | 100.5 | 75.5 | 
Max field on axis 7 mm gap | 0.73 | 1.18 | T
Nominal current | 150 | 390 | A
Ramp to nominal current | 450 | 300 | s
Operating gap | 7 | 7 | mm
Injection gap | 15 | 15 | mm
Beam heat load | 4 | 4 | W
Design temperature | 4.2 | 4.2 | K
Iron formers
NbTi superconductor
Tight tolerances <50 um on key dimensions
Movable gap
Cold corrector coils for minimization of field integrals
Conduction-cooling design
C. Boffo Beam Dynamics meets Vacuum etc. 8-10 Match 2017

## Slide 7: SCU15 The device
Mover system
Adjusting feet
Cryostat
RF bellow
Cryocoolers
Coils
Beam pipe
Thermal shield
C. Boffo Beam Dynamics meets Vacuum etc. 8-10 Match 2017

## Slide 8: Requirements for the vacuum chamber A dream project for an engineer
Thermal
    Beam heat load of 4W (plus conductive and radiative loads) would require at least 3 cryoccolers to operate at 4.2K
    Provide cooling along the vacuum chamber
    Minimize length of warm to cold transition (impact on active length of undulator)
Mechanical
    Minimize thickness (reduce difference between magnetic and beam gap)
    Flat center area of at least 300 mm ( magnet width to minimize magnetic roll off)
    Sustain differential pressures in both directions of 1 bar (during installation or failure)
    Movable gap between 7 and 15 mm (flexible elements are required)
    Taper between 7 mm to standard 32 mm warm ANKA beam pipe height
Beam
    Internal copper coating to reduce surface resistance
    Integration of cold BPM
    Integration of cold RF bellows (compensation for cooldown shrinkage)
C. Boffo Beam Dynamics meets Vacuum etc. 8-10 Match 2017

## Slide 9: First generation vacuum chamber Concept
Liner
Beam
Magnet
Magnet
Cooling circuit B
Cooling circuit A
RF Bellow
BPM
50 K
Magnet
10 K
Minimization of difference between beams stay clear 7 mm and magnet gap 8 mm
Formed 0.3 mm 316L foil as chamber (leaves 0.2 mm distance to magnet)
Only 20 mm center straight with smooth angle to provide space for cooling
Magnet
GAP
C. Boffo Beam Dynamics meets Vacuum etc. 8-10 Match 2017
Cooling provided by copper elements soft soldered to the foil
Beam shifted 2.5 mm toward inside of chamber to reduce beam heat load
Lateral spring elements to provide flexibility to open and close gap
RF bellow sustain temperature gardients between 300 and 50 K

## Slide 10: SCU15 vacuum chamber Technological development
Forming of stainless steel foils with high precision and small angles (elastic limit)
Coating of internal and external surfaces with galvanic deposited copper (measured RRR 190)
Laser welding of the chamber
Soft soldering of cooling elements
Ultrasonic cleaning of the full chamber (Al, SST316L and Copper)
Bake out at 120 C for 12 hours
C. Boffo Beam Dynamics meets Vacuum etc. 8-10 Match 2017

## Slide 11: SCU15 vacuum chamber Qualification and performance
S. Casalbuoni et al., Superconducting Undulator Workshop, Didcot, UK, 2014
Vacuum <5*E-10 mbar static
<5*E-9 mbar dynamic
Leak rate < 5*E-10 mbar l s
C. Boffo Beam Dynamics meets Vacuum etc. 8-10 Match 2017

## Slide 12: Operation in the ANKA ring Beam lifetime
S.Casalbuoni et al., ASC2016
Beam lifetime not affected with SCU15 in the ring and in operation.
C. Boffo Beam Dynamics meets Vacuum etc. 8-10 Match 2017

## Slide 13: SCU20 vacuum chamber Improvements and results
Position of the 50 K temperature level after the taper
Magnets width reduced so that the vacuum chamber cross section can be reduced
Taper inside cryostat 7 mm to 15 mm and outside cryostat from 15 mm to 32 mm (reduced heat load)
RF bellow does not see temperature gradient
No cold BPM
C. Boffo Beam Dynamics meets Vacuum etc. 8-10 Match 2017
Vacuum <5*E-10 mbar
Leak rate < 1*E-10 mbar l s

## Slide 14: RF Bellows Design comparison
Warm
Cold
Warm
Cold
CF75
CF100
Fingers
Clips
support
Bellow
C. Boffo Beam Dynamics meets Vacuum etc. 8-10 Match 2017

## Slide 15: Summary
Designing a flexible vacuum chamber for superconducting undulators is challenging
SCU15 demonstrated that the required performance can be achieved
Design improvements for the SCU20 vacuum chamber focused on manufacturability and reproducibility
C. Boffo Beam Dynamics meets Vacuum etc. 8-10 Match 2017

## Slide 16: Thank you for your attention
If you want the best insertion device
for your light source
CONTACT US
We will deliver your SCU in 24 months