## Slide 1: Radiation damage caused by neutron capture in boron doped silicon pixel sensors
ADvanced
MOnolithic
Sensors for
Benjamin Linnik, Tobias Bus,
Michael Deveaux, Dennis Doering, Ali Yazgili for the CBM-MVD collaboration
27.3.2017
Institut für Kernphysik, Goethe University, Frankfurt am Main

## Slide 2: What is the task and why MAPS can do it?
Study matter at extreme conditions by reconstructing secondary vertices of dileptons and open charm particle
Need:
Good spatial resolution
High granularity
Vacuum compatible design
Radiation tolerant
Low material budget
MAPS:
CMOS sensors have low material budget
Excellent spatial resolution
Good time resolution
Radiation tolerant

## Slide 3
MVD
(Micro Vertex Detector)

## Slide 4: How do we test for radiation hardness?
Damage in pure silicon can be rescaled with the NIEL model
By definition a 1 MeV neutron has a hardness factor of 1
NIEL is correct for pure silicon
Neutron energys below 20 keV are often considered neglectable
Sensors are often irradiated for test purposes with higher energetic neutrons only
…BUT

## Slide 5: Is the NIEL hypothesis valid for P-doped sensors?
15µm
10-40µm
50µm
particle
CMOS Monolithic Active Pixel Sensors
Are being optimized to tolerate extremely high radiation doses (ionizing and non-ionizing).
Based typically on P-doped silicon
=> Contains Boron
Boron (10B) is known to:
Capture thermal neutrons with huge cross section (~1000 b)
Decay n+10B => 7Li + 4He + 3 MeV
Fast ions are created in Si
Additional bulk damage is created
Does 10B cause sizable additional radiation damage w.r.t standard NIEL model?
Boron

## Slide 6: Theoretical estimate
http://www.nndc.bnl.gov/sigma/getPlot.jsp?evalid=14969&mf=3&mt=107&nsub=10
(Natural) Boron doping [1/cm³]
Neutron flux [n/cm²]
Energy dependent
cross section
+
Boron decays [1/cm³]
Decay energy
+
Energy deposit [J/cm³]
Most energy deposit ionizing.
How to get NIEL?
Notes: Doping, boron decay cross section high at low energay

## Slide 7: From ion energy to NIEL
Idea: Compare number of vacancies:
caused by fission ions (unknown hardness factor)
caused by protons (known hardness factor)
Tool: SRIM (software and references: www.srim.org)
Simulates flight of ions in matter (~MeV energies)
Simulate vacancies cause by p, 4He and 7Li
Results:
 | Vacancies
p (30 MeV) | 0.7 / 40µm
4He | 277 / ion
7Li | 613 / ion
40µm Si target: Avoid energy loss
=> const. hardness factor
Notes: Read alout whats written there

## Slide 8: Result after normalization:
1 neq
CPS Sensitive layer
P++, substrate
1017/cm³
Si dominated
10B dominated
10B – fission => additional radiation damage in highly doped structures

## Slide 9: Does boron decay additionally damage the sensor?
P-Well
~3 µm
~ 7 µm
SiO2
P++
P-Epi (sensitive)
P++ Substrate
N-Well
In first order:
Lowly doped sensitive volume not affected
Ions are created in highly doped volumes.
~ 7 µm
~ 3 µm
Penetration depth of ions (SRIM)
He
Li
Likely:
Only part of sensitive volume affected
„Effective“ hardness factor depending on sensor geometry, etc...
Possible damage mechanism:
Ions are created in P++
Ions enter sensitive volume, create sizable (?) damage here

## Slide 10: How do we test for additional damage?
MEDAPP
Direct 235U fission neutrons
99% of all neutrons >100 keV
FRM II, Garching
PGAA
Cold neutrons 1.8 x 10-3 eV
Sensor: MIMOSA-19, IPHC, Strasbourg
Design: AMS 0.35 LR, Year 2006
Pixel: 12 µm pitch
Doping assumption:
=> Not depleted, charge collection by diffusion
Idea: Compare radiation damage caused by fast and cold neutrons
9.5µm
Observables: Charge collection efficiency

## Slide 11: What are our results on the additional damage?
Sensor illuminated with 109Cd (22.1 keV X-ray), detect clusters
Summed charge of 4 pixels
Expected: CCE shrinks with irradiation (1 MeV neutrons)
Not expected: CCE increases with
irradiation (Cold neutrons)
Response differs fundamentally between cold  1MeV Neutrons
Effective hardness factor cannot be extracted

## Slide 12: Experimental results: CCE
Only hits in depleted volume
-------- Ignore this region ---------
(noise, X-ray fluorescence etc.)
Gain increases after irradiation
Decrease of diode capacity?
More depletion?
Number of entries increases after irradiation by factor x2.
Scales with depleted volume
More depletion!
Less doping
Abrupt flat junction (?):
Doping decreases by factor x4
Potential explaination:
Intense acceptor removal (factor x4 from P=1015/cm³)
Additional depletion improves CCE, dominates trapping
! No significant acceptor removal observed with 1 MeV neutrons for <2x1013neq/cm²
Preliminary!

## Slide 13: Summary and cautious conclusion
Does 10B fission cause sizable rad. damage in P-doped Si?
Theoretical estimate:
P>1017/cm³ => Expect additional damage w.r.t standard NIEL curve
Fission ions may damage lowly doped silicon indirectly due to 7µm range
Experimental study (MIMOSA-19, ~1015/cm³ epi layer, ~1019/cm³ substrate ):
Observation:
CCE:
  Cold neutrons cause strong acceptor removal, CCE increases
  Acceptor removal exceeds finding for 2x1013neq/cm² (1MeV)
Preliminary conclusion:
10B fission seems to cause rad. damage beyond standard NIEL
Risk of unexpected effects in case of high thermal neutron doses.