## Slide 1
Radiation hardness of fully depleted
CMOS Monolithic Active Pixel Sensors
Tobias Bus, Benjamin Linnik, Michael Deveaux
ADvanced
MOnolithic
Sensors for
Notes: Hey gays,

## Slide 2: MAPS – Monolithic Active Pixel Sensors
The CBM-MVD
MimoSIS design goals:
 | MIMOSIS – Expected performance
CMOS Process | Tower/Jazz 0.18 µm Quad-Well
Pixel dimensions | 30.1 x 26.9 µm²
Spatial resolution | ~ 5µm
Material budget | 50 µm Si (0.05 % X0)
Radiation tolerance | > 3Mrad (@-20°C). > 3x1013neq/cm²

## Slide 3: MAPS – Monolithic Active Pixel Sensors
Reset
+3.3V
+3.3V
Output
SiO2
SiO2
SiO2
N++
N++
N+
P+
P-
P+
15µm
50µm
Notes: Übergang verbessern zu dieser Folie. Um Ergebnisse zu verstehen Funktionsweise. E-Feld einführen.-

## Slide 4: Effects of non-ionizing radiation
e-
Defects due
to radiation
Diode
Non-ionizing radiation
Energy deposition into the crystal
e-
e-
Readout
Readout
Trapping & recombination
of signal electrons
Leakage current → higher noise
Cooling decreases this effect
Particle
Detecting layer
Depleting the sensor allows to accelerate the charge collection.
=> More radiation tolerance.
Notes: Defect states in the crystal structure Absorption nicht, recombination and generation centers. Singalladung verlieren, Thermische rauschen als effektals
One major weak point of CMOS sensors regarding non-ionizing radiation is the slow diffusion of charge as non-ionizing radiation creates defects in the epitaxial layer, which become recombination centres for the signal electrons. After recombination, signal electrons become unavailable for the charge collection. If the charge is collected trough diffusion, it has a longer path until it is collected in the diode and therefore a higher chance of being absorbed before detected.

## Slide 5: Pipper – 2: A fully depleted HR-MAPS
Standard pixel
Pipper - 2
Issue:
Standard CMOS restricted to few volts
=> Too few for full depletion.
Analysis:
Restriction due to transistor gates.
Diodes and metal lines tolerate higher
voltages.
Approach:
Use AC-couping to separate vulnerable
transistors from HV on diode.
Depletion voltage up to 40V possible.
Apply to 22x22 µm2 pixels.

## Slide 6: Standard sensor – Test results
Fe-55
Epi-layer
Depleted volume
Depleted volume
Epi-layer
Standard sensor – Only few hits from depleted volume.
Other hits: Reduced amplitude (charge sharing).

## Slide 7: Pipper – 2 – Test results
Hits mostly in depleted volume peak.
No modification for >20V => indicator for full depletion

## Slide 8: Vllt keine zeit dafür?
Epi-layer
Depleted volume
Depleted volume
20V
Standard sensor
Pipper - 2

## Slide 9: Test with 90Sr beta rays
T = -55° C | Signal MPV (e) | Avg. noise (e) | S/N
1013neq/cm2 | 1290 | 23.19 | 55.6
5·1014neq/cm2 | 860 | 27.48 | 31.3
1290e
860e
S/N (Sr-90) >15  typically > 99% MIP - efficiency
Notes: Zeit lassen beim erkären.
Plots erklären, Charge Spektrum erklären. MPV,.

## Slide 10: Summary and conclusion
This work
Radiation tolerance (MIMOSA-series)
A CMOS sensor allowing for
40V depletion voltage in Tower/Jazz 0.18µm has been built and tested.
Results suggest full depletion.
Laboratory tests suggest tolerance to >5 x 1014 neq/cm².
(Remaining S/N>30 if cooled).