## Slide 1
High rate time of flight system
for FAIR-CBM
International conference on technology and instrumentation in particle physics, May 22-26,
Beijing
  Wang Yi for CBM-TOF group
Department of Engineering Physics, Tsinghua University

## Slide 2
  Introduction on FAIR and CBM-TOF
Structure of CBM-TOF
Development of low resistive glass
Design of strip-MRPC and pad-MRPC
Beam test @GSI and SPS
Conclusions
Outline

## Slide 3
The phase diagram of strongly interacting matter

## Slide 4
SIS100/300
SIS18
HESR
CR
Compressed Baryonic Matter
Super Fragment-Separator:
Nuclear Structure and Astrophysics
Anti-Proton Physics
p-Linac
100 m
FAIR phase 1
FAIR phase 2
Atomic, Plasma, Applied Physics
Facility for Antiproton and Ion Research
Primary Beams
1012/s; 1.5 GeV/u; 238U28+
1010/s 238U73+ up to 35 GeV/u
3x1013/s 30 GeV protons
Secondary Beams
range of radioactive beams up to 1.5 - 2 GeV/u; up to factor 10 000 higher in intensity than presently
antiprotons 3 - 30 GeV

## Slide 5
Time of Flight
Projectile
Spectator
Detector
DAQ/FLES HPC cluster
(SIS100)
Dipol
Magnet
Silicon
Tracking
System
Micro
Vertex
Detector
Ring
Imaging
Cherenkov
Transition
Radiation
Detector
(SIS100)
Muon
Detector
(SIS100)
Layout of CBM detector

## Slide 6
The structure of CBM-TOF wall
CBM-ToF Requirements
Full system time resolution sT ~ 80 ps
Efficiency > 95 %
Rate capability  30 kHz/cm2
Polar angular range 2.5°– 25°
Occupancy < 5 %
Low power electronics
(~100.000 channels)
Free streaming data acquisition
Au+Au, Center, 10AGeV
Simulated with CBM ROOT

## Slide 7
MRPC
2
3
Optic (~50m)
CBM CLK (40MHz)
ToF CLK (160MHz)
MRPC
MRPC
MRPC
ToF SYNC Signal
Counting-Room
CAVE
Example for 192 Channel
Electronics & Readout chain

## Slide 8
Padi8
GET4
FPGA - TDC
TOF electronics

## Slide 9
Precision between two channels
PADI X & GET4 V1.23
below 30ps
below 30ps
below 30ps
Pulser test of PADIX & GET4

## Slide 10
The voltage drop in the gas gap:
Two main ways to improve rate capability:
Reducing bulky resistivity of electrode glass (CBM)
Reducing the avalanche charge (ATLAS)
Other methods:
Reducing the thickness of glass
Warming the detector
The smaller the voltage drop, the higher efficiency and higher rate capability!
How to increase rate of MRPC

## Slide 11
Development of low resistive glass
Performance of the glass
Glass mass production
Yield >100m2/month
Aging test with X-ray source
Online test system. The efficiency and time resolution can be obtained by cosmic ray while irradiated by X-rays. 0.1C/cm2 charge is accumulated in 35 days.

## Slide 12
Rate: 70kHz/cm2
Time resolution: 40 ps
Rate capability of high rate MRPC
Even though the rate is 70kHz/cm2, the efficiency is still higher than 90% and the time resolution is about 80ps.
Test results at Nuclotron, Dubna

## Slide 13
Prototype design for CBM-TOF
Strip-MRPC
Inner zone-MRPC

## Slide 14
14
14
Glass: low resistive glass
0.7mm thick, 27cm x 25cm
Strip: 27cm x 0.7cm, 0.3cm interval, 24 strips
Gas gap: 8 x 0.25mm, two stacks
Gas box: 600mm x 500mm x 72mm
Design of strip-MRPC for high rate region
Differential strip: 7mm wide+3mm interval
h
w
t
ground
Feed trough: Micro-strip, 50Ω

## Slide 15
15
15
Experimental Setup:
Particle trajectory
Buc-2013
THU-Pad
Buc-Ref
PMT
HD-Ref
Beam time in October 2014 at GSI
1.1 GeV 152Sm beam On 0.3mm/4mm/5mm Pb target
Flux rate several hundreds Hz/cm2
THU-Strip
HD-P2
BEAM
Beam test @GSI, Oct.2014
Particle trajectory

## Slide 16
16
High rate test in February 2015 at SPS CERN
13 GeV Ar beam
Flux rate around 1kHz/cm2
Buc-2013
THU-Pad
Buc-Ref
PMT
HD-Ref
THU-Strip
HD-P2
Experimental Setup:
USTC
Up setting
Down setting
Beam test @ SPS Feb 2015

## Slide 17
The data analysis is based on CBM ROOT, macro developed by TOF Group.
Analysis Procedure: 3 Main Steps.
1
Unpacking
2
Cluster Building
3
Analysis
Converting LMD files into unpacked ROOT file, containing timing, TOT, super module type, super module, RPC, strip, side information of each hit.
Initial calibration: Align center of each strip in Detector Under Test and Reference Detector.
Iterative calibration: Calibrate data in time-walk, gain and velocity correction.
Build calibrated hits into clusters.
Calculating observables from fully calibrated hits include cluster size, time resolution and efficiency.
Data analysis method

## Slide 18
Calibration method
Time-walk correction
Gain correction
Strip alignment correction
Velocity correction
Large signals arrive at discriminator threshold faster, leading to a dependence of measured time and amplitude of the analogue signal.
Amplification gain of PADI varies between each channel, which should be corrected out to get initial amplitude for time-walk correction.
Different cable length and electronic delay lead to the shifting of calculated center of different strip, influencing the position of hits.
Slower particles need a longer time to cross the distance between Dut and Mref, widen the time difference distribution.

## Slide 19
19
Analysis Setting:
Particle
Lower part of setup:
Diamond
THU-Strip
HD-Ref
BRef:
Starting counter for events.
Dut:
Counter under test.
MRef:
Reference measure for Dut.
Analysis Procedure:
Init_calib.sh (Initial calibration)
Iter_calib.sh (Iterative calibration)
  iteration procedure: 1-6-8-2-10-2-10
Iter_hits.sh (Analysis)
  analysis correction procedure: 1-2-3-4-1
Cut Selection: Cut 1
tofAnaTestbeam->SetMul4Max(1.);
tofAnaTestbeam->SetCh4Sel(8.);
tofAnaTestbeam->SetDCh4Sel(7.); tofAnaTestbeam->SetPosY4Sel(0.5);
tofAnaTestbeam->SetMulDMax(1.); tofAnaTestbeam->SetDTDia(0.);
Analysis results: GSI Oct 2014

## Slide 20
Run: Sun1205 – 5500V: Analysis Process
Before Calibration
After Calibration
Time-walk correction
Velocity correction

## Slide 21
Run: Sun1205 – 5500V Time Resolution
Threshold | Efficiency | Time Resolution | Cluster Size
170mV | 97.0% | 71.6ps | 1.7
180mV | 97.0% | 68.9ps | 1.7
190mV | 97.0% | 71.0ps | 1.6
200mV | 96.7% | 68.9ps | 1.6
Analysis Result under Different Threshold
Efficiency:
Around 97%
Time resolution:
Around 70ps
Results of strip-MRPC

## Slide 22
Performance of Inner zone-MRPC

## Slide 23
CBM components | TDR approved | Start production | Ready for installation | Ready for beam
Micro Vertex Detector (MVD) | 01.04.17 | 30.04.18 | 31.12.19 | 30.06.20
Silicon Tracking System (STS) | 05.07.13 | 31.03.17 | 31.03.20 | 31.12.20
Ring Imaging Cherenkov Detector (RICH) | 07.01.14 | 31.12.16 | 31.12.19 | 31.12.20
Muon Detector (MUCH) | 28.02.15 | 31.12.16 | 31.12.19 | 31.12.20
Transition Radiation Detector (TRD) | 01.04.17 | 31.12.17 | 31.12.20 | 31.12.21
Time of Flight System (TOF) | 30.04.15 | 01.01.17 | 31.12.19 | 31.12.20
Electromagnetic Calorimeter (ECAL) | 31.12.16 | 30.06.18 | 31.12.19 | 31.12.20
Projectile Spectator Detector (PSD) | 28.02.15 | 31.12.15 | 31.12.18 | 31.12.19
Dipol Magnet | 01.10.13 | 30.06.17 | 31.12.19 | 30.06.20
Online Systems (DAQ and FLES) | 31.12.17 | 30.06.18 | 30.06.19 | 31.12.19
CBM mile stones

## Slide 25
Summary
The rate of CBM-TOF reach 25kHz/cm2
Time resolution ~60ps
Free running mode
120 square meters
It will first used in STAR-eTOF
Mini CBM will be set up soon!
Participate FAIR Phase 0
experiments…
Structure of Mini CBM

## Slide 26
Thanks for your attention !