## Slide 1: Evaluation of Innovative Cooling Concepts with High-Performance Carbon Materials for Vertex Detectors operated in Vacuum
Daniela Mijatovic
IKF University Frankfurt
This work has been supported by BMBF (05P15RFFC1), GSI and HIC for FAIR
DPG Frühjahrtagung in Bochum 2018

## Slide 2: Outline
Motivation
Convective and Conductive Cooling
The Sensor Carrier
The Experimental Setup
Performance Measurement
Summary

## Slide 3: Motivation The Micro Vertex Detector MVD

## Slide 4: Motivation The Micro Vertex Detector MVD
Task
Tracking of charged particles in fixed target set-up
Precise determination of secondary decay vertices of short lived particles (50 - 70 µm along beam axis)
Requirements
  Close to the target
  High radiation hardness
  Low material budget and vacuum operation
    Actively cooled sensors
MVD
Low Material Budget
Efficient Cooling
Inside the acceptance
Outside the acceptance
Convective cooling with heat sink
Conductive cooling with high performance sensor carrier

## Slide 5: The Sensor Carrier Thermal Pyrolithic Graphite TPG
Mechanical Stable
Excellent heat conductivity in-plane (1600 W/mK)
Thin
CVD Diamond is used for St. 1 and 2

## Slide 6: Convective and Conductive Cooling within one Quadrant
Convective Cooling:
Liquid cooled Al-heat sink
Conductive Cooling:
Sensor carrier clamped to the heat sink (TPG)
Heat-sink balcony
Acceptance

## Slide 7: Convective and Conductive Cooling The Quadrant
Liquid cooled Al-heat sink
Micro Cables
50µm thin sensor
prototypes
(test placing, bonding, gluing)
Sensor Carrier (TPG)

## Slide 8: Convective and Conductive Cooling Heat Flow
2. Heat transferred by conduction over the sensor carrier
1. Sensors produce heat (200 – 500 mW/ )
3. Sensor carrier is clamped to the Al- heat sink
4. Cooling liquid circulating inside the heat sink transfers the heat by convection

## Slide 9: Convective and Conductive Cooling Heat Flow
2. Heat transferred by conduction over the sensor carrier
1. Sensors produce heat
3. Sensor carrier is clamped to the Al- heat sink
4. Cooling liquid circulating inside the heat sink transfers the heat by convection
Can be achieved by materials with a very high heat conductivity

## Slide 10: The Experimental Setup
Goal:
Measuring thermal performance with infrared (IR) thermography of sensor carriers in vacuum for quantitative evaluation
IR Camera: VarioCAM head HiRes 640
IR advantages:
Contactless temperature measurement
High resolution spatial temperature profile
needs
A standardized test setup

## Slide 11: The Experimental Setup
AIR
VACUUM
Measured object
Ge window (coated)
IR Camera + lens
IR measuring point
X
Bolometer
array
2 cm
24 cm
X
Pt 100 sensors

## Slide 12: The Experimental Setup
VACUUM
Measured object
Ge window coated
IR Camera + lens
X
Measuring point
X
Bolometer
array
X
X
Al-heat sink
Sensor carrier TPG
AIR
IR Image
Kapton Heater by OMEGA LUX
(heat load 790 )
(Backside)

## Slide 13: Experimental Setup Calibration
Many parameters influences the measurements. That is why Pt100 sensors were used as reference measurement and calibration
The calibration is not universal
  A continuous re-calibration is necessary
Absolut temperature is not need to evaluate the thermal performance of a material

## Slide 14: Thermal Performance Measurement
The thermal performance was characterized by analyzing heat-up curves of TPG with different thicknesses ( and 500 )
1st Notice:
Thickness of the material effects strongly the end temperature and heat distribution
2nd Notice:
Curves can be described with an exponential function
[K]

## Slide 15: Thermal Performance Measurement
The thermal performance was characterized by analyzing heat-up curves of TPG with different thicknesses ( and 500 )
2nd Notice:
Curves can be described with an exponential function
Heat equation:
[K]

## Slide 16: Thermal Performance Measurement Single exp. Fit
Fit range
Fitting the heat- up curves during the first 15 seconds with
T(t) =
t = 15s
[K]

## Slide 17: Thermal Performance Measurement Two-Term exponential Curve Fit
Fitting the complete heat up curve with
a two-term exponential curve fit:
T(t) =
[K]

## Slide 18: Thermal Performance Measurement Single and Two-Term in Comparison

## Slide 19: Thermal Performance Measurement Three-Term exponential Curve Fit
Fitting the complete heat up curve with a three-term exponential curve fit:
T(t) =
[K]

## Slide 20: Thermal Performance Measurement Fits in Comparison for TPG 254 µm

## Slide 21: Thermal Performance Measurement Fits in Comparison
The relaxation time is connected to the heat conductivity.
A short relaxation time is an indicator for a high heat conductivity.
describes relaxation time of the sensor carrier (TPG)
gives information about the contact between carrier and heat sink
gives information about thermal performance of the heat sink
Fits | Time range [s] | [s] | [s] | [s]
Single Fit | 13.2 | 4.69 0.04 | XX | XX
Two Term Fit | 175 | 4.48 0.03 | 34.17 0.23 | XX
Three Term Fit | 175 | 3.65 0.04 | 54.59 2.23 | 14.92 0.67
Fits | Time range [s] |  |  | 
Single Fit | 13.2 |  | XX | XX
Two Term Fit | 175 |  |  | XX
Three Term Fit | 175 |  |  | 
[K]

## Slide 22: Thermal Performance Measurement Fits in Comparison for TPG 254 µm
 | 14.87 0.01
 | 8.23 0.11
 | 4.14 0.08
 | 2.78 0.14
T(t) =

## Slide 23: Summary
Established Experimental Setup with IR Thermography:
Setup too complex to achieve reliable absolute values without calibration.
Empiric calibration with a reference measurement (Pt100) is not universal.
Reliable results achievable with continuous recalibration.
Measurement of Thermal Performance with IR Thermography:
Thermal performance of TPG was evaluated.
An analytic function was used to fit our measurements.
  Single exponential Fit fits the best to the data but to understand the whole system a two / three term fit is necessary

## Slide 24: Backup

## Slide 25: The Compressed Baryonic Matter Experiment
Fixed-target experiment
High energy: 11AGeV
Nucleus-Nucleus & Proton-Nucleus collision: very high interaction rate: 100kHz / 1MHz
Research goals:
  Open Charm
  Di-Leptons
  Multi-strange-particles
CBM

## Slide 26: The Cooling Concept The Quadrant
Liquid cooled Al-heat sink
Micro Cables
50µm thin sensor
prototypes
(test placing, bonding, gluing)
Sensor Carrier (TPG)
One Quadrant

## Slide 27: The Cooling Concept
Valves for Stations
Flow Meters
Pump
Huber CC-405
One Quadrant

## Slide 28: The Sensor Carrier Thermal Pyrolithic Graphite TPG

## Slide 29: Calibration
Aspects that could influence the measurement:
Window between vacuum chamber and camera
Temperature of the window
Ambient Light
Shiny Surfaces (reflections) with low emissivity
Software settings
  Emissivity
Reflection of the chamber

## Slide 30: Thermal Performance Measurement Single exp. Fit
Fit range
Fitting the heat- up curves during the first 15 seconds with
T(t) =
t = 15s
[K]

## Slide 31: Thermal Performance Measurement Single and Two-Term in Comparison

## Slide 32: Thermal Performance Measurement Fits in Comparison
describes relaxation time of the sensor carrier (TPG)
gives information about the contact between carrier and heat sink
gives information about thermal performance of the heat sink
Fits | Time range [s] | [s] | [s] | [s] |  |  |  | 
Single Fit | 13.2 | 4.69 0.04 | XX | XX | 11.25 0.04 | 11.87 0.02 | XX | XX
Two Term Fit | 175 | 4.48 0.03 | 34.17 0.23 | XX | 14.73 0.04 | 9.85 0.03 | 4.96 0.03 | XX
Three Term Fit | 175 | 3.65 0.04 | 54.59 2.23 | 14.92 0.67 | 14.87 0.01 | 8.23 0.11 | 2.78 0.14 | 4.14 0.08
Fits | Time range [s] |  |  |  |  |  |  | 
Single Fit | 13.2 |  | XX | XX |  |  | XX | XX
Two Term Fit | 175 |  |  | XX |  |  |  | XX
Three Term Fit | 175 |  |  |  |  |  |  | 

## Slide 33: Thermal Performance Measurement Single exponential Fit
Fit range
Fitting the heat- up curves during the first 15 seconds with
 | Time [s] |  | Covarianz | Chi-Square
TPG 254 um | 13.2 | 4.6968 | 0.0416 | 0.0059
TPG 500 um | 15.0 | 3.7837 | 0.0074 | 0.0861
 | Time [s] |  | Covarianz | Chi-Square
TPG 254 um | 13.2 | 4.6968 | 0.0416 | 0.0059
TPG 500 um | 15.0 | 3.7837 | 0.0074 | 0.0861
t = 15s
The short relaxation times describe the excellent thermal performance of TPG (heat conductivity =1600 W/mK)

## Slide 35: The Experimental Setup
AIR
VACUUM
Measured object
Ge window coated
IR Camera + lens
IR measuring point
X
Bolometer
array
2 cm
24 cm
X
Pt 100 sensors