## Slide 1: Materialforschung für Beschleuniger
M. Bender* and C. Trautmann,
MAT
* m.bender@gsi.de

## Slide 2: Next generation accelerators: pushing the limitis of the technically feasible
LHC
MAX IV
FAIR
Spiral 2
HIAF
FRIB
ESS
FCC
…
2010
2020
2035
2025
Performance increase:
Higher energy
Higher intensity / luminosity
Pulsed beams
Cryogenic structures
Technical challenges for
Power
Radiation
Timing
Data
Materials (construction & operation)
Cryo
Vacuum
…

## Slide 3: Technical challenges: Radiation hardness of beam exposed materials
mA - A beam current
1012 U s-1
130 kJ / bunch
365 MJ total
T = 2K
P = 10-12 mbar
SFRS target
Stripper foils
Collimators
Beam dumps

## Slide 4: Online test methods, monitoring systems
Problems:
Beam monitoring on target and beam catchers
How to predict and localize failure
In extreme operation conditions
In high radiation fields
  Targets
  Beam catcher
data
calc.
Thermal imaging
Laser vibrometer
Eddy current
Possible monitor systems to be tested:

## Slide 5: New (old) methods
Acoustic emission monitoring:
LHC collimators (D. Deboy, CERN)

## Slide 6: Pressure pulses & shock waves
DT = 200 K
Dt = 50 µs
5x1014 i/cm2 1014 i/cm2 1013 i/cm2 5x1012 i/cm2
radiation damage  swelling
stress waves  compression
stress concentrators + fatigue  crack
Graphite target / Pulse structure | Maximum compressive stress (MPa) | Maximum tensile stress (MPa)
45 µm (single pulse) | -53.3 | 0.5
45 µm (double pulse) | - 56.4 | 0.7
Finite element simulations

## Slide 7: Offline test methods, e.g. degradation of thermal properties
Thermal simulation shows cooling problem with radiation-damaged graphite: - degradation of thermal diffusivity: 70-40 W/(m K) -> 15 W/(m K)
Laser flash analysis of irradiated graphite

## Slide 8: New materials
Figure of merit for materials resistance to ion beam-induced thermal stress
CFC
graphite

## Slide 9: Dynamic vacuum instabilities

## Slide 10: Investigation of dynamic outgassing
Vacuum diagnostic
Flange or window
Cooled aperture
Sample 
Cooling /Heating
Turbo pump
UHV-Pump
IZ, TSP
Bypass-
valve
Electron-gun
keV-sputter-gun
TDS setup operating as standard analysis tool
Additional electron source installed for ESD
Investigation of different materials, treatments and coatings, to find low-desorbing materials
Amount of desorbed gas as function of thermal properties, purity and thickness of coating

## Slide 11: Joint research to reduce outgassing channels
bulk diffusion
surface diffusion
desorption
Ion
e-
h

## Slide 12: Conclusion
Due to extreme conditions, materials research is important for next generation accelerators
  Combined radiation, heat, pressure
  Transient processes, pulsed impact
Evolution of new reliable materials in progress
Development of monitoring systems to predict lifetime of materials or detect material failure
Vacuum problematic largely understood
  Startup of database for materials & treatments
Thin film coatings
  NEG getters for vacuum performance
  aC for low secondary electron yields
Thank you for your attention!